Supporting Information

Cu-doped SnO2/rGO nanocomposites for ultrasensitive H2S detection under low temperature

Tingting Chen1,2, Jianhai Sun1 ,*, Ning Xue 1, Wen Wang3, Kaisheng Jiang 1,2, Tianye Zhou1 ,2, Hao Quan 1,2

1 State Key Laboratory of Transducer Technology, Aerospace Information Research Institute, Chinese Academy of Sciences, Beijing 100194, China.

2 School of Electronic, Electrical and Communication Engineering, University of Chinese Academy of Sciences, Beijing 100049, China.

3 State Key Laboratory of Acoustics, Institute of Acoustics, Chinese Academy of Sciences, Beijing 100190, China.

Corresponding Author

* Prof. J. Sun - E-mail: sunjh@aircas.ac.cn

Figure S1. SEM patterns of rGO and Cu-SnO2/rGO-2.

Figure S2. XRD patterns of samples: (a) pure SnO2 and Cu-SnO2-(1-4), (b) pure SnO2, Cu-SnO2-2, and Cu-SnO2/rGO-(1-3). The right side shows the corresponding enlarged views of (110) and (101) peaks.

Table S1. Recent literature about H2S sensors based on SnO2.

| Sensing Materials | Temp. [℃] | Con. [ppm] | Res. a) | Res./Rec. time [s] | LOD [ppb] | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Cu-SnO2/rGO | 120 | 10 | 1415.7 | 120/15 | 50 | This work |
| Cu-SnO2 | 180 | 100 | 25.3 | 10.1/42.4 | 10 | [1] |
| Nb2O5/SnO2 | 275 | 20 | 4 | 20/97 | 1 [ppm] | [2] |
| SnO2-CuO | 200 | 5 | 1395 | 5.27/- | 1 [ppm] | [3] |
| ZnO-SnO2 | 350 | 1 | 317 | ~10/450 | 100 | [4] |
| Co,N-GQDs/SnO2 | 260 | 100 | 37.3 | 3/13 | 50 | [5] |
| Si/SiO2 | 100 | 50 | 3.5 | - | 10 [ppm] | [6] |
| CNTs/SnO2/CuO | RT | 50 | 400 | 4/10 [min] | 10 [ppm] | [7] |
| WO3-coated SnO2 | 200 | 1 | 177 | - | 100 | [8] |
| SnO2@ZnO NW | 250 | 1 | 6.24 | 14/39 | 1 [ppm] | [9] |
| a-SnO2 | 250 | 1 | 2.4 | 540/- | 210 | [10] |
| LLTO-SnO2 | 260 | 30 | 19 | <1/60 | 500 | [11] |
| CuO-SnO2 | 125 | 10 | 1056 | - | - | [12] |

Table S2. Peak position to peak area ratio for three oxygen species in O1s of pristine SnO2, Cu-SnO2-2 and Cu-SnO2/rGO-2.

| Materials | Absorbed oxygen (Oabs) |  | Oxygen vacancy (Ov) |  | Lattice oxygen (Olat) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Binding energy [eV] | Peak area [%] | Binding energy [eV] | Peak area [%] | Binding energy [eV] | Peak area [%] |
| Pristine SnO2 | 532.2 | 10.5 | 531.0 | 27.0 | 530.4 | 62.5 |
| Cu-SnO2-2 | 532.2 | 13.3 | 531.1 | 31.1 | 530.5 | 55.6 |
| Cu-SnO2/rGO-2 | 532.1 | 20.0 | 531.0 | 27.4 | 530.5 | 52.6 |

Figure S3. (a) UV-vis diffuse reflectance spectrum and (b) Kubelka-Munk function curve plotted against photon versus the energy of absorbed light of pristine SnO2, Cu-SnO2-2, and Cu-SnO2/rGO-2. The relationship between (αhv)2 and photon energy hv is obtained according to the formula (αhv)2 = A (hv-Eg), where α, A, h and v are the absorption coefficient, absorption constant, Plank constant and light frequency, respectively. The bandgap of pristine SnO2, Cu-SnO2-2, and Cu-SnO2/rGO-2 are 3.70, 3.65, and 3.56 eV, respectively.

Reference

- Zhang, S., et al. Facile fabrication of a well-ordered porous Cu-doped SnO2 thin film for H2S sensing. ACS Appl. Mater. Interfaces 6, 14975-14980 (2014).

- Mao, L. et al. Excellent long-term stable H2S gas sensor based on Nb2O5/SnO2 core-shell heterostructure nanorods. Appl. Surf. Sci. 602, 154339 (2022).

- Park, K. R. et al. Design of highly porous SnO2-CuO nanotubes for enhancing H2S gas sensor performance. Sens. Actuators B Chem. 302, 127179 (2020).

- Phuoc, P. H. et al. Comparative study on the gas-sensing performance of ZnO/SnO2 external and ZnO–SnO2 internal heterojunctions for ppb H2S and NO2 gases detection. Sens. Actuators B Chem. 334, 129606 (2021).

- Chen, T. et al. Co, N-doped GQDs/SnO2 mesoporous microspheres exhibit synergistically enhanced gas sensing properties for H2S gas detection. J. Mater. Chem. A 10, 10759 (2022).

- Bang, J. H. et al. Porous Si/SnO2 nanowires heterostructures for H2S gas sensing. Ceram. Int. 46, 604-611 (2020).

- Zhao, Y., Zhang, J., Wang, Y. & Chen, Z. A highly sensitive and room temperature CNTs/SnO2/CuO sensor for H2S gas sensing applications. Nanoscale Res. Lett. 15, 1-8 (2020).

- Hoa, T. T. N. et al. Highly selective H2S gas sensor based on WO3-coated SnO2 nanowires. Mater. Today Commun. 26, 102094 (2021).

- Zhu, L. et al. Hierarchical highly ordered SnO2 nanobowl branched ZnO nanowires for ultrasensitive and selective hydrogen sulfide gas sensing. Microsyst. Nanoeng. 6, 1-13 (2020).

- Paolucci, V. et al. Bidimensional Engineered Amorphous a-SnO2 Interfaces: Synthesis and Gas Sensing Response to H2S and Humidity. ACS Sens. 7, 2058-2068 (2022).

- Li, X. et al. Mechanism of enhanced H2S sensor ability based on emerging Li0.5La0.5TiO3-SnO2 core-shell structure. Sens. Actuators B Chem. 352, 131054 (2022).

- Chen, Z., Xu, Z. & Zhao, H. Flame spray pyrolysis synthesis and H2S sensing properties of CuO-doped SnO2 nanoparticles. Proc. Combust. Inst. 38, 6743-6751 (2021).