Development of coal fly ash modified graphite-polyurethane composite electrodes for the determination of Cd(II) in batteries and water

Caio Ribeiro de Barros1, Priscila Cervini1, Rafael Martos Buoro1, 
Elizabet M. van der Merwe2 and Éder T. G. Cavalheiro1*

Supplementary Material

Table S1 Elemental and atomic percentage found at the matrix and modifier regions as determined by EDX

| Element | GPU Matrix |  |  | FA Modifier |  |
| --- | --- | --- | --- | --- | --- |
|  | Element % | Atomic % |  | Element % | Atomic % |
| C | 96.1 | 98.5 |  | ND | ND |
| O | ND | ND |  | 30.9 | 44.5 |
| Mg | <0.1 | <0.1 |  | 1.4 | 1.3 |
| Al | 1.2 | 0.6 |  | 22.2 | 19.0 |
| Si | 1.3 | 0.6 |  | 38.7 | 31.8 |
| K | 0.3 | 0.1 |  | 1.8 | 1.1 |
| Ca | 0.3 | 0.1 |  | 1.3 | 0.8 |
| Fe | 0.6 | 0.1 |  | 3.8 | 1.6 |

*ND = Not Detected

Table S2 TGA/DTG data for the GPU and GPU-FA composites

| Sample | Attribution | Temperature interval / ºC | Mass loss / % |
| --- | --- | --- | --- |
| GPU | Polymer decomposition | 200.45 – 484.9 | 28.4 |
|  | Polymer decomposition | 484.9 – 660.7 | 10.4 |
|  | Graphite combustion | 660.7 – 854.7 | 60.7 |
|  | Residue | 900 | 0.534 |
| GPU-FA 2.5% | Polymer decomposition | 207.9 – 596.4 | 35.7 |
|  | Polymer decomposition | 596.4 – 649.4 | 6.09 |
|  | Graphite combustion | 649.4 – 896.6 | 54.7 |
|  | Residue | 900 | 3.53 |
|  | Net Residue* | 900 | 2.99 |
| GPU-FA 5% | Polymer decomposition | 218.6 – 534.0 | 25.45 |
|  | Polymer decomposition | 534.0 – 671.1 | 14.5 |
|  | Graphite combustion | 671.1 – 895.7 | 54,7 |
|  | Residue | 900 | 5.37 |
|  | Net Residue* | 900 | 4.84 |
| GPU-FA 10% | Polymer decomposition | 213.4 – 597.6 | 30.8 |
|  | Polymer decomposition | 597.6 – 633.5 | 4.64 |
|  | Graphite combustion | 633.5 – 885.1 | 53.4 |
|  | Residue | 900 | 10.9 |
|  | Net Residue* | 900 | 10.4 |

*Net Residue: GPU-FA residue measured at 900 ºC – GPU residue at 900 ºC

Table S3 Values of parameters obtained from EIS spectra for GPUE and GPUE-FA 5% (m/m)

| Simulated parameters | GPUE | GPUE-FA 5%a |
| --- | --- | --- |
| RS / Ω | 29.3 | 79.4 |
| R1 / Ω | 91.8 | 122 |
| R2 / Ω | 27.1 | - |
| W1 / 10-3 S s(1/2) | 0.819 | 1.38 |
| W2 / 10-3 S s(1/2) | 0.293 | - |
| G (Ka) / s-1 | 307.1 | - |
| G (Y0) / 10-3 S s(1/2) | 0.508 | - |
| CPE1 / 10-6 S sN | 12.9 | 134 |
| CPE2 / 10-6 S sN | 39.4 | 5.42 |
| N (CPE1) | 0.869 | 0.62 |
| N (CPE2) | 0.953 | 0.95 |
| 2 / 10-4 | 4.64 | 3.68 |

a 5.0% FA, m/m

Table S4 – Concentration of concomitants in water samples as determined by FAAS

| Water sample Concomitant | Cconcomitant / µmol L-1 |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Artesian Well |  | Mineral |  | Tap |
| Li+ | ND | ND |  | ND |  |
| Na+ | 148 ± 1 | 51.5 ± 0.5 |  | 83.8 ± 0.2 |  |
| Ca2+ | 8.4 ± 0.1 | 19.220 ± 0.003 |  | 6.93 ± 0.04 |  |
| Mg2+ | 67.0 ± 0.4 | 64.8 ± 0.2 |  | 35.2 ± 0.1 |  |
| Fe3+ | ND | ND |  | 4.25 ± 0.09 |  |
| Ni2+ | ND | ND |  | ND |  |
| Pb2+ | ND | ND |  | ND |  |
| Zn2+ | ND | ND |  | 10.16 ± 0.06 |  |

*ND = Not Detected