Syntheses and Electro-catalyzed Hydrogenation from Water of Three Molecular Catalysts Based on Substituted Tetraphenylporphyrin Cobalt(II) Complexes

Zong Wang, Yin Liu, Ting Li, Yong-Zhen He, Yan-Lin Chen, Xin-Yi Jiang, Chun-Lin Ni*,

Le-Min Yang, Wei Liu*

College of Materials and Energy, Institute of Biomaterial, South China Agricultural University, Guangzhou 510642, P. R. China.

Supplementary Materials

Table of context

| 1 | Fig. S1. The above picture shows the IR spectra of the ligands (black lines) and their complexes (red lines) of 1, 2, 3, and 4. The Acvatar 360 FT-IR infrared spectrometer was used to scan and analyze the KBr film in the range of 400-4000cm-1. |
| --- | --- |
| 2 | Fig. S2. The UV-Vis Spectra of the ligands (black lines) and the complexes (red lines) 1(a), 2(b), 3(c) and 4(d). N,N-Dimethylformamide is used as solvent, and the UV-Visible 2550 spectrometer is used to scan in the range of 200-800 nm. |
| 3 | Fig. S3. The LC-MS spectra of complexes 1, 2, 3, and 4 were sequenced. ESI-MS analyses were measured on a AB SCIEXAPI3200, and the chromatographic pure methanol as a solvent. |
| 4 | Fig. S4. (a) CV of H2T(H)PP (0.91 mM) in DMF. (b) CV of H2T(OH)PP (0.88 mM) in DMF. (c) CV of H2T(CN)PP (0.84 mM) in DMF. (d) CV of H2T(COOH)PP (0.76 mM) in DMF. Conditions: 0.10 M [n-Bu4N]ClO4 as supporting electrolyte, glassy carbon working electrode (1 mm diameter). Pt counter electrode. Ag/AgNO3 reference electrode, scan rate 100 mV/s, Ferrocene internal standard (*). |
| 5 | Fig. S5. (a) CVs of complex 3 in different concentration; (b) CVs of 2.79 µM complex 3, showing the variation in catalytic current with pH (scan rate: 100 mV/s). Conditions: 0.25 M phosphate buffered solution at pH 7.0, glassy carbon working electrode (1 mm diameter), Pt wire counter electrode, Ag/AgCl reference electrode. |
| 6 | Fig. S6. (a) CVs of complex 4 in different concentration; (b) CVs of 3.02 µM complex 4, showing the variation in catalytic current with pH (scan rate: 100 mV/s). Conditions: 0.25 M phosphate buffered solution at pH 7.0, glassy carbon working electrode (1 mm diameter), Pt wire counter electrode, Ag/AgCl reference electrode. |
| 7 | Fig. S7. (a) Charge buildup versus time from electrolysis of 4.38 M complex 1 in a 0.25 M buffer (pH 7.0) under a series of applied potentials; (b) Charge buildup versus time from electrolysis of 3.74 M complex 2 in a 0.25 M buffer (pH 7.0) under a series of applied potentials; (c) Charge buildup versus time from electrolysis of 5.36 M complex 3 in a 0.25 M buffer (pH 7.0) under a series of applied potentials; (d) Charge buildup versus time from electrolysis of 5.15 M complex 4 in a 0.25 M buffer (pH 7.0) under a series of applied potentials; (e) charge build versus time from electrolysis of 0.25 M buffer solution (pH=7); all data have been deducted blank. |
| 8 | Fig. S8. (a) GC traces after a 1-h controlled-potential electrolysis at −1.45 V vs Ag/AgCl of 4.38 M complex 1 in 0.25 M phosphate buffer (pH 7.0). A standard of CH4 was added for calibration purposes. (b) Measured (black) and calculated (red) pH changes assuming a 99.13% Faradic efficiency of complex 1 during electrolysis. (the theoretical pH change over time can be calculated by the equation of where I = current (A), t = time (s), F = Faraday constant (96485 C/mol), V = solution volume (0.03 L)). |
| 9 | Fig. S9. (a) GC traces after a 1-h controlled-potential electrolysis at −1.45 V vs Ag/AgCl of 3.74 M complex 2 in 0.25 M phosphate buffer (pH 7.0). A standard of CH4 was added for calibration purposes. (b) Measured (black) and calculated (red) pH changes assuming a 99.6% Faradic efficiency of complex 2 during electrolysis. (the theoretical pH change over time can be calculated by the equation of where I = current (A), t = time (s), F = Faraday constant (96485 C/mol), V = solution volume (0.03 L)). |
| 10 | Fig. S10. (a) GC traces after a 1-h controlled-potential electrolysis at −1.45 V vs Ag/AgCl of 5.36 M complex 3 in 0.25 M phosphate buffer (pH 7.0). A standard of CH4 was added for calibration purposes. (b) Measured (black) and calculated (red) pH changes assuming a 100.4% Faradic efficiency of complex 2 during electrolysis. (the theoretical pH change over time can be calculated by the equation of where I = current (A), t = time (s), F = Faraday constant (96485 C/mol), V = solution volume (0.03 L)). |
| 11 | Fig. S11. (a) GC traces after a 1-h controlled-potential electrolysis at −1.45 V vs Ag/AgCl of 5.15 M complex 4 in 0.25 M phosphate buffer (pH 7.0). A standard of CH4 was added for calibration purposes. (b) Measured (black) and calculated (red) pH changes assuming a 99.0% Faradic efficiency of complex 3 during electrolysis. (the theoretical pH change over time can be calculated by the equation of where I = current (A), t = time (s), F = Faraday constant (96485 C/mol), V = solution volume (0.03 L)). |
| 12 | Fig. S12. (a) Charge buildup versus time from 4.38 M complex 1 in a 0.25 M buffer (pH 7.0) under -1.40 V vs Ag/AgCl. (b) Charge buildup versus time from 3.74 M complex 2 in a 0.25 M buffer (pH 7.0) under −1.40 V vs Ag/AgCl. (c) Charge buildup versus time from 5.36 M complex 3 in a 0.25 M buffer (pH 7.0) under -1.40 V vs Ag/AgCl.(d) Charge buildup versus time from 5.15 M complex 4 in a 0.25 M buffer (pH 7.0) under −1.40 V vs Ag/AgCl. |
| 13 | Eq. S1. The calculation of TOF for complex 1 (DMF) |
| 14 | Eq. S2. The calculation of TOF for complex 2 (DMF) |
| 15 | Eq. S3. The calculation of TOF for complex 3 (DMF) |
| 16 | Eq. S4. The calculation of TOF for complex 4 (DMF) |
| 17 | Eq. S5. The calculation of TOF for complex 1 (buffer, pH 7.0) |
| 18 | Eq. S6. The calculation of TOF for complex 2 (Buffer, pH 7.0) |
| 19 | Eq. S7. The calculation of TOF for complex 3 (Buffer, pH 7.0) |
| 20 | Eq. S8. The calculation of TOF for complex 4 (Buffer, pH 7.0) |

Fig. S1.The above picture shows the IR spectraof the ligands (black lines) and their complexes (red lines) of 1, 2 , 3, and 4. The Acvatar 360 FT-IR infrared spectrometer was used to scan and analyze the KBr film in the range of 400-4000cm-1.

Fig. S2. The UV-Vis Spectra of the ligands (black lines) and the complexes (red lines) 1(a), 2(b), 3(c) and 4(d). N,N-Dimethylformamide is used as solvent, and the UV-Visible 2550 spectrometer is used to scan in the range of 200-800 nm.

Fig. S3. The LC-MS spectra of complexes1, 2, 3, and 4 were sequenced. ESI-MS analyses were measured on a AB SCIEXAPI3200, and the chromatographic pure methanol as a solvent.

Fig. S4. (a) CV of H2T(H)PP (0.91 mM) in DMF. (b) CV of H2T(OH)PP (0.88 mM) in DMF. (c) CV of H2T(CN)PP (0.84 mM) in DMF. (d) CV of H2T(COOH)PP (0.76 mM) in DMF. Conditions: 0.10 M [n-Bu4N]ClO4 as supporting electrolyte, glassy carbon working electrode (1 mm diameter). Pt counter electrode. Ag/AgNO3 reference electrode, scan rate 100 mV/s, Ferrocene internal standard (*).

(a)

Ccomplex 3

(b)

Current (mA)

Fig. S5. (a) CVs of complex 3 in different concentration; (b) CVs of 2.79 µM complex 3, showing the variation in catalytic current with pH (scan rate: 100 mV/s). Conditions: 0.25 M phosphate buffered solution at pH 7.0, glassy carbon working electrode (1 mm diameter), Pt wire counter electrode, Ag/AgCl reference electrode.

Ccomplex 4

(a)

Fig. S6. (a) CVs of complex 4 in different concentration; (b) CVs of 3.02 µM complex 4, showing the variation in catalytic current with pH (scan rate: 100 mV/s). Conditions: 0.25 M phosphate buffered solution at pH 7.0, glassy carbon working electrode (1 mm diameter), Pt wire counter electrode, Ag/AgCl reference electrode.

(b)

(d)

Fig. S7. (a) Charge buildup versus time from electrolysis of 4.38 M complex 1 in a 0.25 M buffer (pH 7.0) under a series of applied potentials; (b) Charge buildup versus time from electrolysis of 3.74 M complex 2 in a 0.25 M buffer (pH 7.0) under a series of applied potentials; (c) Charge buildup versus time from electrolysis of 5.36 M complex 3 in a 0.25 M buffer (pH 7.0) under a series of applied potentials; (d) Charge buildup versus time from electrolysis of 5.15 M complex 4 in a 0.25 M buffer (pH 7.0) under a series of applied potentials; (e) charge build versus time from electrolysis of 0.25 M buffer solution (pH=7); all data have been deducted blank.

Fig. S8. (a) GC traces after a 1-h controlled-potential electrolysis at −1.45 V vs Ag/AgCl of 4.38 M complex 1 in 0.25 M phosphate buffer (pH 7.0). A standard of CH4 was added for calibration purposes 3.62 mL H2 was measured by GC based on CH4. (b) Measured (black) and calculated (red) pH changes assuming a 99.13% Faradic efficiency of complex 1 during electrolysis. (The theoretical pH change over time can be calculated by the equation of  where I = current (A), t = time (s), F = Faraday constant (96485 C/mol), V = solution volume (0.03 L).

（a）

（b）

Fig. S9. (a) GC traces after a 1-h controlled-potential electrolysis at −1.45 V vs Ag/AgCl of 3.74 M complex 2 in 0.25 M phosphate buffer (pH 7.0). A standard of CH4 was added for calibration purposes 3.24 mL H2 was measured by GC based on CH4. (b) Measured (black) and calculated (red) pH changes assuming a 99.6% Faradic efficiency of complex 2 during electrolysis. (The theoretical pH change over time can be calculated by the equation of  where I = current (A), t = time (s), F = Faraday constant (96485 C/mol), V = solution volume (0.03 L).

(a)

(b)

Fig. S10. (a) GC traces after a 1-h controlled-potential electrolysis at −1.45 V vs Ag/AgCl of 5.36 M complex 3 in 0.25 M phosphate buffer (pH 7.0). A standard of CH4 was added for calibration purposes. 5.11 mL H2was measured by GC based on CH4. (b) Measured (black) and calculated (red) pH changes assuming a 100.4% Faradic efficiency of complex 3 during electrolysis. (The theoretical pH change over time can be calculated by the equation of  where I = current (A), t = time (s), F = Faraday constant (96485 C/mol), V = solution volume (0.03 L).

(a)

(b)

Fig. S11. (a) GC traces after a 1-h controlled-potential electrolysis at −1.45 V vs Ag/AgCl of 5.15 M complex 4 in 0.25 M phosphate buffer (pH 7.0). A standard of CH4 was added for calibration purposes. 8.56 mL H2was measured by GC based on CH4. (b) Measured (black) and calculated (red) pH changes assuming a 99.0% Faradic efficiency of complex 4 during electrolysis. (The theoretical pH change over time can be calculated by the equation of  where I = current (A), t = time (s), F = Faraday constant (96485 C/mol), V = solution volume (0.03 L).

Fig. S12. (a) Charge buildup versus time from 4.38 M complex 1 in a 0.25 M buffer (pH 7.0) under -1.40 V vs Ag/AgCl. (b) Charge buildup versus time from 3.74 M complex 2 in a 0.25 M buffer (pH 7.0) under -1.40 V vs Ag/AgCl. (c) Charge buildup versus time from 5.36 M complex 3 in a 0.25 M buffer (pH 7.0) under -1.40 V vs Ag/AgCl.(d) Charge buildup versus time from 5.15 M complex 4 in a 0.25 M buffer (pH 7.0) under -1.40 V vs Ag/AgCl.

Eq. S1 The calculation of TOF for complex 1 (DMF)

Eq. S2. The calculation of TOF for complex 2 (DMF)

Eq. S3. The calculation of TOF for complex 3 (DMF)

Eq. S4 The calculation of TOF for complex 4 (DMF)

Eq. S5. The calculation of TOF for complex 1 (buffer, pH 7.0)

Eq. S6. The calculation of TOF for complex 2 (buffer, pH 7.0)

Eq. S7. The calculation of TOF for complex 3 (buffer, pH 7.0)

Eq. S8. The calculation of TOF for complex 4 (buffer, pH 7.0)