Electronic Supporting Information

Friedel-Crafts Acylation of Furan: Development of A Green Process Using Chromium-exchanged Dodecatungstophosphoric Acid: Effect of Support, Mechanism and Kinetic Modelling

Deepak S. Desai+ and Ganapati D. Yadav+*

+Department of Chemical Engineering,

Institute of Chemical Technology,

Nathalal Parekh Marg, Matunga,

Mumbai 400019, India.

E-mail address: gd.yadav@ictmumbai.edu.in; gdyadav@yahoo.com.

Tel.: +91-22-3361-2010. Fax: +91-22-3361-1020.

ORCID

Deepak S. Desai: 0000-0003-1333-562X

Ganapati D. Yadav: 0000-0002-8603-3959

Table of Content

Figure S1. TGA analysis of (a) 20% w/w DTP/K-10, (b) 20% w/w Cr0.66-DTP/K-10.

Figure S2. NH3-TPD pattern of (a) K-10, (b) 20% w/w DTP/K-10, (c) 20% w/w Cr0.66-DTP/K-     10, and (d) reused 20% w/w Cr0.66-DTP/K-10.

Figure S3. SEM images of (a) Fresh 20% w/w Cr0.66-DTP/K-10, and (d) reused 20% w/w Cr0.66-DTP/K-10.

Figure S4. N2 adsorption-desorption isotherms of (a) 20% DTP/K-10 (b) fresh 20% w/w Cr0.66-DTP/K-10 (c) reused 20% w/w Cr0.66-DTP/K-10.

Figure S5. Effect of speed of agitation on conversion of furan: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), catalyst 20% w/w Cr0.66-DTP/K-10, catalyst loading 0.0125 g/cm3, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Figure S6. Effect of catalyst loading on conversion of furan: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), catalyst 20% w/w Cr0.66-DTP/K-10, speed of agitation 1000 rpm, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Figure S7. Plot of initial rate vs. catalytic loading: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), speed of agitation 1000 rpm, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Figure S8. Effect of mole ratio on conversion of furan: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), catalyst loading 0.0125 g/cm3, speed of agitation 1000 rpm, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Table S1. Comparison of earlier literature reports of furan acylation with current work.

Figure S9. Plot of XB vs. time.

Figure S10. Plot of - ln (1 - XB) vs. time.

Figure S11. Plot of ln [M-XB/M(1-XB)] vs. time.

Figure S12. Reusability of the catalyst: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), catalyst 20% w/w Cr0.66-DTP/K-10 catalyst loading 0.0125 g/cm3, speed of agitation 1000 rpm, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Characterization of different catalyst:

Figure S1. TGA analysis of (a) 20% w/w DTP/K-10, (b) 20% w/w Cr0.66-DTP/K-10.

Figure S2. NH3-TPD pattern of (a) K-10, (b) 20% w/w DTP/K-10, (c) 20% w/w Cr0.66-DTP/K-10, and (d) reused 20% w/w Cr0.66-DTP/K-10.

Figure S3. SEM images of (a) Fresh 20% w/w Cr0.66-DTP/K-10, and (d) reused 20% w/w Cr0.66-DTP/K-10.

Figure S4. N2 adsorption-desorption isotherms of (a) 20% DTP/K-10 (b) fresh 20% w/w Cr0.66-DTP/K-10 (c) reused 20% w/w Cr0.66-DTP/K-10.

Optimization of different Reaction Parameters

Figure S5. Effect of speed of agitation on conversion of furan: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), catalyst 20% w/w Cr0.66-DTP/K-10, catalyst loading 0.0125 g/cm3, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Figure S6. Effect of catalyst loading on conversion of furan: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), catalyst 20% w/w Cr0.66-DTP/K-10, speed of agitation 1000 rpm, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Figure S7. Plot of initial rate vs. catalytic loading: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), speed of agitation 1000 rpm, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Figure S8. Effect of mole ratio on conversion of furan: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), catalyst loading 0.0125 g/cm3, speed of agitation 1000 rpm, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Table S1. Comparison of earlier literature reports of furan acylation with current work.

| Sr. No. | Catalyst | Catalyst to furan ratio (wt %) | Reaction temperature (C) | Furan to acetic anhydride (moles) | Time (min) | Solvent | Yield (Ya) % | Conversion of furan, % | Selectivity of 2-acyl furan, % | Reusability | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Ce-B-zeolite | NR | 200 |  |  | solventless | NR | 23 | 99 | NR | (Hoelderich, 1989) |
| 2 | HZSM-5 (19.7) | # | 150 | 1:1 | 180 | solventless | 22.9 | 44.1 | 83 | NR | (Reddy et al. 1998) |
|  | HZSM-5 (30) |  |  |  | 120 |  | 41.7 | 93 | 72 |  |  |
|  | HZSM-5 (280) |  |  |  | 120 |  | 38.8 | 94.2 | 66.6 |  |  |
|  | CeZSM-5 (30) |  |  |  | 180 |  | 29.7 | 65 | 73.8 |  |  |
|  | LaZSM-5 (30) |  |  |  | 120 |  | 32 | 85.8 | 60.5 |  |  |
|  | HY |  |  |  | 120 |  | 13.4 | 58.3 | 37 |  |  |
|  | CeHY |  |  |  | 60 |  | 18.6 | 48.8 | 60.4 |  |  |
| 3 | In(OTf)3 + LiClO4 |  | Ambient temperature |  |  | Nitromethane | 61.2 | NR | NR | NR | (Chapman et al. 2001) |
| 4 | AlCl3 | 30.6 | Ambient temperature | 1:2 | 240 | Nitromethane | 2.5 | NR | NR | NR | (Komoto et al. 2002) |
|  | ZnCl2 |  |  |  |  |  | 37.7 |  |  |  |  |
|  | SnCl2 |  |  |  |  |  | 31.5 |  |  |  |  |
|  | Sn(OTf)2 |  |  |  |  |  | 53 |  |  |  |  |
| 5 | Beta-I zeolite | 73.5 | 40 | 1:2 | 480 | 1,2- Dichloroethane | NR | 40 | 88 | NR | (Kantam et al. 2005) |
|  | Beta-II zeolite |  | 25 |  | 720 |  |  | 26 | 100 |  |  |
| 6 | Zn(OTf)2.6H2O | 10 | Ambient temperature | 1:1.5 | 240 | Nitromethane | 46.4 | NR | NR | NR | (He et al. 2008) |
| 7 | Beta zeolite | 28 | 60 | 1:5 | 120 | solventless | 56.3 | NR | NR | NR | (Álvaro et al. 2009) |
| 9 | H-Beta zeolite | 46 | 60 | 1:5 | 90 | solventless | 87.4 | 99.8 | 100 |  | (Xiong et al. 2015) |
|  |  | 42 | 67 | 1:5 | 126 |  | 88.8 | 100 | 100 | NR |  |
| 10 | UDCaT-5 | 25.6 | 90 | 1:5 | 120 | solventless | NR | 82.1 | 100 | 3 | Unpub. |
| 1 | 20% w/w Cr0.66-DTP/K-10 (Current work) | 9.6 | 50 | 1:5 | 180 | solventless | NR | 88 | 100 | 4 | - |

Ya - the molar yield of 2-acetylfuran, #  - continuous reactor used, NR- not reported

Development of Theoretical Model

Using LHHW mechanism the mathematical model for the various reactions has been  already published by our laboratory (Yadav and Chandan 2014; Rasal et al. 2018; Desai and Yadav 2019), hence the rate equation for acylation can be written as

(a) zero order in both reactants, where the conversion will be linear with time

-dXBdt=kwCB0

-dXBdt=k1w

Where,

k1=kCB0

Integrating above equation the following is obtained,

XB=kt      (Figure S9)

Figure S9. Plot of XB vs. time.

It shows that the zero order kinetics is not valid.

(b) First order or pseudo-first order in acetic anhydride and first order in furan since its concentration is limiting and acetic anhydride is taken in excess (M>1)

-dXBdt=k2KB0(1-XB)(M-XB)

Which on integration gives:

ln(M-XB)M(1-XB)=k2CB0(M-1)t

When M>>1, then equation can be written as a pseudo-first order equation leading to:

-ln(1-XB)=kt   (Figure S10)

Figure S10. Plot of - ln (1 - XB) vs. time.

It also shows that it is not a pseudo-first order kinetics

(c) Second order, first order in each species.

-dXBdt=krC2B0w(1-XB)(M-XB)

This upon integration leads to:

ln(M-XB)M(1-XB)=k1CB0(M-1)t   (Figure S11)

Figure S11. Plot of ln [M-XB/M(1-XB)] vs. time.

Based on preliminary analysis, the Eley-Rideal mechanism was proposed. Here, we consider D (furan), B (acetic anhydride), product E (2-acyl furan), and co-product F (acetic acid).

The first step involves the acetic anhydride (B) adsorption on a catalytic site (S):

CH3C+O  + CH3COOH

(CH3CO)2O  +  H+

kB

(B)

(S)

(BS)

(F)

The rate of chemisorption of B:

-rB=kBCBCs-k'BCBsCF                                                                                (1)

-rB=0 at equilibrium

kBCBCs=k'BCBsCF                                                                                           (2)

Since  KB= kBk'B

CBs=KB CBCSCF

The reaction between chemisorbed BS and D takes place as follows:

(3a)

Considering, the surface reaction between the chemisorbed BS and reactant D as rate limiting step. The rate of acylation of furan based on the conversion of acetic anhydride B is given as:

- dCBdt=kCDCBs                                                                                                 (4)

Substituting CBS in above equation,

- dCBdt=kCDkBCBCSCF=kKBCDCBCSCF                                                                    (5)

The total catalytic site balance can be written as,

Ct=w=KB CBCSCF+Cs                                                                                      (6)

Considering,

CS=w 1 +kBCB /CF                                                                                              (7)

After substituting the value of Cs in Eq. (5)

- dCBdt=kKBwCDCB(CF+ kBCB )=rD= rB                                                                          (8)

CB=CB0 (1-XB)                                                                                             (8a)

CD=CD0- CB0XB=CB0(M-XB)                                                                  (8b)

CF=CB0XB                                                                                                         (8c)

Substituting in terms of XB and integrating Equation 8 with M≠ 1, we get

- ln1-XB-KBM-1-MlnM-XBM= kKB(M-1)wt                   (9)

Here, the values of KBM-1-M was very small nearly equals to -M:

- ln1-XB+M lnM-XBM= kKB(M-1)wt                                           (10)

For M=1,

- ln1-XB+XB(1-XB)= kKBwt                                                                       (11)

Figure 13 (a), 13 (b), 13 (c) for M = 1, 3, 5 respectively shows results.  Using Eq. (3) graphs plotted with respect to time for different temperature and the rate constants were calculated using Polymath 6.0 Software (Table 4).

Reusability of Catalyst:

Figure S12. Reusability of the catalyst: Furan 2.50 g (0.036 mol), acetic anhydride 18.74 g (0.18 mol), catalyst 20% w/w Cr0.66-DTP/K-10 catalyst loading 0.0125 g/cm3, speed of agitation 1000 rpm, temperature 50 ºC, total volume 20 cm3, reaction time 180 min.

Nomenclature

B	Reactant species B, acetic anhydride

BS	Chemisorbed B

D	Rectant species D, furan

E	2-Acyl furan

F	Acetic acid

B0	Concentration of B in bulk liquid phase, (mol cm-3)

CB	Concentration of B, (mol cm-3)

CD	Concentration of D, (mol cm-3)

CF	Concentration of F, (mol cm-3)

k	Reaction rate constant (cm6 mol-1 g-1 s-1)

KB	Adsorption equilibrium constant for B (cm3 mol-1)

M	Mole ratio A to B

w	Catalyst loading (g cm-1)

XB	Fractional conversion of B

REFERENCES

Álvaro VFD, Brigas AF, Derouane EG, (2009) Mild liquid-phase Friedel-Crafts acylation of heteroaromatic compounds over zeolite Beta. J Mol Catal A Chem 305:100–103. https://doi.org/10.1016/j.molcata.2009.02.003

Chapman CJ, Frost CG, Hartley JP, Whittle AJ (2001) Efficient aromatic and heteroatom acylations using catalytic indium complexes with lithium perchlorate. Tetrahedron Lett 42:773–775. https://doi.org/10.1016/S0040-4039(00)02122-5

Desai DS, Yadav GD (2019) Green Synthesis of Furfural Acetone by Solvent-Free Aldol Condensation of Furfural with Acetone over La2O3-MgO Mixed Oxide Catalyst. Ind Eng Chem Res 58:16096–16105. https://doi.org/10.1021/acs.iecr.9b01138

He F, Wu H, Chen J, Su W (2008) Unexpectedly high activity of Zn(OTf)2·6H2O in catalytic Friedel-Crafts acylation reaction. Synth Commun 38:255–264. https://doi.org/10.1080/00397910701750292

Hoelderich WF (1989) Zeolites: Catalysts for the synthesis of organic compounds. Stud. Surf. Sci. Catal. 49, 69–93. https://doi.org/10. 1016/S0167-2991(08)61709-7

Kantam ML, Venkata K, Ranganath S (2005) Friedel – Crafts acylation of aromatics and heteroaromatics by beta zeolite. 225:15–20. https://doi.org/10.1016/j.molcata.2004.08.018

Komoto I, Matsuo J, Kobayashi S (2002) Catalytic Friedel–Crafts Acylation of Heteroaromatics. Top Catal 19:43–47. https://doi.org/10.1023/A:1013829215544

Rasal KB, Yadav GD, Koskinen R, Keiski R (2018) Solventless synthesis of cyclic carbonates by direct utilization of CO2 using nanocrystalline lithium promoted magnesia. Mol Catal 451:200–208. https://doi.org/10.1016/j.mcat.2018.01.012

Reddy PR, Subrahmanyam M, Kulkarni SJ (1998) Vapour phase acylation of furan and pyrrole over zeolites ∗. 54:95–100. https://doi.org/10.1023/A:1019015619247

Xiong Y, Chen W, Ma J, et al (2015) Methods to delay deactivation of zeolites on furan acylation: continuous liquid-phase technology and solvent effects. RSC Adv 5:103695–103702. https://doi.org/10.1039/C5RA16139H

Yadav GD, Chandan PA (2014) A green process for glycerol valorization to glycerol carbonateover heterogeneous hydrotalcite catalyst. Catal Today 237:47–53. https://doi.org/10.1016/j.cattod.2014.01.043