Supporting Information

Figure S1. Phase diagram of Pd-Ru.

Figure S2. TEM image of Pd NPs and the corresponding particle size distribution.

Figure S3. TEM image of Pd4Ru NPs and the corresponding particle size distribution.

Figure S4. TEM image of PdRu NPs and the corresponding particle size distributiont.

Figure S5. TEM image of PdRu4 NPs and the corresponding particle size distribution.

Figure S6. TEM image of PdRu4 NPs and the corresponding particle size distribution.

Figure S7. (a) Mosaic image of Pd4Ru based on the value of each element in outlier matrix with HAADF-STEM image as background. (b) overlapping Pd and Ru elemental distribution in Pd4Ru sample with HAADF-STEM image as background. (c) overlapping Pd and Ru elemental distribution image. (d) Ru elemental distribution image. (e) Pd elemental distribution image.

Figure S8. (a) Mosaic image of PdRu based on the value of each element in outlier matrix with HAADF-STEM image as background. (b) overlapping Pd and Ru elemental distribution in PdRu sample with HAADF-STEM image as background. (c) overlapping Pd and Ru elemental distribution image. (d) Ru elemental distribution image. (e) Pd elemental distribution image.

Figure S9. (a) Mosaic image of PdRu4 based on the value of each element in outlier matrix with HAADF-STEM image as background. (b) overlapping Pd and Ru elemental distribution in PdRu4 sample with HAADF-STEM image as background. (c) overlapping Pd and Ru elemental distribution image. (d) Ru elemental distribution image. (e) Pd elemental distribution image.

Figure S10. Partial radial distribution function (pRDF) in melting process obtained from molecular dynamics simulation. The pRDF evolution curve of Ru-Pd atom pair were highlighted by red rectangle in corresponding PdRu4, PdRu and Pd4Ru models.

Figure S11. The SROs of Pd4Ru, PdRu and PdRu4 model changed with the increasing temperature.

Figure S12. Selected area electron diffraction (SAED) patterns of Pd, Pd4Ru, PdRu, PdRu4, Ru, and Au.

Figure S13. Ring integrated curves from SAED patterns of Pd, Pd4Ru, PdRu, PdRu4, and Ru.

Figure S14. Wavelet-transformed reduced structure function F(Q) (G(r,Q)) of Pd

Figure S15. Wavelet-transformed reduced structure function F(Q) (G(r,Q)) of Pd4Ru

Figure S16. Wavelet-transformed reduced structure function F(Q) (G(r,Q)) of PdRu

Figure S17. Wavelet-transformed reduced structure function F(Q) (G(r,Q)) of PdRu4

Figure S18. Wavelet-transformed reduced structure function F(Q) (G(r,Q)) of Ru

Figure S19. CO stripping curves of Pd, Pd4Ru, PdRu, PdRu4, and Ru.

Figure S20. Cyclic voltammetry curve of Pd, Pd4Ru, PdRu, PdRu4, and Ru in 1 M KOH.

Figure S21. Cyclic voltammetry curve of Pd, Pd4Ru, PdRu, PdRu4, and Ru in 0.1 M H2SO4 with the scanning rate of 50 mV/s and 5 mV/s.

Figure S22. D-band center of surface atoms in Pd and corresponding average d-band center of surface atoms.

Figure S23. D-band center of surface atoms in random Pd4Ru alloy and corresponding average d-band center of surface atoms.

Figure S24. D-band center of surface atoms in random PdRu alloy and corresponding average d-band center of surface atoms.

Figure S25. D-band center of surface atoms in random PdRu4 alloy and corresponding average d-band center of surface atoms.

Figure S26. D-band center of surface atoms in Ru and corresponding average d-band center of surface atoms.

Figure S27. Contour mapping of limiting potential against HBE and OHBE

Figure S28. Ru PDF G(r) fitting by fcc Ru structure.

Figure S29. (a) The curve of value of total area divided by the area of circles in edge against number of pixels in a unit. (b) uncertainty of outlier values changes with the number of pixels on which a unit was predicated.

Figure S30. The force error, energy error and total loss function of Pd4Ru test sets

Figure S31. The force error, energy error and total loss function of PdRu test sets

Figure S32. The force error, energy error and total loss function of PdRu4 test sets

Table S2. Comparison between tafel slope and εd

| Tafel Slope (mV/dec) | εd |
| --- | --- |
| 384 | -1.5046 |
| 107 | -1.59663 |
| 64 | -1.626 |
| 63 | -1.66495 |
| 69 | -1.215 |