SUPPORTING INFORMATION

Dye adsorption revisited: Application of the cationic dye adsorption method for the quantitative determination of the acidic surface groups of nanocellulose materials

Jun Araki†*

†Faculty of Textile Science and Technology, Shinshu University, Tokida 3–15–1, Ueda, Nagano prefecture, 386–8567, Japan

Materials and Methods

Materials and equipment.	Several cellulose starting materials were used. Cotton-derived cellulose powders were obtained by hydrolyzing the absorbent cotton (S Cotton, Suzuran Sanitary Goods Co. Ltd., Nagoya, Japan) using 2.5 M hydrochloric acid, as reported previously (Araki et al. 2001), followed by freeze-drying to obtain fine dry cellulose powders. Wood-derived microcrystalline cellulose (MCC) powders were purchased from Nacalai Tesque Inc. (Kyoto, Japan). Softwood bleached kraft pulp (SBKP) obtained from Alabama pine was donated by Azumi Filter Paper Co. Ltd., Osaka, Japan. Silica gel particles with surface mercapto (–SH) groups (SiliaMetS® Thiol, 1.52 mmol/g, –SH groups) were purchased from Silicycle Inc. (Quebec, Canada). Toluidine blue O (TBO, commercially known as “Basic Blue 17”) was purchased from Tokyo Chemical Industry Co. Ltd. (Tokyo, Japan). The other chemical reagents were purchased from Wako Pure Chemical Industries Ltd. (Osaka, Japan) or Nacalai Tesque Inc. (Kyoto, Japan), unless stated otherwise. An aqueous hydrochloric acid solution (1 mol/L) was prepared by diluting 8.45 mL of commercial concentrated hydrochloric acid up to 100 mL with deionized water. The 10-fold dilution of the 1 mol/L HCl with deionized water yielded 0.1 mol/L aqueous HCl. Deionized water was used throughout the study.

It is quite vital to avoid the uses of any glassware during the measurements because cationic dyes, such as TBO and methylene blue (MB), are appreciably adsorbed onto the negatively charged glass surfaces, affecting the resulting TBO concentrations. Preliminary examinations indicated that storage of the TBO solution with an absorbance of up to 1.0 in glass vials for a few days caused the complete adsorption of the contained TBO molecules and resulted in colorless solutions. The details are explained below. All the pipetting operations were conducted using well-calibrated micro/macropipettes with polypropylene (PP) tips, unless otherwise noted.

Preparation of the TBO solution.	TBO was purified via repeated recrystallization, as reported previously (Pal & Schubert, 1962). First, a stock solution of TBO was prepared as follows. The recrystallized, anhydrous TBO (0.1870 g, 5.0 × 10−4 mol) was stirred with deionized water (50–60 mL) in a Teflon® beaker overnight at room temperature. The resultant solution exhibiting slight insolubilities were filtered off using No. 5B filter paper, followed by dilution using a 100-mL PP volumetric flask to yield an approximately 5.0 × 10−3 mol/L solution. The concentration of this stock TBO solution can be precisely determined by drying small portions (~5 mL) of the solution at 105 °C overnight. The dye solution used for the measurements was prepared by diluting 10 mL of the stock solution, pipetted with a 10-mL PP volumetric pipette, up to 100 mL using a 100-mL PP volumetric flask. The TBO concentration of the obtained dye solution was assumed to be 1/10th of that of the stock solution. The diluted dye and stock solutions were stored in polyethylene (PE) bottles with an inner cap and PTFE liner coating, which were then sealed with Parafilm® and kept in the dark. The dye solution prepared as above and the stock solution can be used for several months.

Preparation of various types of CNWs from different cellulose resources.	Carboxylated cellulose nanowhiskers (CCNWs) with different levels of surface carboxylation were prepared according to a previous study (Araki et al. 2001); fifty grams of absorbent cotton was boiled for 30 min in 500 mL of 2.5 M aqueous HCl, followed by washing with water using filtration, homogenization with a Waring-type blender for 30 min, and repeated centrifugations (1600 G, 5 min) to obtain an aqueous suspension of CNWs without any surface carboxyls. The CNW suspension that was neutralized by dialysis was carboxylated via TEMPO (2,2,6,6-tetramethyl-1-pyperidibyloxy) radical-mediated surface carboxylation (see Araki et al. 2001 for detailed experimental conditions). The degrees of oxidation (i.e., the amount of introduced surface carboxyl groups) were controlled by the amounts of added NaClO. The obtained samples were designated as CCNW5, CCNW20, CCNW50, and CCNW100, and the numbers included in every sample name indicates the weight percentage of added NaClO with respect to the weight of CCNWs in oxidation reaction mixtures.

The suspensions of CNWs and CCNWs were adjusted to a concentration of 5 mg/mL, which was equivalent to 0.5 wt%. The suspensions of CNWs and CCNW100 were further mixed in various volume ratios of 1:4, 2:3, 5:5, 3:2, and 4:1. The carboxyl contents of every mixture were calculated from the separate titration results of CNWs/CCNW100 and every mixing ratio, which were compared with the values obtained via dye adsorption measurements.

The sulfated cellulose nanowhiskers (SCNWs), i.e., CNW samples with different numbers of surface sulfate/carboxyl groups, were prepared via the hydrolysis of the respective cellulose materials (including the aforementioned cotton powders, MCC powders, and SBKP) using 65 wt% sulfuric acid under the conditions summarized in Table 1 in the main text. Subsequently, purification was conducted via repeated centrifugation and dialysis against water to achieve neutrality. The experimental procedure has been described in a previous study (Araki et al. 1998).

The samples containing carboxyl and mercapto groups were prepared by mixing CCNW50 and SiliaMetS® thiol in various mixing ratios, as summarized in Table 2 in the main text.

Dye adsorption protocol 1. Determination of the carboxyl contents in CCNWs.	The protocol includes the application of two separate measurement techniques for the CCNW samples, namely, in deionized water (designated herein simply as “in water”) and in 0.1 M aqueous HCl (designated herein as “pH = 1”). The experiment conducted in water is as follows. A mixture comprising 0.1 mL of the aqueous nanowhisker suspensions of CNWs, CCNWs, or CNW/CCNW (containing 5 mg/mL solid content that was equivalent to approximately 0.5 mg of the nanowhisker solid), 2.9 mL of water, and 2.0 mL of the aforementioned TBO solution was added to a 5-mL PP centrifuge microtube. Subsequently, mixing was conducted using an MMS-100 shaker (EYELA, Tokyo, Japan) at approximately 120 rpm overnight. Although overnight shaking was performed throughout this study, a shaking time of 2 h is sufficient (see the main text for details). The well-shaken samples were centrifuged at 3500 rpm for 10 min, and the obtained supernatant, which contained excess TBO, was precisely diluted by a factor of 10 (e.g., 0.4 mL of the supernatant was mixed with 3.6 mL of water in a PP test tube). The absorbance at 628 nm (Aw) of the diluted supernatant was measured using a Shimadzu UV-2450 UV–Vis spectrometer (Kyoto, Japan) and a pair of quartz cuvettes. The baseline readings were measured using water. The calibration curve for the TBO concentration range of 0–2.5 × 10−5 M (see Figure S1) yielded the molar extinction coefficient of TBO in water (w) as 45312 L/mol·cm, which was comparable with the previously reported values (Pal and Schubert 1962; Vleugels et al. 2017; Fradi et al. 2014; Merrill and Spencer 1948; Wehr et al. 2010). The number of surface anionic groups present under the “in water” conditions (Sw) (mmol/g) was calculated as follows:

Sw=cTBO×2×10-3-Awεw×5×10-2cCNW×v×10-3×103=cTBO×0.2-Awεw×5cCNW×v×104,			(1)

where cTBO is the concentration of the TBO solutions (ca. 5.0 × 10−4 mol/L, which was precisely calculated from the concentration of the TBO stock solution), cCNW is the solid concentration of the CNW, CCNW, or CNW/CCNW mixtures (5.0 mg/mL in the standard protocols), and v is the volume of the nanowhisker suspensions used for a single measurement (0.1 mL in the standard protocols). Because the carboxyl groups herein were the only surface anionic groups, the Sw value calculated using Equation 1 directly corresponded with the carboxyl contents. This protocol, wherein 0.5 mg of the nanowhisker solid content was used, corresponded to the quantification of 0–2.0 mmol/g of surface anionic groups.

The experiments conducted under the “pH = 1” conditions are as follows. 0.5 mL of the aqueous nanowhisker suspensions containing 5 mg/mL of solid content (or a precisely determined value), 0.5 mL of 1 mol/L aqueous HCl, 2.0 mL of water, and 2.0 mL of the TBO measurement solution were mixed in a 5-mL PP centrifuge microtube. Subsequently, shaking was conducted for more than 2 h (as stated above) on a shaker. This was followed by centrifugation, yielding the supernatant, which was then diluted by a factor of 10. The absorbance of the resulting solutions (ApH1) was measured at 628 nm. Baseline readings were obtained using 0.1 M aqueous HCl. Another calibration curve for pH = 1 was plotted separately for the same TBO concentration ranges (see Figure S1); the molar extinction coefficient of TBO for pH = 1 (pH1) was 41751 L/mol·cm. The absorbance measurements and calibration curve plotting must be conducted after mixing the calibration sample at pH = 1 to stand overnight and undergo subsequent centrifugation because the absorbance values were observed to slightly decrease after a series of these procedures was conducted. This phenomenon was only observed in the “pH = 1” samples. The number of surface anionic groups determined for pH = 1 (SpH1) (mmol/g) was calculated according to the following equation:

SpH1=cTBO×2×10-3-ApH1εpH1×5×10-2cCNW×v×10-3×103=cTBO×0.2-ApH1εpH1×5cCNW×v×104			(2)

Dye adsorption protocol 2. Determination of the sulfate/carboxyl contents in SCNWs.	This protocol was identical with protocol 1, wherein two separate experimental conditions could be observed for the SCNW samples, namely, “in water” and “in pH = 1.” However, there was one notable difference; here, the sample amount increased because the sulfate/carboxyl group content in typical SCNW samples was comparatively lower (80–300 µmol/g) than the carboxyl content in CCNWs (1.0–1.8 mmol/g). Thus, large sample volumes were required to eliminate the introduction of errors during the evaluation process. The “in water” experiments were conducted as follows. 0.5 mL of the aqueous SCNW suspensions containing 5 mg/mL solid content (the concentration of the suspension may be arbitrary, but the value should be precisely determined) as 2.0–3.0 mg of the nanowhisker solid, 2.5 mL water, and 2.0 mL of the respective TBO solution were mixed in a 5-mL PP centrifuge microtube. After mixing using a shaker, the supernatant was centrifuged and diluted. The absorbance measurements were performed as stated in Protocol 1 to obtain Aw and Sw (Equation 1). This protocol in which 2.5 mg of the nanowhisker solid content was employed corresponded to the quantification of 0–0.4 mmol/g of surface anionic groups.

The experiments conducted under the “in pH = 1” conditions were similar to those highlighted in Protocol 1. 0.5 mL of the aqueous nanowhisker suspensions with 5 mg/mL of solid content (or a precisely determined value), 0.5 mL of 1 M aqueous HCl, 2.0 mL of water, and 2.0 mL of the respective TBO solution were mixed in a 5-mL PP centrifuge microtube. After shaking using a shaker, the supernatant was centrifuged and diluted. The subsequent absorbance measurements, which were identical to those stated in Protocol 1, were used to obtain ApH1 and SpH1 (Equation 2).

In this protocol, Sw corresponded to the total surface group contents (i.e., the sum of the sulfate and carboxyl groups), whereas SpH1 was linked to the sulfate group contents. The carboxyl contents of the SCNWs were calculated by subtracting SpH1 from Sw.

Dye adsorption protocol 3. Determination of the carboxyl contents in CCNWs in the presence of mercapto groups.	CCNW50 was mixed with SiliaMetS® thiol in various mixing ratios, as summarized in Table 2 in the main text, to obtain different –COOH/–SH ratios. The mixtures were subjected to dye adsorption protocol 1 for carboxyl quantification and titration, as stated below.

Effect of the adsorption time on the calculated carboxyl contents.	0.4 mL of the two CCNW samples (namely, CCNW5 and CCNW100) containing a solid content of 5 mg/mL each, 11.6 mL water, and 8 mL of the respective TBO solution were mixed in two 50-mL PP centrifuge tubes, followed by continuous shaking using a shaker. Next, 2-mL aliquots of the mixture were sequentially pipetted from the two sample mixtures after shaking for 0.5, 1, 2, 4, 6, 8, or 24 h. Every aliquot was centrifuged (6000 rpm, 10 min), and the supernatants that underwent 10-fold dilution were subjected to absorbance experiments, as stated in protocol 1. The apparent carboxyl contents at every adsorption time were recalculated according to the definitions expressed in Equation 1.

pH/conductometric titration.	The surface sulfate/carboxyl groups were also quantified via pH/conductometric titration according to ISO regulations (Johnston et al., 2018) with some minor modifications. Aqueous suspensions of CNWs, CCNWs, or SCNWs, which contained 500–700 mg of the nanowhisker solids, were mixed with 2 mL of 0.1 M aqueous NaCl and 2 mL of 0.1 mol/L aqueous HCl (the latter was not added in the SCNW experiments), followed by dilution with water up to a total weight of 200 g. The samples were titrated using 0.1 mol/L of aqueous NaOH (for the CCNW samples) or 0.01 M NaOH (for the CNW/SCNW samples); a 0.2-mL aliquot of the titrant (0.1-mL aliquot around the neutralization points for higher-resolution results) was added, and the experiment was allowed to continue until the pH/conductivity readings settled. The pH and conductivity of the samples were monitored using SevenCompact Duo S213-meter (Mettler Toledo, OH, USA) equipped with pH and conductivity electrodes (InLab Expert Pro-ISM and Inlab 751-4mm, respectively, Mettler Toledo, OH, USA), and the values obtained were subsequently plotted against the amount of added NaOH after correcting for conductivity by volume (Ragab & Amin, 2004). The titrants were standardized using potassium hydrogen phthalate (Johnston et al., 2018). The carboxyl group contents were determined based on the conductometric titration curves according to a previously reported protocol (Johnston et al., 2018); the contents were determined from the two sharpest inclinations in the pH titration curves corresponding to the inflection points in the conductometric titration curves when the neutralization points and were extremely difficult to determine.

Figure S1. Calibration curves of the TBO absorption values in water and in pH = 1.

References

Araki J, Wada M, Kuga S (2001) Steric stabilization of a cellulose microcrystal suspension by poly(ethylene glycol) grafting. Langmuir 17:21–27.

Araki J, Wada M, Kuga S, Okano T (1998) Flow properties of microcrystalline cellulose suspension prepared by acid treatment of native cellulose. Colloids Surfaces A 142:75–82.

Fradj AB, Lafi R, Gzara L, Hamzaoui AH, Hafiane R (2014) Spectrophotometric study of the interaction of toluidine blue with poly (ammonium acrylate). J Mol Liq 194:110–114.

Johnston LJ, Jakubek ZJ, Beck S, Araki J, Cranston ED, Danumah C, Fox D, Li H, Wang J, Mester Z, Moores A, Murphy K, Rabb SA, Rudie A, Stephan C (2018) Determination of sulfur and sulfate half-ester content in cellulose nanocrystals: An interlaboratory comparison. Metrologia 55:872.

Merrill RC, Spencer RW (1948) Spectral changes of some dyes in soluble silicate solutions. J Am Chem Soc 70:3683–3689.

Pal MK, Schubert M (1962) Measurement of the stability of metachromatic compounds. J Am Chem Soc 84:4384–4393.

Ragab GH, Amin AS (2004) Atomic absorption spectroscopic, conductometric and colorimetric methods for determination of fluoroquinolone antibiotics using ammonium reineckate ion-pair complex formation. Spectrochim Acta Part A: Mol Biomol Spectroscopy 60:973–978.

Vleugels LFW, Ricois S, Voets IK, Tuinier R (2017) Reversal of metachromasy revisited; displacement of Toluidine-blue from alginate by surfactants. Colloids Surfaces A: Physicochem Eng Asp 529:454–461.

Wehr JB, Pax F, Blamey C, Menzies NW (2010) Comparison between methods using copper, lanthanum, and colorimetry for the determination of the cation exchange capacity of plant cell walls. J Agric Food Chem 58:4554–4559.