Supporting Information

Self-Constructed Interface of Co2P/Co3Fe7 Nanoparticles Encapsulated in N-Doped Carbon Nanotubes as Superior Bifunctional Oxygen Electrocatalysts for Rechargeable Zn-Air Batteries

Ailing Feng1 · Liang Liu2 · Peitao Liu1 · Yanqing Zu · Fengbo Han · Xiaodong Li · Shijiu Ding · Yanan Chen

Institute of Physics & Optoelectronics Technology, Baoji University of Arts and Sciences, Baoji 721016, P.R. China

* Corresponding author.

E-mail address: ailingfeng@bjwlxy.edu.cn (A. Feng), liupt@bjwlxy.edu.cn (P. Liu).

Fig. S1 XRD patterns of Co/Co2P@N-C (blue), Co2P/Co3Fe7@N-C-1 (gray), Co2P/Co3Fe7@N-C-2 (green), Co2P/Co3Fe7@N-C (red),  and Co2P/Co3Fe7@N-C-3 (yellow).

Fig. S2 (a) Nitrogen adsorption-desorption isotherms, and (b) pore-size distribution of Co2P/Co3Fe7@N-C.

Fig. S3 ORR LSV curves of Pt/C (purple), Co/Co2P@N-C (blue), Co2P/Co3Fe7@N-C-1 (gray), Co2P/Co3Fe7@N-C-2 (green), Co2P/Co3Fe7@N-C (red),  and Co2P/Co3Fe7@N-C-3 (yellow).

Fig. S4 (a) ORR LSV curves in O2-saturated 1 M KOH with different rotation rates (400-2400 rpm), and (b) the corresponding Koutecky-Levich plots obtained at different potentials for Co/Co2P@N-C.

Fig. S5 (a) ORR LSV curves in O2-saturated 1 M KOH with different rotation rates (400-2400 rpm), and (b) the corresponding Koutecky-Levich plots obtained at different potentials for Co2P/Co3Fe7@N-C-1.

Fig. S6 (a) ORR LSV curves in O2-saturated 1 M KOH with different rotation rates (400-2400 rpm), and (b) the corresponding Koutecky-Levich plots obtained at different potentials for Co2P/Co3Fe7@N-C-2.

Fig. S7 (a) ORR LSV curves in O2-saturated 1 M KOH with different rotation rates (400-2400 rpm), and (b) the corresponding Koutecky-Levich plots obtained at different potentials for Co2P/Co3Fe7@N-C.

Fig. S8 (a) ORR LSV curves in O2-saturated 1 M KOH with different rotation rates (400-2400 rpm), and (b) the corresponding Koutecky-Levich plots obtained at different potentials for Co2P/Co3Fe7@N-C-3.

Fig. S9 (a) OER LSV curves, and (b) the corresponding Tafel curves of  Ir/C (purple), Co/Co2P@N-C (blue), Co2P/Co3Fe7@N-C-1 (gray), Co2P/Co3Fe7@N-C-2 (green), Co2P/Co3Fe7@N-C (red),  and Co2P/Co3Fe7@N-C-3 (yellow).

Fig. S10 EIS of Co/Co2P@N-C (blue), Co2P/Co3Fe7@N-C-1 (gray), Co2P/Co3Fe7@N-C-2 (green), Co2P/Co3Fe7@N-C (red), and Co2P/Co3Fe7@N-C-3 (yellow) for OER.

Fig. S11 The CV curves of (a) Co/Co2P@N-C, (b) Co2P/Co3Fe7@N-C-1, (c) Co2P/Co3Fe7@N-C-2, (d) Co2P/Co3Fe7@N-C, and (e) Co2P/Co3Fe7@N-C-3 in 1 M KOH. (f) The corresponding electrochemical double-layer capacitances.

Fig. S12 Chronoamperometric stability of Co2P/Co3Fe7@N-C and commercial Pt/C for a long-term testing time of 10 h.

Fig. S13 OER polarization curves of Co2P/Co3Fe7@N-C before and after 5000 cycles.

Fig. S14 Chronoamperometric stability of Co2P/Co3Fe7@N-C and commercial Ir/C for a long-term testing time of 10 h.

Fig. S15 OER polarization curves of Co2P/Co3Fe7@N-C before and after 5000 cycles.

Fig. S16 XRD pattern of Co2P/Co3Fe7@N-C after (a) ORR and (b) OER stabilities test.

Fig. S17 Charge-discharge gap curves of Co2P/Co3Fe7@N-C and commercial Pt/C + Ir/C.

Fig. S18 Specific discharging capacity curves at 5, 10, and 20 mA cm-2, and specific capacity was normalized to consume Zn mass.

Fig. S19 The cycling stability of Co2P/Co3Fe7@N-C-based Zn-air batteries at a current density of 10 mA cm-2.

Fig. S20 Liquid zinc-air batteries luminescence test of Co2P/Co3Fe7@N-C as air cathode.

Fig. S21 Photograph of the flexible all-solid-state ZAB (Co2P/Co3Fe7@N-C-based ZAB and Pt/C + Ir/C-based ZAB) showing open-circuit potentials of about 1.4V and 1.38V, respectively.

Fig. S22 Photograph of the button-like all-solid-state ZAB (Co2P/Co3Fe7@N-C-based ZAB and Pt/C + Ir/C-based ZAB) showing open-circuit potentials of about 1.4V and 1.38V, respectively.

Table S1 The various N species contents in the Co/Co2P@N-C and Co2P/Co3Fe7@N-C.

| N-types | Co/Co2P@N-C | Co2P/Co3Fe7@N-C |
| --- | --- | --- |
| Pyridinic-N | 34.8 % | 45.1 % |
| Graphitic-N | 48 % | 41.9% |
| Pyrrolic-N | 17.2 % | 13 % |

Table S2 Comparison of the bifunctional activity of Co2P/Co3Fe7@N-C with some of the previously reported nonprecious catalysts.

| Catalysts | ORR: E1/2 (V) | OER: Ej=10 (V) | ΔE= Ej=10 - E1/2 (V) | Refs. |
| --- | --- | --- | --- | --- |
| Co2P/Co3Fe7@N-C | 0.86 | 1.47 | 0.61 | This work |
| Pt/C+Ir/C | 0.840 | 1.53 | 0.690 | This work |
| Co/Co2P@NCNTs | 0.9 | 1.58 | 0.68 | [1] |
| Co2P@CNF | 0.804 | 1.691 | 0.887 | [2] |
| Co2P/NPG | 0.81 | 1.55 | 0.74 | [3] |
| FeCo/Co2P@NPCF | 0.79 | 1.56 | 0.77 | [4] |
| C/CoFe-30–650 | 0.81 | 1.58 | 0.77 | [5] |
| NPSC-Co2Fe1 | 0.85 | 1.6 | 0.75 | [6] |
| CoFe/N-GCT | 0.79 | 1.67 | 0.88 | [7] |
| FeCo-NCps | 0.84 | 1.60 | 0.76 | [8] |
| FeCo-Nx-CN-30 | 0.88 | 1.67 | 0.79 | [9] |
| CoFe@HNSs | 0.897 | 1.601 | 0.704 | [10] |
| Ni3FeN/NRGO | 0.72 | 1.63 | 0.91 | [11] |
| Ni3Fe/N-C sheet | 0.76 | 1.60 | 0.84 | [12] |
| Co3O4/PGC | 0.68 | 1.77 | 1.09 | [13] |
| Pt/C+RuO2 | 0.85 | 1.62 | 0.77 | [14] |
| Pt@CoS2-NrGO | 0.85 | 1.465 | 0.615 | [15] |
| CoNC@LDH | 0.84 | 1.47 | 0.63 | [16] |
| Co9S8/MnS-USNC | 0.9 | 1.59 | 0.69 | [17] |

Table S3 Comparison of the performances of Co2P/Co3Fe7@N-C-based liquid ZAB with some of the previously reported nonprecious catalysts.

| Catalysts | OCP (V) | Peak power density (mW cm-2) | Cycle numbers @j (mA cm-2) | Refs. |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Co2P/Co3Fe7@N-C | 1.48 | 152.3 | 1596@2 | This work |  |  |
| Co-CMS | 1.46 | 219 | 3560@2 | [18] |  |  |
| CoFe@NC/KB-800 | 1.44 | 160 | (over 600)@2 | [19] |  |  |
| NiCo2O4/NCNTs/NiCo | 1.5 | 95.57 | 293@2 | [20] |  |  |
| CoFe/FeNC | N/A | 154.1 | 1050@5 | [21] |  |  |
| Fe-Co4N@N-C | 1.46 | 105 | 220@5 | [22] |  |  |
| CoFe@NCNT/CFC | 1.426 | N/A | 990@1 | [23] |  |  |
| FeCo@Co/NC-8 | 1.52 | 178 | N/A | [24] |  |  |
| PdNi/Ni@N-C | 1.41 | 108.5 | (over 600)@2 | [25] |  |  |
| FeCo/Se-CNT | 1.543 | 173.4 | 210@5 | [26] |  |  |
| FeNi/N-LCN | 1.49 | 162 | 1650@5 | [27] |  |  |
| NiFe@C@Co CNFs | 1.442 | 130 | 1200@5 | [28] |  |  |
| ODAC-CoO-30 | 1.45 | 128.5 | 450@5 | [29] |  |  |
| CuCo@N-C | 1.51 | 170 | 1476@3 | 1476 | [30] |

Table S4 Comparison of the performances of Co2P/Co3Fe7@N-C-based solid-state ZAB with some of the previously reported nonprecious catalysts.

| Catalysts | OCP (V) | Peak power densit (mW cm-2) | Cycle numbers @j (mA cm-2) | Refs. |
| --- | --- | --- | --- | --- |
| Co2P/Co3Fe7@N-C | 1.4 | 62.5 | 372@2 | This work |
| CoFe/FeNC | 1.465 | 108.6 | 54@2 | [21] |
| Fe-Co4N@N-C | 1.34 | 72 | N/A | [22] |
| CoFe@NCNT/CFC | 1.426 | 37.7 | 94@1 | [23] |
| FeCo/Se-CNT | 1.405 | 37.5 | 120@5 | [26] |
| ODAC-CoO-30 | 1.41 | 42 | 36@2 | [29] |
| (Zn)Co-NCF | N/A | 25 | 60@2 | [31] |
| CS-NFO@PNC-700 | 1.32 | 51 | (over 240)@5 | [32] |
| CoFe@NCNT/CFC | 1.426 | 37.7 | (over 100)@1 | [33] |
| PdNi/Ni@N-C | 1.4 | 66.5 | (over 45)@1 | [25] |
| NCOSH | 1.33 | 110 | (over 240)@1 | [34] |
| NPMC/CoFe | 1.37 | 121.1 | N/A | [35] |

References

- Wu M, Zhang G, Chen N et al (2021) Self-reconstruction of Co/Co2P heterojunctions confined in N‑doped carbon nanotubes for zinc-air flow batteries. ACS Energy Lett 6(4): 1153-1161. https://doi.org/ 10.1021/acsenergylett.1c00037.

- Gao J, Wang J, Zhou L et al (2019) Co2P@N, P-codoped carbon nanofiber as a free-standing air electrode for Zn-air batteries: synergy effects of Co-Nx satellite shells. ACS Appl Mater Interfaces 11(10): 10364-10372. https://doi.org/10.1021/acsami.8b20003.

- Shao Q, Li Y, Cui X et al  (2020) Metallophthalocyanine-based polymer-derived Co2P nanoparticles anchoring on doped graphene as high-efficient trifunctional electrocatalyst for Zn-air batteries and water splitting. ACS Sustain Chem Eng 8(16): 6422-6432. https://doi.org/10.1021/acssuschemeng.0c00852.

- Shi Q, Liu Q, Ma Y et al (2020) High‐performance trifunctional electrocatalysts based on FeCo/Co2P hybrid nanoparticles for zinc-air battery and self‐powered overall water splitting. Adv. Energy Mater 10(10): 1903854. https://doi.org/ 10.1002/aenm.201903854.

- Shi F, Zhu K, Li X et al (2021) Porous carbon layers wrapped CoFe alloy for ultrastable Zn-air batteries exceeding 20,000 charging-discharging cycles. J Energy Chem 61: 327-335. https://doi.org/ 10.1016/j.jechem.2021.01.032.

- He K, Zai J, Liu X et al (2020) One-step construction of multi-doped nanoporous carbon-based nanoarchitecture as an advanced bifunctional oxygen electrode for Zn-air batteries. Appl Catal B: Environ 265: 118594. https://doi.org/ 10.1016/j.apcatb.2020.118594.

- Liu X, Wang L, Yu P et al (2018) A stable bifunctional catalyst for rechargeable zinc-air batteries: Iron-cobalt nanoparticles embedded in a nitrogen-doped 3D carbon matrix. Angew Chem Int Ed 57(49): 16166-16170. https://doi.org/10.1002/anie.201809009.

- Liu J, He T, Wang Q et al (2019) Confining ultrasmall bimetallic alloys in porous N-carbon for use as scalable and sustainable electrocatalysts for rechargeable Zn-air batteries. J Mater Chem A 7(20): 12451-12456. https://doi.org/ 10.1039/c9ta02264c.

- Li S, Cheng C, Zhao X et al (2018) Active salt/silica-templated 2D mesoporous FeCo-Nx-carbon as bifunctional oxygen electrodes for zinc-air batteries. Angew Chem Int Ed 57(7): 1856-1862. https://doi.org/ 10.1002/anie.201710852.

- Zhang X, Zhu Z, Tan Y et al (2021) Co, Fe codoped holey carbon nanosheets as bifunctional oxygen electrocatalysts for rechargeable Zn-air batteries. Chem Commun  57(16): 2049-2052. https://doi.org/ 10.1039/d0cc07767d.

- Fan Y, Ida S, Staykov A et al (2017) Ni-Fe nitride nanoplates on nitrogen-doped graphene as a synergistic catalyst for reversible oxygen evolution reaction and rechargeable Zn-air battery. Small 13(25): 1700099. https://doi.org/10.1002/smll.201700099.

- Fu G, Cui Z, Chen Y et al (2017) Ni3Fe-N doped carbon sheets as a bifunctional electrocatalyst for air cathodes. Adv Energy Mater 7(22): 1601172. https://doi.org/10.1002/aenm.201601172.

- Zhang H, Zhang J, Li Y et al (2019) Continuous oxygen vacancy engineering of the Co3O4 layer for an enhanced alkaline electrocatalytic hydrogen evolution reaction. J Mater Chem A 7(22): 13506-13510. https://doi.org/ 10.1039/c9ta03652k.

- Zhang Z, Deng Y-P, Xing Z et al (2019)  "Ship in a bottle" design of highly efficient bifunctional electrocatalysts for long-lasting rechargeable Zn-air batteries. ACS Nano 13(6): 7062-7072. https://doi.org/10.1021/acsnano.9b02315

- Logeshwaran N, Ramakrishnan S, Chandrasekaran S-S et al (2021) An efficient and durable trifunctional electrocatalyst for zinc-air batteries driven overall water splitting. Appl Catal B: Environ 297: 120405. https://doi.org/ 10.1016/j.apcatb.2021.120405.

- Zhao C-X, Liu J-N, Wang J et al (2021) A ΔE  = 0.63 V bifunctional oxygen electrocatalyst enables high-rate and long-cycling zinc-air batteries. Adv Mater 33 (15):  2008606. https://doi.org/ 10.1002/adma.202008606.

- Li J, Li W, Mi H et al (2021) Bifunctional oxygen electrocatalysis on ultra-thin Co9S8/MnS carbon nanosheets for all-solid-state zinc-air batteries. J Mater Chem A 9(39): 22635. https://doi.org/ 10.1039/d1ta07019c.

- Liang S, Zou L-C, Zheng L-J et al (2022) Highly stable Co single atom confined in hierarchical carbon molecular sieve as efficient electrocatalysts in metal-air batteries. Adv Energy Mater 12(11): 2103097. https://doi.org/10.1002/aenm.202103097.

- Ren S, Duan X, Ge F et al (2022) Novel MOF-derived hollow CoFe alloy coupled with N-doped ketjen black as boosted bifunctional oxygen catalysts for Zn-air batteries. Chem Eng J 427: 	131614. https://doi.org/10.1016/j.cej.2021.131614.

- Chen C, Su H, Lu L-N et al (2022) Interfacing spinel NiCo2O4 and NiCo alloy derived N-doped carbon nanotubes for enhanced oxygen electrocatalysis. Chem Eng J 408: 127814. https://doi.org/10.1016/j.cej.2020.127814.

- Peng Z, Wang H, Xia X et al (2020) Integration of CoFe alloy and Fe/Fe3C nanoparticles into N-doped carbon nanosheets as dual catalytic active sites to promote the oxygen electrocatalysis of Zn-air battery. ACS Sustain Chem Eng 8 (24): 9009-9016. https://doi.org/10.1021/acssuschemeng.0c01729.

- Xu Q, Jiang H, Li Y et al (2019) In-situ enriching active sites on co-doped Fe-Co4N@N-C nanosheet array as air cathode for flexible rechargeable Zn-air batteries Appl Catal B: Environ 256: 117893. https://doi.org/ 10.1016/j.apcatb.2019.117893.

- Liu L, Zhang X. Yan F et al (2020) Self-supported N-doped CNT arrays for flexible Zn-air batteries. J Mater Chem A 8(35): 18162-18172. https://doi.org/10.1039/d0ta05510g.

- Song L, Zhang J, Sarkar S et al (2021) Interface engineering of FeCo-Co structure as bifunctional oxygen electrocatalyst for rechargeable zinc-air batteries via alloying degree control strategy. Chem Eng J 18: 133686. https://doi.org/10.1016/j.cej.2021.133686.

- Li Z, Li H, Li M et al (2021) Iminodiacetonitrile induce-synthesis of two-dimensional PdNi/Ni@carbon nanosheets with uniform dispersion and strong interface bonding as an effective bifunctional eletrocatalyst in air-cathode. Energy Storage Mater 42: 118-128. https://doi.org/ 10.1016/j.ensm.2021.07.027.

- Zhang H, Zhao M, Liu H et al (2021) Ultrastable FeCo bifunctional electrocatalyst on Se-doped CNTs for liquid and flexible all-solid-state rechargeable Zn-air batteries. Nano Lett 21(5): 2255-2264. https://doi.org/ 10.1021/acs.nanolett.1c00077.

- Li X, Liu Y, Chen H et al (2021) Rechargeable Zn-air batteries with outstanding cycling stability enabled by ultrafine FeNi nanoparticles-encapsulated N-doped carbon nanosheets as a bifunctional electrocatalyst. Nano Lett 21(7): 3098-3105. https://doi.org/ 10.1021/acs.nanolett.1c00279.

- Chen X, Pu J, Hu X et al (2022) Janus hollow nanofiber with bifunctional oxygen electrocatalyst for rechargeable Zn-air battery. Small 21(16): 2200578. https://doi.org/10.1002/smll.202200578.

- Tian Y, Liu X, Xu L et al (2021)  Engineering crystallinity and oxygen vacancies of Co(II) oxide nanosheets for high performance and robust rechargeable Zn-air batteries. Adv Funct Mater 31(20): 2101239. https://doi.org/10.1002/adfm.202101239

- Liu P, Hu Y, Liu X et al (2019)  Cu and Co nanoparticle co-decorated N-doped graphene nanosheets: A high efficiency bifunctional electrocatalyst for rechargeable Zn-air batteries. J Mater Chem A 7(20): 12851-12858. https://doi.org/10.1039/c9ta02894c

- Ma Y, Chen D, Li W et al (2022) Highly dispersive Co@N-C catalyst as freestanding bifunctional cathode for flexible and rechargeable zinc-air batteries. Energy Environ Mater. 5(2): 543-554. https://doi.org/10.1002/eem2.12315.

- Ramakrishnan S, Velusamy D-B, Sengodan S et al (2022) Rational design of multifunctional electrocatalyst: an approach towards efficient overall water splitting and rechargeable flexible solid-state zinc-air battery. Appl Catal B: Environ 300: 120752. https://doi.org/ 10.1016/j.apcatb.2021.120752.

- Liu L, Zhang X, Yan F et al (2020) Self-supported N-doped CNT arrays for flexible Zn-air batteries. J Mater Chem A 8(35): 18162-18172. https://doi.org/10.1039/d0ta05510g.

- Zheng X, Cao Y, Wu Z et al (2022) Rational design and spontaneous sulfurization of NiCo-(oxy)Hydroxysulfides nanosheets with modulated local electronic configuration for enhancing oxygen electrocatalysis. Adv Energy Mater 12(15): 2103097. https://doi.org/10.1002/aenm.202103275.

- Ma Y, Gan L, Li D et al (2019)  Rational modulation of N, P co-doped carbon nanotubes encapsulating Co3Fe7 alloy as bifunctional oxygen electrocatalysts for zinc-air batteries. J Power Sources 441: 227177. https://doi.org/10.1016/j.jpowsour.2019.227177.