# An agarose-alginate microfluidic device for the study of spheroid invasion, ATRA inhibits CAFs-mediated matrix remodeling

Patients' pathological conditions

| Fibroblasts | Age (year) | Tumor size (cm) | Depth of invasion | Type |
| --- | --- | --- | --- | --- |
| CAF N.1 | 57 | 15.0 | M (Metastasis) | Mixed ductal and lobular |
| CAF N.2 | 49 | 3.4 | T (Primary tumor) | Invasive Ductal |
| CAF N.3 | 59 | 6.0 | N (Spread to nearby lymph nodes) | Invasive Lobular |

Agents for decellularization

We prepared the first decellularization solution using 1 M NaCl, 10 mM Tris, and 5 mM EDTA in distilled water for 30 minutes while mixing at 500 rpm for 30 minutes. For osmotic shock treatment, NaCl and Tris were added, while EDTA was used to weaken cell-cell adhesion.

PBS was mixed at 500 rpm with 0.5 wt% SDS, 10 mM Tris, and 25 mM EDTA to prepare the second decellularization solution. Using SDS, nuclear and cytoplasmic membranes were dissolved and DNA was removed.

Chip feature details

| Feature |  | Size(µm) | Feature | Size(µm) |
| --- | --- | --- | --- | --- |
| Ports diameter |  | 1000 | Barrier blocks | 150*150 |
| Channels width | Barrier | 200 | Distance between blocks | 225 |
|  | Cell culture | 800 | Microwells diameter | 400 |
|  | Trigger | 2000 | Microwells depth | 400 |
| Channels depth |  | 200 |  |  |

Figure 1. Schematic plan from microchip.

Viability Assay

Figure 2. Viability assay using AO/PI Cell Viability Kit. Image B shows staining with AO and represents living cells. Image C shows staining with PI, which is only able to penetrate dead cells. Image D shows the merging of the two staining, representing the percentage of cell viability.