Supporting Information

Sub-nanometric high entropy alloy cluster: hydrogen spillover-driven synthesis on CeO2 and structural reversibility

Naoki Hashimoto1, Kohsuke Mori1,2*, Shuichiro Matsuzaki1, Kazuki Iwama1, 
Naoto Kamiuchi3, Hideto Yoshida3, and Hiromi Yamashita1,2*

1 Division of Materials and Manufacturing Science, Graduate School of Engineering, Osaka University, 2-1 Yamada-oka, Suita, Osaka 565-0871, Japan.

Tel & FAX: +81-6-6879-7457, +81-6-6879-7457,

E-mail: mori@mat.eng.osaka-u.ac.jp, yamashita@mat.eng.osaka-u.ac.jp

2 Innovative Catalysis Science Division, Institute for Open and Transdisciplinary Research Initiatives (ICS-OTRI), Osaka University, Suita, Osaka 565-0871, Japan.

3 The institute of Scientific and Industrial Research, Osaka University, 8-1 Mihogaoka, Ibaraki, Osaka 567-0047, Japan.

Figure S1. (a,b) HR-TEM images and (c) SAED of CeO2-NRs.

Figure S2. (a,b) HR-TEM images and (c) SAED of CeO2-NCs.

Figure S3. XRD patterns of CeO2-NRs, CeO2-NPs and CeO2-NCs.

Figure S4. H2-TPR profiles of quinary CoNiCuZnPd specimens deposited on various CeO2 supports.

Figure S5. (a) A HAADF-STEM image and (b)-(f) EDX-mappings of CoNiCuZnPd/CeO2-NRs. (g) EDX analysis in the indicated region.

Figure S6. (a) A HAADF-STEM image and (b)-(f) EDX-mappings of CoNiCuZnPd/CeO2-NPs.

Figure S7. (a) A HAADF-STEM image and (b)-(f) EDX-mappings of CoNiCuZnPd/CeO2-NCs.

Figure S8 In situ XANES spectra at the (a) Co, (b) Ni, (c) Cu, (d) Zn and (e) Pd K-edge of CoNiCuZnPd/CeO2-NPs under H2 condition with elevated temperature from 200 to 400 °C.

Figure S9. In situ XANES spectra at the (a) Co, (b) Ni, (c) Cu, (d) Zn and (e) Pd K-edge of CoNiCuZnPd/CeO2-NCs under H2 condition with elevated temperature from room temperature to 400 °C.

Figure S10. In situ FT-EXAFS spectra at the (a) Co, (b) Ni, (c) Cu, (d) Zn and (e) Pd K-edge of CoNiCuZnPd/CeO2-NPs under H2 condition with elevated temperature from 200 to 400 °C.

Figure S11. In situ FT-EXAFS spectra at the (a) Co, (b) Ni, (c) Cu, (d) Zn and (e) Pd K-edge of CoNiCuZnPd/CeO2-NCs under H2 condition with elevated temperature from room temperature to 400 °C.

Figure S12. FT-EXAFS spectra of (a) CoNiCuZnPd/CeO2-NPs and (b) -NCs at Pd K-edge and fit curve.

Figure S13. Simulated XANES spectrum of bulk HEA (Co13Ni13Cu12Zn13Pd13).

Figure S14. NO reduction activity over CoNiCuZnPd/CeO2-NRs and monometallic M/CeO2-NRs (M=Co, Ni, Cu, Zn and Pd).

Figure S15. Adsorption energy of (a,b) NO and (c,d) H on fcc and hcp hollow sites for quinary CoNiCuZnPd(111) and monometallic slabs respectively.

Figure S16. Experimental protocol for in situ XAFS measurement under NO/H2 conditions

Figure S17. In situ XANES and FT-EXAFS spectra at Pd K-edge for Pd/CeO2-NRs under cyclic NO/H2 conditions.

Figure S18. In situ XANES and FT-EXAFS spectra at Pd K-edge for CoNiCuZnPd/CeO2-NRs under cyclic NO/H2 conditions

Figure S19. In situ XANES spectra at Co K-edge for CoNiCuZnPd/CeO2-NRs under cyclic NO/H2 conditions.

Figure S20. In situ XANES spectra of CoNICuZnPd/CeO2-NRs at Ni K-edge under cyclic NO/H2 conditions.

Figure S21. In situ XANES spectra of CoNICuZnPd/CeO2-NRs at Cu K-edge under cyclic NO/H2 conditions.

Figure S22. In situ XANES spectra of CoNICuZnPd/CeO2-NRs at Zn K-edge under cyclic NO/H2 conditions.

Figure S23. Simulated XANES spectrum at Pd K-edge for oxidized HEA model ((Pd3@(Co3Ni2Cu3Zn2)O6).

Table S1. Curve fitting results at Pd K-edge for CoNiCuZnPd/CeO2

Table S2. The list of employed 25 configuration patterns for the calculation of the adsorption energies of NO and H on fcc on-top

Table S3. The list of employed 30 configuration patterns for the calculation of the adsorption energy of NO and H on fcc hollow.

Table S4. The list of employed 30 configuration patterns for the calculation of the adsorption energy of NO and H on hcp hollow.