Supporting Information

Injectable bioactive copper-based metal organic framework embedded dual-crosslinked alginate hydrogel for potential antimicrobial applications

Kihak Gwon1, Seonhwa Lee1, Youngmee Kim2, Jun Choi2, Sujin Kim2, Sung-Jin Kim2, Hye Jin Hong3, Youngmin Hwang4, Munemasa Mori4 and Do Nam Lee1*

1 Ingenium College of Liberal Arts (Chemistry), Kwangwoon University, Seoul 01897, Republic of Korea

2 Department of Chemistry and Nano Science, NanoBio-Energy Materials Center, Ewha Womans Universiry, Seoul 03760, Republic of Korea

3 Department of Physiology and Biomedical Engineering, Mayo Clinic, Rochester, MN, 55902, USA

4 Columbia Center for Human Development (CCHD), Pulmonary Allergy & Critical Care Medicine, Department of Medicine, Columbia University Irving Medical Center, New York, NY 10032, USA

Corresponding Author: D.N. Lee.

E-mail addresses: donamlee@hanmail.net. 1 Ingenium College of Liberal Arts (Chemistry), Kwangwoon University, Seoul 01897, Republic of Korea

Figure S1. Synthesis and characterization of methacrylated alginate (ALG-MA). (A) Synthesis of ALG-MA via transesterification reaction between alginate and methacrylic anhydride. (B) The 1H nuclear magnetic resonance (NMR) spectra of HA-MA. The degree of methacrylation was calculated by comparing the methacrylate peaks of MA at −5.6 (Peak b) and −6.1 ppm (Peak a) and methyl protons peak at 1.9 ppm (Peak c).

Table S1. Crystallographic data for Cu(AZPY)-MOF.

|  | Cu(AZPY)-MOF |
| --- | --- |
| Chemical formula | C20H20Cu2N4O10 |
| Formula weight | 603.48 |
| Wavelength (Å) | 0.71073 |
| Space group | C 2/c |
| a (Å) | 24.679 (11) |
| b (Å) | 13.156 (5) |
| c (Å) | 8.534 (3) |
|  (°) | 90 |
|  (°) | 93.86 (3) |
|  (°) | 90.00 |
| Volume (Å3) | 2766.5 (18) |
| Z | 4 |

Table S2. Antibacterial and antifungal activities of Cu(AZPY)-MOF (Cu(AZPY)), alginate hydrogel (Dual-ALG), and Cu(AZPY)-MOF encapsulated alginate hydrogel (Cu(AZPY)@Dual-ALG) against MRSA, C. albicans, and S. mutans.

| Test strain | Test sample | Test resultsa, b |  |  |
| --- | --- | --- | --- | --- |
|  |  | Early conc. (CFU·mL-1) | After 24 h, conc. (CFU·mL-1) | Reduction rate of bacteria (%) |
| MRSA | Blank | 1.7 × 104 | 1.0 × 105 | - |
|  | Cu(AZPY) | 1.7 × 104 | <10 | 99.9 |
|  | Blank | 2.1× 105 | 2.8 × 106 | - |
|  | Dual-ALG | 2.1 × 105 | 1.7× 105 | 93.9 |
|  | Blank | 2.1 × 105 | 2.8 × 106 | - |
|  | Cu(AZPY)@Dual-ALG | 2.1 × 105 | <10 | 99.9 |
| S. mutans | Blank | 2.5 × 104 | 2.8 × 105 | - |
|  | Cu(AZPY) | 2.5 × 104 | 2.7 × 104 | 90.3 |
|  | Blank | 2.5 × 105 | 5.3 × 106 | - |
|  | Dual-ALG | 2.5 × 105 | 8.2 × 104 | 98.4 |
|  | Blank | 2.5 × 105 | 5.3 × 106 | - |
|  | Cu(AZPY)@Dual-ALG | 2.5 × 105 | <10 | 99.9 |
| C. albicans | Blank | 1.3 × 104 | 2.2 × 105 | - |
|  | Cu(AZPY) | 1.3 × 104 | <10 | 99.9 |
|  | Blank | 3.5 × 105 | 4.7 × 106 | - |
|  | Dual-ALG | 3.5 × 105 | 4.1 × 106 | 12.7 |
|  | Blank | 3.5 × 105 | 4.7 × 106 | - |
|  | Cu(AZPY)@Dual-ALG | 3.5 × 105 | 1.0 × 106 | 78.7 |

aTest method: KCL-FIR1002: 2021 for Cu-Azpy and KCL-FIR1003: 2018 for Dual-ALG and Cu(AZPY)@Dual-ALG

bTest environment: (37.0 ± 0.2) °C, Conc. 20 μg·mL−1 of Cu(AZPY), 2 mg·mL−1 of Dual-ALG and Cu(AZPY)@Dual-ALG