Synergetic degradation of carbamazepine using hybrid advanced oxidation processes of hydrodynamic cavitation/ UV/ ZnO/ZnFe2O4 for persulfate activation

Kuldeep Roya and Vijayanand S. Moholkar*b

a School of Chemical Engineering, Vellore Institute of Technology, Vellore, Tamil Nadu, India

b Department of Chemical Engineering, Indian Institute of Technology Guwahati, Guwahati, Assam, India

* Author for correspondence. Fax: +91 361 258 2291. E-mail: vmoholkar@iitg.ac.in

Supplementary Materials

(A)

|  | Diameter of each hole (dh) = 2 mm Number of holes (Nh) = 4 Flow area = 12.56 mm2 Perimeter of holes = 25.12 mm  = 2.00 mm–1, βo = 0.036 (B) |
| --- | --- |

Fig. S1. (A) Schematic of hydrodynamic cavitation reactor coupled with a UV source (for the photochemical system); (B) Geometrical specifications of 4–hole orifice plate used as a cavitator.

Fig. S2. Simulated time profile of  ions utilization in a hybrid oxidative kinetic modelling