Table 1 The atomic percentage of Si, C and O in the two positions (S1 and S2) of MEH-PPV/SiNWs nanocomposites obtained after immersion durations of 60 min and 150 min

|  | Position S1 |  |  | Position S2 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Si | C | O | Si | C | O |
| MEH-PPV/SiNWs (60 min) | 49 % | 41 % | 6 % | 29 % | 43 % | 7 % |
| MEH-PPV/SiNWs (150 min) | 59 % | 39 % | 3 % | 47 % | 50 % | 4 % |

Table 2 Electrical parameters of Ag/MEH-PPV/SiNWs diodes before annealing treatment determined from Cheung functions.

.

| dim (min) | n | Rs (Ω) | φb (eV) |
| --- | --- | --- | --- |
| 0 | 3.93 | 261 | 0.658 |
| 30 | 3.28 | 1250 | 0.640 |
| 60 | 3.41 | 879 | 0.650 |
| 90 | 3.48 | 945 | 0.659 |
| 120 | 3.52 | 813 | 0.667 |
| 150 | 3.68 | 445 | 0.659 |

Table 3 The experimentally m values of Ag/MEH-PPV/SiNWs diodes before annealing, at low voltages (L. V.) and at high voltages (H. V.), obtained from I-V curves plotted in Log-Log scale for different immersion durations.

| dim (min) | L.V. | H. V. |
| --- | --- | --- |
| 0 | 1.02 | 1.01 |
| 30 | 1.20 | 1.10 |
| 60 | 1.34 | 1.15 |
| 90 | 1.56 | 1.20 |
| 120 | 1.04 | 1.12 |
| 150 | 1.06 | 1.04 |

Table 4 The experimentally parameters obtained from C-2-V plots of Ag/MEH-PPV/SiNWs diodes elaborated at different immersion durations

| dim (min) | V0 (eV) | Vd (eV) | NA (m-3) | Vp(eV) | φb(eV) |
| --- | --- | --- | --- | --- | --- |
| 0 | 1.430 | 1.456 | 4 x 1015 | 0.156 | 1.612 |
| 30 | 1.245 | 1.271 | 3.1 x 1015 | 0.162 | 1.433 |
| 60 | 0.744 | 0.770 | 1.8 x 1015 | 0.176 | 0.946 |
| 120 | 0.876 | 0.902 | 3.3 x 1015 | 0.161 | 1.063 |
| 150 | 0.558 | 0.584 | 3.9 x 1015 | 0.156 | 0.740 |

Table 5 The experimentally n, Rs, and φb values of Ag/MEH-PPV/SiNWs diodes elaborated at different immersion durations for annealing temperatures ranging from 100°C to 250°C determined from eq.3 and eq. 5 (O.C.: Ohmic Character).

|  | 100°C |  |  | 150°C |  |  | 200°C |  |  | 250°C |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | n | Rs (Ω) | φb(eV) | n | Rs (Ω) | φb(eV) | n | Rs (Ω) | φb(eV) | n | Rs (Ω) | φb(eV) |
| 0 min | 3.97 | 261 | 0.660 | 3.95 | 251 | 0.663 | 3.99 | 228 | 0.646 | O.C. | - | O.C. |
| 30 min | 3.33 | 1090 | 0.673 | 3.18 | 1640 | 0.656 | 3.48 | 821 | 0.681 | 3.51 | 678 | 0.555 |
| 60 min | 3.55 | 800 | 0.822 | 3.57 | 596 | 0.651 | 3.58 | 562 | 0.641 | O.C. | - | O.C. |
| 90 min | 3.55 | 819 | 0.833 | 3.58 | 783 | 0.847 | 3.59 | 597 | 0.711 | 3.61 | 543 | 0.662 |
| 120 min | 3.50 | 702 | 0.700 | 2.88 | 1978 | 0.534 | 3.40 | 676 | 0.527 | O.C. | - | O.C. |
| 150 min | 3.26 | 820 | 0.334 | O.C. | - | O.C. | O.C. | - | O.C. | O.C. | - | O.C. |