TABLE I.  Macroscopic moment μtot [41], orbital, spin and total uranium 5f moments deduced from XMCD spectra at 2.7 K for the applied field along the easy a-axis. The orbital, μLU (5f), and spin, μSU (5f) moments are calculated for two possible 5f2 and 5f3 electron configurations using the theoretical values for the < Tz >/< Sz > ratios, 1.16 and 0.62, respectively [35]. The bold values are those obtained for a f-count ne5f = 2.8 [28,29] estimated from band structure calculations and our XMCD data. The < Tz >/< Sz > values of 0.73 and 0.84 for  ne5f=2.8 and 2.6 were estimated using linear interpolation of ionic values in the intermediate coupling scheme.

| H (T) | μtot (μB /f.u.) | ne5f | μLU 5f (μB/atom U) | μSU 5f (μB /atom U) | μtotU5f (μB /atom U) | -μLU5fμSU5f |
| --- | --- | --- | --- | --- | --- | --- |
| 17 | 0.88 | 3 2.8 2.6 2 | 1.58 1.61 1.64 1.72 | - 0.75 - 0.68 - 0.63 - 0.52 | 0.83 0.93 1.01 1.20 | 2.11 2.37 2.60 3.31 |