Supplementary Information:

Controlling the Propagation Asymmetry of Hyperbolic Shear Polaritons in Beta-Gallium Oxide

Joseph Matson*, Sören Wasserroth*, Xiang Ni*, Maximilian Obst, Katja Diaz-Granados, Giulia Carini, Enrico Maria Renzi, Emanuele Galiffi, Thomas Folland, Lukas M. Eng, J. Michael Klopf, Stefan Mastel, Sean Armster, Vincent Gambin, Martin Wolf, Susanne C. Kehr, Andrea Alù, Alexander Paarmann, Joshua D. Caldwell

S1. Complex-momentum eigenvalue analysis for surface shear polaritons

We assume plane wave solution ei(kxx+kyy-iκz-ωt) for the components of hyperbolic shear polaritons (HShPs) in bGO which exponentially decay away from the interface, thus source-free Maxwell equations read

ϵxx-(-κz2+ky2)ϵxy+kxky-ikxκzϵxy+kxkyϵyy-(-κz2+kx2)-ikyκz-ikxκz-ikyκzϵzz-(ky2+kx2)ExEyEz=0,            (1)

We then have the polynomial equation by solving Eq. (1)

ϵzzκz4+ϵzzϵxx+ϵyy-ϵzzkx2-ϵzzky2-ϵxxkx2+ϵyyky2+2ϵxykxkyκz2+ϵzz-kx2-ky2ϵxxϵyy-ϵxy2-ϵxxkx2+ϵyyky2+2ϵxykxky=0.#2

Therefore, the solutions of κz are obtained as

κ±2=-b±b2-4ac2a,                                                               (3)

where

a=ϵzz, 
b=ϵzzϵxx+ϵyy-ϵzzkx2-ϵzzky2-ϵxxkx2+ϵyyky2+2ϵxykxky, 
c=ϵzz-kx2-ky2ϵxxϵyy-ϵxy2-ϵxxkx2+ϵyyky2+2ϵxykxky.                  (4)

To guarantee the physical solutions, the solutions in Eq. (3) need to satisfy b2-4ac≥0, and κ±2≥0 so two unphysical solutions are eliminated. To simplify the expression of eigenfield solutions, we apply rotation to Maxwell equations in the xy plane: Rϕ=cos⁡(ϕ)sin⁡(ϕ)0-sin⁡(ϕ)cos⁡(ϕ)0001 , and also replace kx and  ky with the following relations kx=qcosϕ, ky=-qsin(ϕ), thus the momentum vectors of surface polariton in the rotated basis become k±=q,0,-iκ±. Permittivity components after rotation turn into
ϵxxt=12ϵxx+ϵyy+ϵxx-ϵyycos2ϕ+2ϵxysin2ϕ,
ϵyyt=12ϵxx+ϵyy+-ϵxx+ϵyycos2ϕ-2ϵxysin2ϕ,

ϵxyt=ϵxycos2ϕ+-ϵxx+ϵyycosϕsinϕ.

ϵzzt=ϵzz.                                                                                                   (5)

Under the rotated basis, Maxwell equations are simplified as

M±=ϵxxt+κ±2ϵxyt-iκ±qϵxytϵyyt-(-κ±2+q2 )0-iκ±q0ϵzzt-q2ExtEytEzt=0,                              (6)

As a result, the general forms of eigenmode in bGO can be expressed as

E+t=m22+m33+,-m21+m33+,-m22+m31+,

H+t=-iκ+ey+,iκ+ex++qez+,-qey+

E-t=m22-m33-,-m21-m33-,-m22-m31-
 H-t=-iκ-ey-,iκ-ex-+qez-,-qey-,                                            (7)

Similarly, the solutions of HShPs in the air have the plane wave form ei(kxx+kyy+iκair-ωt), where κair=q2-ϵair. The eigenmodes can be decomposed into two independent solutions

TM:  E=-iκair,0,q, H=[0,ϵair,0];

TE: E=0,1,0, H=[iκair,0,-q].                                               (8)

To procure the isofrequency contours (IFCs) of HShPs, we impose the continuous conditions for tangential fields at the boundary z=0 and obtain the linear equations

Da+a-aTMaTE=0,                                                           (9)

Where the matrix D is

D=ex+ex--iκair0ey+ey-01hx+hx-0iκairhy+hy-ϵair0,                                            (10)

and a± and aTM/TE are the coefficients of wave components in bGO and air, respectively. For the lossless case, IFC dispersion of the surface polariton in k-space is obtained from the secular equation detD=0. Since we aim to study the eigenmodes and obtain IFC of shear polaritons supported by the lossy and anisotropic bGO, we have to adopt the complex-valued form for their in-plane momentum vector  qc=qr+iqi=(kx+iκx,ky+iκy), where qr and qi are not necessarily in parallel. Particularly, we impose the condition that qi follows the same direction as the one of in-plane Poynting vector: qi||S|| (The detailed study of this condition will be present in somewhere else). Consequently, we can solve the complex-valued dispersion of shear polaritons with enough number of equations

f1kx,κx,ky,κy=RdetD=0;
f2kx,κx,ky,κy=IdetD=0.                                           (11)

The damping rate γ=|qi|/|qr| of shear polaritons can be evaluated from the complex-valued solutions in Eq. (11).

S2. FOM calculation explanation

To quantify the shear effect of the hyperbolic polaritons both theoretically and experimentally, we propose a global figure of merit (FOMSh) for the shear asymmetry as a function of disc radius which reads

FOMShR=i-1ikikRdkγikikRdkγ, 	 		             	(12)

Where the line integration follows the path of IFCs of HShPs calculated from Eq. (11). The upper bound in the integration is

kR/k0=λ2R,                                                              (13)

which is the radius of white circle in k-space in Figure S1, λ is the free space wavelength, R is the radius of the disc launcher. The lower bound in the integration ki is the intersection of the rotated hyperbola axis and hyperbolic dispersion in the according quadrant, as shown in Figure S1. We are also able to extract this FOMSh from our direct measurement and simulation of the HShPs launched from the different sized launchers (detailed in Figure SXXX). However, we need to account for the oblique incidence shifting the dispersion in k-space. We account for this by shifting kR by the amount:

Δk=k0cosθinccosϕ,sinϕ			              (14)

Where ϕ is the azimuthal angle of the beam incidence, and θinc is the angle of the incident beam from the sample surface. This shifted momentum is indicated by the green circles in Figure S1.

Figure S1 - The schematic of quadrant division in k-space, and the cut-off radii (white circles or green circles with shift Δk) correspond to excitation limitation of various discs launchers in real space. The red curves are IFCs of HShPs produced from the complex-momentum eigenmode study in Sec. S1.

S3. Description of shear “clockwise” vs “counter-clockwise” bias

In the manuscript, we refer to the orientation of the shear effect by the counter-clockwise redistribution of the polariton intensity within the polariton hyperbola (Fig. S2b). This counter-clockwise orientation also describes the tilt of the polariton wavefront (Fig. S2a).

Figure S2 – Orientation of Shear. a) Experimental image from main figure 3c – launched at 720cm-1 by a 2 µm gold disc. b) Fourier transform of a (from Main figure 3f), with white arrow indicating the shear bias of the polariton. This corresponds to a left-handed shear of the polariton dispersion about the [010] axis. c-d) Fake images, from flipping (a-b) about the vertical axis. This illustrates the “counter-clockwise” bias we would observe on a [0-10] surface, which would still be a left-handed rotation about [010].

S4. Analysis of propagation lengths and polariton wavelength

In this section, we briefly analyze the polariton wavelengths and propagation lengths. In the FEL s-SNOM, we took large area measurements of the polaritons launched by a 2µm disc so that the polariton fully decays in the scan area (Fig. S3 a,b). By nature of in-plane hyperbolic polaritons propagating from a disc antenna, there is not a clear point from which to extract the polariton features, however we can get a rough view of the polariton characteristics by taking linecuts of the field profile at different angles from the antenna.

Here, we have taken three linecuts distributed through the hyperbolic propagation and fit to an exponentially decaying sine wave.

yx=y0+Ae-xt0sinπx-xcw					(15)

Which gives us w for the polariton wavelength, and t0 for the decay length of the polariton propagation.

Figure S3 – HShP Propagation Length. a,b) Experimental image of HShPs launched by 2um gold disc at 712cm-1 (712cm-1), with 3 linescans taken from the disc along the HShP propgagation fringes. c-d) Linescans from a-b, fitted with a decaying sine wave. e) Polariton wavelength from fitted linescans in a-d, showing wavelengths ~3-4 µm, with the wavelength being longest along the top edge of the hyperbola due to the shear tilt. f) Number of propagation cycles (propagation length divided by wavelength (e)) from fitted linescans (a-d).

S5. Frequency varying measurements of bGO polaritons launched from different antenna sizes

In Figure 4 of the main text, we demonstrate the frequency-dependent rotation of the shear polaritons launched by a 2 µm gold disc antenna. Here, we show similar measurements on 1 µm (Fig. S4) and 4 µm gold discs (Fig. S5).

Figure S4 – Frequency dependent rotation of HShP propagation from 1-µm discs. a-h) Rotated polariton axis plotted, as in Figure 4 of the main text, against s-SNOM collected near-field plots of HShPs launched by a 1-µm diameter gold disc, at varying frequencies (Scale bar = 2 µm).

Figure S5 – Frequency dependent rotation of HShP propagation from 4-µm discs. a-d) Rotated polariton axis plotted, as in Figure 4 of the main text, against s-SNOM collected near-field plots of HShPs launched by a 4-µm diameter gold disc, at varying frequencies (Scale bar = 2 µm).

S6. Finite element modeling concerning the two mechanisms

Figure S6 - (a) Finite element modeling of HShPs propagation excited by dipole source at frequency of 712 cm-1. (b) Fourier transform of image in (a). The red curves in (b) are the dispersion of HShPs calculated from theory, and the white circle represents the free space light cone.

As we explained in the main text, the asymmetry propagation of HShPs in disc-launcher excitation arises from two mechanisms: the first mechanism comes from the off-diagonal imaginary component of permittivity tensor, causing the inherent asymmetry in polariton propagation, as seen in near-field point-dipole excitations in Figure S6. The second mechanism is the orientation-dependent phase matching condition between the illuminated disc launcher and the excited polaritons. For example, when alignment of the incident light direction to the one of the asymptotic lines of the hyperbolic wave in real space, the hyperbolic waves in the other branch of asymptotic line get stronger excitation. To verify asymmetry effect from the second mechanism, we perform finite element simulations for disc-launcher excitation with and without the intrinsic shear mechanism. To control and remove the intrinsic shear effect in the simulation, we first diagonalize the real permittivity tensor of bGO by the following procedure

ϵxx'ϵxy'0ϵxy'ϵyy'000ϵzz=Rωϵxxϵxy0ϵxyϵyy000ϵzzR-1ω,                       (16)

where Rω is the SO(3) matrix and its rotational angle depends on the frequency ω. As a result, ϵxy' is an imaginary number. Next, we manually insert a tuning parameter f in front of ϵxy', and rotate matrix in the left side of Eq. (16) back to the original coordinate frame

ϵxx''ϵxy''0ϵxy''ϵyy''000ϵzz=R-1ωϵxx'f*ϵxy'0f*ϵxy'ϵyy'000ϵzzRω.                (17)

Consequently, when f=1, the permittivity tensor in the left side of Eq. (17) becomes the original permittivity tensor. When f=0, it preserves the optical response of the original tensor but gets rid of the intrinsic shear effect. We deploy the permittivity tensor in the left side of Eq. (17) in COMSOL simulation with and without intrinsic shear effects by tuning f between 1 and 0. As a result, the asymmetry propagation in the case f=0 (Figure S7 (a,b)) is solely caused by the orientation-dependent phase matching between the illuminated disc and polaritons wave. When we turn on the intrinsic shear effect, the asymmetry effect of HShPs is enhanced (Figure S7 (c,d)) because the two mechanisms contribute to the shear-asymmetry effect constructively.

Figure S7 - Compare the disc-launcher excitations with and without intrinsic shear effect. (a,c) Finite element modeling of HShPs propagation by disc-launcher excitation at frequency of 720 cm-1 without (a) and (c) with intrinsic shear effect. (b,d) Fourier transform of image in (a,c). The red dashed arrow represents the orientation of illuminating light.

S7. FOM Calculation

Figure S8- Sampling the experimental Fourier spectrum of HShPs excitation by illuminating gold disc-launchers of different size. (a-c) Fourier spectra of experimental near-field images of HShP propagation launched by a (6,4,2) µm gold disc at a frequency of 720 cm-1, with illumination incident from the lower left corner. (e-f) 1D Fourier intensity distribution extracting along the IFCs of HShPs for various disc-launchers in (a-c). White circles in (a-c) intersecting dispersion of HShP determine the upper bound of the integration in k-space of FOM calculation, and the radius of the circle is calculated by Eq. (13). Light green (grey) shaded regions in (e-f) correspond to the odd (even) quadrants in k-space in Figure S1.

Figure S9. Sampling the simulated Fourier spectrum of HShPs excitation by illuminating gold disc-launchers of different size.

S8. Simulating shear polariton propagation at various frequencies

We also calculated the polariton propagation from a 2 µm gold disc for select frequencies from the main text Figure 4 (Fig. S10). These show excellent agreement at varying excitation frequencies.

Figure S10 – a-d) Select frequencies from main figure 4 – with e-h) corresponding COMSOL simulations of the HShP propagation.