Supporting Information

Tough and biodegradable polyurethane-silica hybrids with rapid sol-gel transition for bone repair

Su Jeong Park1,2, Seung Hyuk Im1, Donghak Kim1,2, DoYeun Park2, Youngmee Jung2,3, Hyung-seop Han2, Soo-Hyun Kim1,2,4*, Justin J. Chung5,6*

Figure S1. FTIR spectra of BPH0 (APTES functionalized polyurethane, black), PCL-diol (red), HDI (blue), and APTES (Green).

Figure S2. Rheology measurements of PCL-diol and hydrolyzed TEOS mixture (30 wt.% silica ratio) for 1 hours of mixing.

Figure S3. Representative uniaxial stress/strain curves of the 0, 10, 20, 30 40 wt. % silica hybrids (Sample size diameter: 11 mm, Thickness: 6.25 mm).

Figure S4. DNA quantification of MC3T3-E1 cells attached on the hybrid scaffolds (*p < 0.05, † p < 0.05, and ††p < 0.01 compared with 30 wt. % silica hybrid on day 1, n=3).

Figure S5. Accelerated degradation test on hybrid scaffolds. Samples were immersed in 1M NaOH at 25 ℃ for 0, 8, 24, 48, 72 and 168 h. Samples and SEM images of the degraded hybrid scaffold samples after accelerated degradation test.

Figure S6. Representative stress-strain curve of BPHS30 after 2 and 4 weeks of immersion in PBS.

Table S1. Mechanical properties of BPHS30 after 2 and 4 weeks of immersion in PBS (n=3).

|  | 2 weeks |  | 4 weeks |  |
| --- | --- | --- | --- | --- |
|  | Young’s modulus (KPa) | Ultimate strength (KPa) | Young’s modulus (KPa) | Ultimate strength (KPa) |
| BPHS30 | 980 ± 266.30 | 575.12 ± 128.51 | 666.67 ± 300.2 | 362.06 ± 76.60 |

Standard deviations are derived from the average values.