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Figure S1. The Optical image of 3 wt% agarose hydrogel 
[image: ]



Figure S2. The SEM image of pure agarose.
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Figure S3. Control absorption spectra of 4-NP after the addition of KBH4 at different reaction times of 0 min (black curve) and 24 h (red curve) using pure agarose hydrogel as catalyst.
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Figure S4. Time dependent absorption spectra of catalytic reduction reactions of 4-NP using HRC-Ag/Agar-1.9 aerogel as catalysts.
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