Electronic supplementary material

for

Sensitive and Rapid Sensing of Dimetridazole in Food and Environmental Samples Using a Water-Stable Luminescent Zwitterionic Cd(Ⅱ) Metal-Organic Framework

Kaimin Wang 1,*, Yanqiu Dong 1, Xiong Zhao 1, Keyan Duan 1, Ruiting Zhao 1, Yanqing Ye 1,*, Jinrong Guo 1, Hao Pan 2, Huaijun Tang 1 and Yulu Ma 2,*

1 Key Laboratory of Green-Chemistry Materials in University of Yunnan Province, School of Chemistry & Environment, Yunnan Minzu University, Kunming 650504, PR China;

2 School of Pharmaceutical Sciences and Yunnan Key Laboratory of Pharmacology for Natural Products, Kunming Medical University, Kunming, Yunnan 650500, PR China;

* Correspondence: 041684@ymu.edu.cn (Kaimin Wang); yey‑qing@163.com (Yanqing Ye); yuluma163@163.com (Yulu Ma)

List of contents

Section A-Figures	3

Figure S1	3

Figure S2	4

Figure S3	5

Figure S4	6

Figure S5	7

Figure S6	8

Section B-Table	9

Table S1	9

Table S2	10

Section A-Figures

Figure S1

Figure. S1 Synthesis of 1,1'-((2,5-dimethyl-1,4-phenylene)bis(methylene))bis(4-carboxypyridin-1-ium) chloride (H2LCl2)

Figure S2

Fig. S2 The FT-IR spectrum of MOF 1

Figure S3

Fig. S3 The TGA curve of MOF 1

Figure S4

Fig. S4 The solid state luminescent spectrum of the ligand H2LCl2 (a) and MOF 1 (b)

Figure S5

Fig. S5 The luminescence intensity of MOF 1 water suspension in different antibiotics.

Figure S6

Fig. S6 The powder X–ray diffraction pattern of MOF 1 after the quenching cycle test

Section B-Table

Table S1

Table S1 Crystallographic and refinement data for MOF 1

| Identification code | MOF 1 |
| --- | --- |
| Empirical formula | C44H52CdCl2N4O14 |
| Formula weight | 1044.23 |
| Crystal system | Orthorhombic |
| Space group | Fddd |
| a/nm | 1.39159(8) |
| b/nm | 2.51962(11) |
| c/nm | 2.70069(12) |
| α/° | 90 |
| β/° | 90 |
| γ/° | 90 |
| V/nm3 | 9.4694(8) |
| Z | 8 |
| ρcalc/(g·cm-3 ) | 1.313 |
| μ/mm–1 | 0.626 |
| Reflections collected | 14179 |
| Independent reflections | 3147 [Rint=0.0325] |
| Goodness-of-fit on F2 | 1.086 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0650, wR2 = 0.1910 |
| Final R indexes [all data] | R1 = 0.0680, wR2 = 0.1937 |

Table S2

Table S2 Selected bond lengths [nm] and bond angles [°] for MOF 1

| Bond lengths (nm) for MOF 1 |  |  |  |
| --- | --- | --- | --- |
| Cd(1)−O(1) | 0.2427(3) | C(4)−N(1) | 0.1336(5).. |
| Cd(1)−O(2) | 0.2429(3). | C(1)−O(1)A | 0.1242(5) |
| Bond angles (°) for MOF 1 |  |  |  |
| O(1)−Cd(1)−O(1)B | 84.36(15). | O(1)C−Cd(1)−O(2) | 82.81(12). |
| O(1)−Cd(1)−O(1)A | 126.79(17). | C(4)−N(1)−C(7) | 118.7(3) |
| O(1)C−Cd(1)−O(2)A | 138.13(11) | C(1)A−O(2)−Cd(1) | 91.0(2). |

Symmetrical operation: (A) -x+5/4, -y+1/4, +z; (B) -x +5/4, +y, -z+1/4; (C) -x+5/2, -y+1/2, -z; (D) +x, -y+1/4, -z+1/4