Supplementary Material

Hierarchical V4C3TX@NiO-reduced graphene oxide heterostructure hydrogel and defective reduced graphene oxide hydrogel as free-standing anode and cathode for high-performance asymmetric supercapacitor

Yuqin Tiana,#, Weiwen Chena,b,#, Zenghui Qiua,b,*, Jian Jinga, Haijun Xua,b,*, Dingjie Panc, Shaowei Chenc,*

- aCollege of Mathematics & Physics, Beijing University of Chemical Technology, Beijing 100029, China

- bBeijing Bioprocess Key Laboratory, Beijing University of Chemical Technology, Beijing 100029, China

- cDepartment of Chemistry and Biochemistry, University of California, 1156 High Street, Santa Cruz, CA, 95064, United States

- #These authors contributed equally to the work.

- *E-mail: zhqiu@buct.edu.cn (Z.H.Q.), hjxu@buct.edu.cn (H.J.X.), and shaowei@ucsc.edu (S.W.C.)

List of Contents

- 2 tables

Table S1.  Comparison of specific capacitance of Ti3C2TX-based heterostructured electrodes.

| Materials | Electrolyte | Specific capacitance | Current density or Scan rate | Ref. |
| --- | --- | --- | --- | --- |
| Ti3C2TX/CNF/PC N,O co-doped C@Ti3C2TX Ti3C2TX/ZIF-67/CoV2O6 1T-MoS2/Ti3C2TX MnO2/Ti3C2TX/CC PPy/Ti3C2TX Ti3C2TX@PDA/NiCo2S4 400-KOH-Ti3C2TX Ti3C2TX/NF MXene/rGO Co2NiO4/Ti3C2TX Ti3C2/Ni-Co-Al-LDH Ti3C2TX@NiO-RGO V4C3TX@NiO-RGO | 1 M KOH 6 M KOH 1 M KOH 1 M H2SO4 1 M LiCl 1 M H2SO4 3 M KOH 1 M H2SO4 6 M KOH 3 M H2SO4 3 M KOH 1 M KOH 1 M KOH 1 M KOH | 143 mF cm−2 250.6 F g-1 285.5 F g−1 386.7 F g−1 411.5 F g−1 458 F g-1 495 F g−1 517 F g−1 654 F g-1 1040 F cm−3 719.5 F g−1 748.2 F g−1 966 F g−1 1014.5 F g−1 | 0.1 mA cm−2 1 A g-1 1 A g-1 1 A g−1 1 A g−1 2 mV s-1 2 mV s-1 1 A g−1 1 A g-1 2 mV s-1 0.5 A g−1 1 A g−1 1 A g−1 1 A g−1 | [1] [2] [3] [4] [5] [6] [7] [8] [9] [10] [11] [12] [13] This work |

Table S2 Comparison of specific capacitance for various carbon materials in aqueous electrolytes reported in the literature.

| Material | Electrolyte | Specific capacitance (F g-1) | Current density (A g-1) | Ref. |
| --- | --- | --- | --- | --- |
| NG-900 aNG TsG AC800NH3 LSG HPCFs C-900 PANecoal-AC5 AC800 N-HPCs PCPs DRGO | 6 M KOH 1 M KOH 6 M KOH 6 M KOH 1 M H3PO4 6 M KOH 6 M KOH 6 M KOH 7 M KOH 6 M KOH 1 M KOH 1 M KOH | 130 132.4 180 196 202 206 210 230 232 335 245 258 | 0.5 0.1 0.5 1 1 1 1 1 0.05 0.1 1 1 | [14] [15] [16] [17] [18] [19] [20] [21] [22] [23] [24] This work |

References

[1]    Chen, W. M.; Zhang, D. T.; Yang, K.; Luo, M.; Yang, P.; Zhou, X. Y. MXene (Ti3C2TX)/cellulose nanofiber/porous carbon film as free-standing electrode for ultrathin and flexible supercapacitors. Chemical Engineering Journal. 2021, 413, 127524.

[2]    Pan, Z. H.; Ji, X. H. Facile synthesis of nitrogen and oxygen co-doped C@Ti3C2 MXene for high performance symmetric supercapacitors. Journal of Power Sources. 2019, 439, 227068.

[3]    Liu, C. L.; Bai, Y.; Li, W. T.; Yang, F. Y.; Zhang, G. X.; Pang, H. In Situ Growth of Three-Dimensional MXene/Metal–Organic Framework Composites for High-Performance Supercapacitors. Angew Chem Int Ed Engl. 2022, 61, e202116282.

[4]     Wang, X.; Li, H.; Li, H.; Lin, S.; Ding, W.; Zhu, X. G.; Sheng, Z. G.; Wang, H.; Zhu, X. B.; Sun, Y. P. 2D/2D 1T-MoS2/Ti3C2 MXene Heterostructure with Excellent Supercapacitor Performance. Advanced Functional Materials. 2020, 30, 0190302.

[5]   Chen, X. H.; Liu, Y.; Zhou, Q.; Su, F. H. Facile Synthesis of MnO2/Ti3C2TX/CC as Positive Electrode of All-Solid-State Flexible Asymmetric Supercapacitor. ChemistrySelect. 2020, 5, 14768-14775.

[6]   Wei, D.; Wu, W. L.; Zhu, J. F.; Wang, C. W.; Zhao, C. H.; Wang, L. A facile strategy of polypyrrole nanospheres grown on Ti3C2-MXene nanosheets as advanced supercapacitor electrodes. Journal of Electroanalytical Chemistry. 2020, 877, 114538.

[7]    Wu, W. L.; Niu, D. J.; Zhu, J. F.; Gao, Y.; Wei, D.; Zhao, C. H.; Wang, C. W.; Wang, F.; Wang, L.;Yang, L. Q. Hierarchical architecture of Ti3C2@PDA/NiCo2S4 composite electrode as high-performance supercapacitors. Ceramics International. 2019, 45, 16261-16269.

[8]     Li, J.; Yuan, X. T.; Lin, C.; Yang, Y. Q.; Xu, L.; Du, X.; Xie, J. L.; Lin, J. H.; Sun, J. L. Achieving High Pseudocapacitance of 2D Titanium Carbide (MXene) by Cation Intercalation and Surface Modification. Advanced Energy Materials. 2017, 7, 1-6.

[9]    Guo, J.; Zhao, Y. Y.; liu, A. N.; Ma, T. L. Electrostatic self-assembly of 2D delaminated MXene (Ti3C2) onto Ni foam with superior electrochemical performance for supercapacitor. Electrochimica Acta. 2019, 305, 164-174.

[9]   Yan, J.; Ren, C. E.; Maleski, K.; Hatter, C. B.; Anasori, B.; Urbankowski, P.; Sarycheva, A.; Gogotsi, Y. Flexible MXene/Graphene Films for Ultrafast Supercapacitors with Outstanding Volumetric Capacitance. Advanced Functional Materials. 2017, 27, 1701264.

[10]    Song, J. R.; Hu, P. F.; Liu, Y.; Song, W. X.; Wu, X. Enhanced Electrochemical Performance of Co2NiO4/Ti3C2TX Structures through Coupled Synergistic Effects. ChemistrySelect. 2019, 4, 12886-12890.

[11]   Zhao, R. Z.; Wang, M. Q.; Zhao, D. Y.; Li, H.; Wang, C. X.; Yin, L. W. Molecular-Level Heterostructures Assembled from Titanium Carbide MXene and Ni-Co-Al Layered Double Hydroxide Nanosheets for All-solid-state Flexible Asymmetric High-Energy Supercapacitors. ACS Energy Letters. 2017, 3, 132-140.

[12]    Chen, W. W.; Peng, Y.; Qiu, Z. H.; Zhang, X.; Xu, H. J. 3D hierarchical Ti3C2TX@NiO-reduced graphene oxide heterostructure hydrogel as free-standing electrodes for high performance supercapacitor. Journal of Alloys and Compounds. 2022, 901, 163614.

[13]    Lee, K. H.; Oh, J.; Son, J. G.; Kim, H.; Lee, S. S. Nitrogen-Doped Graphene Nanosheets from Bulk Graphite using Microwave Irradiation. ACS Appl Mater Interfaces. 2014, 6, 6361-6368.

[14]   Zheng, B.; Chen, T. W.; Xiao, F. N.; Bao, W. J.; Xia, X. H. KOH-activated nitrogen-doped graphene by means of thermal annealing for supercapacitor. Journal of Solid State Electrochemistry. 2013, 17, 1809-1814.

[15]   Wen, P.; Gong, P. W.; Mi, Y. J.; Wang, J. Q.; Yang, S. R. Scalable fabrication of high quality graphene by exfoliation of edge sulfonated graphite for supercapacitor application. RSC Advances. 2014, 4, 35914-35918.

[16]    Benedetti, M.; Girelli, C. R.; Antonucci, D.; De Pascali, S. A.; Fanizzi, F. P. New method for the synthesis of [PtCl{ŋ1-CH2C(O)R}(N-N)] ketonyl derivatives starting from the Zeise’s salt. Inorganica Chimica Acta. 2014, 413, 109-114.

[17]    Guo, J. R.; Xu, X. T.; Hill, J. P.; Wang, L. P.; Dang, J. J.; Kang, Y. Q.; Li, Y. L.; Guan, Y. S.; Yamauchi, Y. Graphene–carbon 2D heterostructures with hierarchically-porous P, N-doped layered architecture for capacitive deionization. Chem Sci. 2021,12,10334-10340.

[18]    Lv, Y.; Gan, L. H.; Liu, M. X.; Xiong, W.; Xu, Z. J.; Zhu, D. Z.; Wright, D. S. A self-template synthesis of hierarchical porous carbon foams based on banana peel for supercapacitor electrodes. Journal of Power Sources. 2012, 209, 152-157.

[19]   Qiu, B.; Pan, C. T.; Qian, W. J.; Peng, Y. J.; Qiu, L. H.; Yan, F. Nitrogen-doped mesoporous carbons originated from ionic liquids as electrode materials for supercapacitors. Journal of Materials Chemistry A. 2013, 1, 6373-6378.

[20]    Zhao, H. Y.; Wang, L. X.; Jia, D. Z.; Xia, W.; Li, J.; Guo, Z. P. Coal based activated carbon nanofibers prepared by electrospinning. J. Mater. Chem. A. 2014, 2, 9338-9344.

[21]   Shang, T. X.; Zhang, M. Y.; Jin, X. J. Easy procedure to prepare nitrogen-containing activated carbons for supercapacitors. RSC Adv. 2014, 4, 39037-39044.

[22]     Yang, X. W.; Zhuang, X. D.; Huang, Y. J.; Jiang, J. Z.; Tian, H.; Wu, D. Q.; Zhang, F.; Mai, Y. Y.; Feng, X. L. Nitrogen-Enriched Hierarchically Porous Carbons Fabricated by Graphene Aerogel Templated Schiff-base Chemistry for High Performance Electrochemical Capacitors. Polymer Chemistry. 2015, 6, 1088-1095.

[23]    Yi, H.; Wang, H. W.; Jing, Y. T.; Peng, T. Q.; Wang, X. F. Asymmetric supercapacitors based on carbon nanotubes@NiO ultrathin nanosheets core-shell composites and MOF-derived porous carbon polyhedrons with super-long cycle life. Journal of Power Sources. 2015, 285, 281-290.