LIST OF TABLES

| Caption | No. |
| --- | --- |
| Surface-active properties of the prepared cationic imine surfactants (ICS-10 and ICS-14) from the surface tension and conductivity measurements at 25 ºC | Table 1 |
| Corrosion parameters obtained from PDP of C- steel electrode in 1 M HCl solution containing different concentrations of ICS-10 and ICS-14 surfactants | Table 2 |
| The values corrosion rate, activation energy and heat of adsorption of carbon steel in 1 M HCl and 0.0005 M ICS-10 and ICS-14 | Table 3 |
| Quantum parameters of ICS-10 and ICS-14 inhibitor molecules | Table 4 |

Table 1:

| Comp. |  |  | Surface tension measurements |  |  |  |  | Conductivity measurements |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | CMCa (mM L-1) | CMCb (mM L-1) |  | γCMC (mN/m) | ΠCMC (mN/m) | Γmax ×1011 (mol cm-2) | Amin (nm2) | CMC (mM L-1) | α | β | (KJ mol-1) | (KJ mol-1) |
| ICS-10 | 1.34 | 0.95 |  | 36.17 | 35.83 | 7.31 | 1.88 | 1.17 | 0.44 | 0.56 | -26.66 | -30.72 |
| ICS-14 | 0.83 | 0.79 |  | 34.46 | 37.54 | 6.11 | 2.68 | 0.86 | 0.49 | 0.51 | -26.53 | -32.29 |

aCMC values obtained from surface tension measurements in distilled water

bCMC values obtained from surface tension measurements in 1.0 M HCl

Table 2:

| Inhibitor code | Inh. Conc. (M) | βa mV. decade-1 | β-c mV. decade-1 | Ecor mV (SCE) | icor µA/cm2 | IE/% | θ |
| --- | --- | --- | --- | --- | --- | --- | --- |
| - | 0 | 63 | 214 | -379 | 720 | - | - |
| ICS-10 | 5 × 10-6 | 62 | 221 | -373 | 367 | 49.02 | 0.4902 |
|  | 1 × 10-5 | 56 | 237 | -372 | 346 | 51.94 | 0.5194 |
|  | 5 × 10-5 | 50 | 208 | -374 | 170 | 76.39 | 0.7639 |
|  | 1× 10-4 | 46 | 242 | -371 | 102 | 85.83 | 0.8583 |
|  | 5 × 10-4 | 55 | 262 | -380 | 61 | 91.53 | 0.9153 |
| ICS-14 | 5 × 10-6 | 51 | 220 | -364 | 203 | 71.81 | 0.7181 |
|  | 1 × 10-5 | 50 | 212 | -384 | 126 | 82.50 | 0.8250 |
|  | 5 × 10-5 | 45 | 212 | -377 | 84 | 88.33 | 0.8833 |
|  | 1× 10-4 | 39 | 188 | -386 | 47 | 93.47 | 0.9347 |
|  | 5 × 10-4 | 43 | 188 | -397 | 39 | 94.58 | 0.9458 |

Table 3: The values corrosion rate, activation energy and heat of adsorption of carbon steel in 1 M HCl and 0.0005 M ICS-10 and ICS-14

| Solution | CR1 293 K | CR2 333 K | θ1 293 K | θ2 333 K | Ea kJ. mol-1 | Qads kJ. mol-1 |
| --- | --- | --- | --- | --- | --- | --- |
| Blank | 1.671×10-4 | 4.018×10-3 | - | - | 64.498 | - |
| ICS-10 | 1.504×10-5 | 3.221×10-3 | 0.910 | 0.198 | 108.858 | -75.276 |
| ICS-14 | 9.758×10-6 | 2.87×10-3 | 0.941 | 0.285 | 115.290 | -74.980 |

Table 4:

| Parameters | ICS-10 | ICS-14 |
| --- | --- | --- |
| EHOMO (eV) | -4.71 | -4.69 |
| ELUMO (eV) | -1.33 | -1.34 |
| ΔE (eV) | 3.38 | 3.35 |
| μ (Debye) | 13.23 | 13.31 |
| η (eV) | 1.69 | 1.68 |
| σ (eV)-1 | 0.59 | 0.60 |
| ΔN (e) | 0.53 | 0.54 |