Electronic Supplementary Information

Resculpting Carbon dots via electrochemical etching

Qingsong Yang1,2, Spyridon Gavalas2, Aleksander Ejsmont2,3, Marta J. Krysmann4, Jiangtao Guo1, Li Li1, Xuhong Guo1,5*, Antonios Kelarakis2*

1State-Key Laboratory of Chemical Engineering, East China University of Science and Technology, Shanghai, China,

2UCLan Research Centre for Smart Materials, School of Natural Sciences, University of Central Lancashire, Preston PR12HE, UK

3Adam Mickiewicz University in Poznań, Faculty of Chemistry, Department of Chemical Technology, Uniwersytetu Poznańskiego 8, 61-614 Poznań, Poland

4UCLan Research Centre for Smart Materials, School of Dentistry, University of Central Lancashire, Preston PR12HE, UK

5Engineering Research Centre of Materials Chemical Engineering of Xinjiang Bingtuan, Shihezi, University, Shihezi, China

SI Figure 1. Normalized (with respect to the Imax at λex=380 nm) PL spectra of 0.01 mg mL–1 aqueous dispersions of C-dots. The excitation wavelength (λex) was varied from 320 to 500 nm as indicated.

SI Figure 2. 0.02 mg ml–1 C-dots dispersions that have been subjected to chronoamperometry treatments for 60 s at 2.0 V in the presence of 0.05, 0.10, 0.15, 0.20, 0.25, 0.30 M KCl. (a) PL spectra (λex = 410 nm) and (b) the corresponding maximum PL intensity (Imax) as a function of KCl concentration.

SI Figure 3. PL spectra (λex = 410 nm) of 0.02 mg ml–1 C-dots pretreated with 1mM NaClO solution for 48 h  and then subjected to chronoamperometry treatments for 60s at the voltages indicated.

SI Figure 4. FTIR spectra of C-dots prior (lower black line) and after (upper red line) the chronoamperometry treatment at 2.0 V for 60 s.

S.I. Table 1. Analysis of the C1s XPS spectrum of untreated C-dots.

| Chemical Bind | Combined energy peak position (eV) | Half peak width (eV) | Peak area % |
| --- | --- | --- | --- |
| sp2 | 284.19 | 1.63 | 19.1 |
| sp3 | 284.8 | 2.26 | 60.6 |
| C–O | 286.05 | 0.50 | 2.4 |
| C=O | 287.96 | 1.65 | 17.8 |
| π–π* | 291.05 | 0.50 | 0.1 |

S.I. Table 2. Analysis of the C1s XPS spectrum of C-dots that have been subjected to chronoamperometry treatment a 2.0 V for 60 s.

| Chemical Bind | Combined energy peak position (eV) | Half peak width (eV) | Peak area % |
| --- | --- | --- | --- |
| sp2 | 284.2 | 0.96 | 4.9 |
| sp3 | 284.81 | 1.7 | 42.4 |
| C–O | 285.94 | 2.29 | 39.6 |
| C=O | 287.97 | 1.17 | 13.1 |