Table 1. Summary and comparison of the pre-set versus deconvoluted statistical parameters for the four synthetic multimodal datasets following a normal distribution.

| Dataset ID (type) | Mode ID (# of data) | Mean (m) |  | Standard deviation (s) |  |  | Fraction (A) (vol.%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Pre-set | Deconvoluted | Pre-set | Deconvoluted | Pre-set |  | Deconvoluted |
| I (equal fraction) | 1 (1,000) | 200.00 | 202.30 | 10.00 | 10.29 | 33.33 |  | 33.81 |
|  | 2 (1,000) | 220.00 | 233.18 | 10.00 | 9.79 | 33.33 |  | 38.10 |
|  | 3 (1,000) | 240.00 | 255.60 | 15.00 | 13.66 | 33.33 |  | 28.09 |
| II (unequal fraction) | 1 (3,000) | 300.00 | 300.00 | 10.00 | 10.23 | 50.00 |  | 50.00 |
|  | 2 (1,000) | 320.00 | 320.00 | 15.00 | 12.81 | 16.67 |  | 16.70 |
|  | 3 (2,000) | 340.00 | 340.00 | 30.00 | 28.85 | 33.33 |  | 33.30 |
| III (equal fraction) | 1 (3,000) | 200.00 | 203.83 | 10.00 | 10.32 | 20.00 |  | 20.05 |
|  | 2 (3,000) | 300.00 | 303.09 | 20.00 | 19.77 | 20.00 |  | 19.43 |
|  | 3 (3,000) | 360.00 | 364.21 | 18.00 | 19.65 | 20.00 |  | 21.17 |
|  | 4 (3,000) | 400.00 | 404.04 | 15.00 | 15.26 | 20.00 |  | 19.26 |
|  | 5 (3,000) | 450.00 | 451.15 | 21.00 | 21.49 | 20.00 |  | 20.08 |
| IV (unequal fraction) | 1 (3,000) | 200.00 | 201.88 | 10.00 | 10.30 | 15.00 |  | 15.20 |
|  | 2 (2,000) | 250.00 | 251.02 | 20.00 | 18.52 | 10.00 |  | 9.48 |
|  | 3 (4,000) | 310.00 | 312.59 | 15.00 | 15.81 | 20.00 |  | 21.86 |
|  | 4 (5,000) | 360.00 | 363.40 | 25.00 | 22.95 | 25.00 |  | 22.93 |
|  | 5 (6,000) | 415.00 | 416.65 | 18.00 | 17.79 | 30.00 |  | 30.53 |

Table 2. Results of qualitative and quantitative mineralogical analyses by XRD for the KS-45, KS-52, and Longmaxi shale.

| Mineral | Ideal chemical formula | Specific gravity | Weight fraction (wt.%) |  |  | Volume fraction (vol.%) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | KS-45 | KS-52 | Shale | KS-45 | KS-52 | Shale |
| Quartz | SiO2 | 2.65 | 53.23 | 17.99 | 43.40 | 53.50 | 19.57 | 43.80 |
| Orthoclase | KAlSi3O8 | 2.61 | 6.06 | / | / | 6.18 | / | / |
| Albite | NaAlSi3O8 | 2.61 | 18.17 | 2.31 | 23.40 | 18.54 | 2.55 | 23.60 |
| Biotite | K(Mg, Fe)3(AlSi3O10)(F,OH) | 3.05 | / | 5.18 | / | / | 4.90 | / |
| Muscovite | KAl2(AlSi3O10)(F,OH)2 | 2.88 | / | 25.56 | 12.00 | / | 25.58 | 10.90 |
| Calcite | CaCO3 | 2.71 | 13.09 | 1.67 | 2.30 | 12.86 | 1.78 | 2.20 |
| Illite | KAl2(AlSi3)O10(OH)2 | 2.69 | 8.10 | 24.66 | 10.00 | 8.01 | 26.42 | 8.90 |
| Chlorite | Mg5Al(AlSi3)O10(OH)8 | 3.20 | / | 19.30 | 5.20 | / | 17.38 | 5.30 |
| Hematite | Fe2O3 | 5.26 | / | 3.33 | / | / | 1.82 | / |
| Rutile | TiO2 | 4.01 | 1.35 | / | / | 0.90 | / | / |
| Pyrite | FeS2 | 5.10 | / | / | 2.00 | / | / | 1.30 |
| Organic matter | / | 1.06 |  |  | 1.70 |  | / | 4.00 |

Table 3. Summary of the Young’s moduli (unit: GPa) of individual minerals or phases for the three rock samples determined by statistical deconvolution of nanoindentation data.

| Mineral or phase | This study |  |  | Reported value (Reference) |
| --- | --- | --- | --- | --- |
|  | KS-45 | KS-52 | Shale |  |
| Quartz | 94.24 | 67.12 | 90.39 | 65.01 – 105.80 17,41 |
| Feldspar | 76.25 | / | / | 51.10 – 85.0 27,42 |
| Muscovite | / | / | 73.59 | 69.05 – 77.5 8,1,2 |
| Calcite | 61.79 | / | / | 64.0 ± 8.00 3 |
| Albite | / | / | 56.79 | 59.0 ± 3.00 4 |
| Mica | / | 49.12 | / | 51.0 ± 4.00 5 |
| Clay matrix | 10.62 | 11.12 | 27.99 | 12.0 – 33.10 6,7 |
| Organic matter | / | / | 15.99 | 0 – 25.00 8 |

Table 4. Summary of the fractions of different particle size groups in flocculated illite suspensions determined by the statistical deconvolution (note that the sum of fractions for ass particle size groups is 1.00)

| Particle group | Size range (μm) | Population fraction, A (%) |  |  |
| --- | --- | --- | --- | --- |
|  |  | pH = 8.61 | pH = 4.51 | pH = 2.25 |
| Primary particles | < 10 | 57.37 | / | 0.45 |
| Flocculi | 10 – 30 | 42.63 | 26.62 | / |
| Microflocs | 30 – 200 | / | 13.56 | 33.66 |
| Macroflocs | > 200 | / | 59.82 | 65.89 |

New References cited in tables:

1.	Ma, F. et al. Distinct responses of nanostructured layered muscovite to uniform and nonuniform straining. Journal of Materials Science 54, 1077–1098 (2019).

2.	Lu, Y. et al. Characterization of Shale Softening by Large Volume-Based Nanoindentation. Rock Mechanics and Rock Engineering 53, 1393–1409 (2020).

3.	Merkel, C. et al. Mechanical properties of modern calcite- (Mergerlia truncata) and phosphate-shelled brachiopods (Discradisca stella and Lingula anatina) determined by nanoindentation. J Struct Biol 168, 396–408 (2009).

4.	Brown, J. M., Abramson, E. H. & Angel, R. J. Triclinic elastic constants for low albite. Phys Chem Miner 33, 256–265 (2006).

5.	Li, Y. et al. Cross-scale characterization of sandstones via statistical nanoindentation: Evaluation of data analytics and upscaling models. International Journal of Rock Mechanics and Mining Sciences 142, 104738 (2021).

6.	Luo, S. et al. Cross-scale characterization of the elasticity of shales: Statistical nanoindentation and data analytics. Journal of the Mechanics and Physics of Solids 140, 103945 (2020).

7.	Luo, S. et al. Big Data Nanoindentation and Analytics Reveal the Multi-Staged, Progressively-Homogenized, Depth-Dependent Upscaling of Rocks’ Properties. Rock Mechanics and Rock Engineering vol. 54 (Springer Vienna, 2021).

8.	Eliyahu, M., Emmanuel, S., Day-Stirrat, R. J. & Macaulay, C. I. Mechanical properties of organic matter in shales mapped at the nanometer scale. Mar Pet Geol 59, 294–304 (2015).