Supporting information

Sorption and transport of Mn2+ in soil amended with alkali modified pomelo biochar

Qiang Ana, b*, Sheng Zhub, Zheng Lib, Shuman Dengb, Fanyu Mengb, Ningjie Jinb

a The Key Laboratory of Eco-Environment in Three Gorges Reservoir Region, Chongqing University, Chongqing 400045, PR China

b College of Environment and Ecology, Chongqing University, Chongqing 400045, PR China

* Corresponding author at: The Key Laboratory of Eco-Environment in Three Gorges Reservoir Region, Chongqing University, Chongqing 400045, PR China

E-mail address: anqiang@cqu.edu.cn (Qiang, An)

Telephone: +86 13996036767

Contents

Fig. S1. Schematic representation of the Mn2+ transport test.

Fig. S2. SEM image (a-b): B0-S (c-d): B10-S (e-f): MBC.

Table S1 Fitting parameters of adsorption kinetics fitted by pseudo first order, pseudo second order and intra-particle diffusion model.

Table S2 Fitting parameters of adsorption isotherm fitted by Langmuir and Freundlich model.

Table S3 Pearson’s correlation coefficients between parameters of adsorption and physicochemical properties of soil.

Table S4 Pearson’s correlation coefficients between parameters of transport and adsorption or saturated hydraulic conductivity.

Fig. S1. Schematic representation of the Mn2+ transport test.

Fig. S2. SEM image (a-b): B0-S (c-d): B10-S (e-f): MBC.

Table S1

Fitting parameters of adsorption kinetics fitted by Pseudo-first-order, Pseudo-second-order, Intra-particle diffusion model.

| Soil | Pseudo-first-order model |  |  | Pseudo-second-order model |  |  | Intra-particle diffusion model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | k1 (min-1) | qe (mg·g-1) | R2 | k2 (g·mg-1·min-1) | qe (mg·g-1) | R2 | k (mg·g-1·min-0.5) | b | R2 |
|  |  |  |  |  |  |  |  | (mg·g-1) |  |
| B0-S | 0.019 | 4.074 | 0.912 | 0.006 | 4.384 | 0.970 | 0.077 | 1.988 | 0.702 |
| B1-S | 0.036 | 4.240 | 0.693 | 0.012 | 4.497 | 0.870 | 0.068 | 2.552 | 0.822 |
| B3-S | 0.031 | 5.261 | 0.516 | 0.009 | 5.581 | 0.767 | 0.087 | 3.087 | 0.862 |
| B5-S | 0.044 | 5.604 | 0.635 | 0.012 | 5.883 | 0.869 | 0.078 | 3.682 | 0.828 |
| B10-S | 0.027 | 7.303 | 0.361 | 0.004 | 7.922 | 0.620 | 0.148 | 3.709 | 0.952 |

Table S2

Fitting parameters of adsorption isotherm fitted by Langmuir and Freundlich model.

| Soil | Langmuir model |  |  | Freundlich model |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qmax (mg·g-1) | KL (L·mg-1) | R2 | Kf (mg·g-1·Ln·mg-n) | n | R2 |
| B0-S | 5.611 | 0.015 | 0.963 | 0.452 | 0.426 | 0.939 |
| B1-S | 5.839 | 0.022 | 0.976 | 0.670 | 0.377 | 0.929 |
| B3-S | 6.279 | 0.028 | 0.934 | 0.817 | 0.367 | 0.998 |
| B5-S | 6.580 | 0.037 | 0.938 | 0.991 | 0.350 | 0.993 |
| B10-S | 8.706 | 0.071 | 0.818 | 2.068 | 0.287 | 0.982 |

Table S3

Pearson’s correlation coefficients between parameters of adsorption and physicochemical properties of soil.

| Parameters | pH | Eh | CEC | TOC |
| --- | --- | --- | --- | --- |
| qe | 0.897* | -0.811 | 0.822 | 0.999** |

Significance between parameters was denoted as *p < 0.05, **p < 0.01. qe was selected at C0 = 300 mg·L-1.

Table S4

Pearson’s correlation coefficients between parameters of transport and adsorption or saturated hydraulic conductivity.

| Parameters | qe | Ks |
| --- | --- | --- |
| R | 0.973** | -0.961** |

-Significance between parameters was denoted as **p < 0.01. When Pearson’s correlation coefficient between qe and R was calculated, qe at C0 was 300 mg·L-1 and R at the UMS filling way were used.