Supporting Information for

Environmental-friendly regenerated lignocellulose functionalized cotton fabric to prepare multi-functional degradable membrane for efficient oil-water separation and solar seawater desalination

Jiangyi Li1, Junkai Gao1, Jiangyu Fang1, Tian Ling1, Mengsheng Xia1, Xue Cao1, Zhi Han2, Yan Chen1

1 School of Naval Architecture and Maritime, Zhejiang Ocean University, Zhoushan 316022, China.

2 School of Energy and Power Engineering, Jiangsu University, Zhenjiang 212013, China



Corresponding author. Tel.: +86 580 2550623.  E-mail: chenyan@zjou.edu.cn.

Fig.S1 The preparation process of DES

Table S1. Elemental compositions of membrane surface

| Membranes | Composition (%) |  |  | Element ratio |
| --- | --- | --- | --- | --- |
|  | C | O | N | O/C |
| CF | 74.57 | 25.06 | 0.37 | 0.34 |
| LC@CF | 65.29 | 34.47 | 0.24 | 0.53 |
| LCPT@CF | 62.35 | 37.09 | 0.56 | 0.59 |

Fig.S2 (a) Biomicroscope image of olive oil-in-water emulsion. (b) Biomicroscope image of olive oil-in-water emulsion after 48 hours.

Comparison of LCPT@CF and other cotton fabric membranes used for the emulsion separation

As shown in Table S2, the LCPT@CF and other cotton fabric membranes used for the emulsion separation were compared in terms of separation efficiency, materials and environmental hazards. The results proved that the LCPT@CF possessed outstanding separation efficiency for oil-in-water emulsion. In addition, the LCPT@CF had excellent environmental friendliness, which was attributed to that lignocellulose and PT complexes had no pollution to the environment. Moreover, the preparation of the LCPT@CF was simple and cost-effective. Therefore, the LCPT@CF possessed great potential for the real-life application in oil-water separation.

Table S2. Comparison of LCPT@CF and other cotton fabric membranes used for the emulsion separation

| Membranes | Coating material | Environmental hazard | Separation efficiency (%) | Ref. |
| --- | --- | --- | --- | --- |
| Mg(OH)2@cotton fabric | Mg(OH)2 | Middle | >99.5 | 1 |
| Caffeic acid/Fe@cotton fabric | Caffeic acid/Fe | Middle | >99.0 | 2 |
| Robustly superhydrophobic cotton fibers | ZnO | Middle | >91.0 | 3 |
| Eleostearic acid-SiO2@cotton fabric | SiO2 and eleostearic acid | Middle | >99.5 | 4 |
| CS@CF | Cement-sand | Small | >97.2 | 5 |
| Cellulose-coated cotton fabric | Cellulose | Small | >93.2 | 6 |
| Superwetting cellulose II based membranes | Cellulose | Small | >99.0 | 7 |
| LCPT@CF | Regenerated lignocellulose | None | >99.9 | This work |

References

1.	Hu, R. et al. Fabrication of special wettability functionalized Mg(OH)2@cotton fabric for oil/water mixtures and emulsions separation. Cellulose 27, 7739–7749 (2020).

2.	Zhou, Q., Yan, B., Xing, T. & Chen, G. Fabrication of superhydrophobic caffeic acid/Fe@cotton fabric and its oil-water separation performance. Carbohydrate Polymers 203, 1–9 (2019).

3.	Wang, J., Han, F., Liang, B. & Geng, G. Hydrothermal fabrication of robustly superhydrophobic cotton fibers for efficient separation of oil/water mixtures and oil-in-water emulsions. Journal of Industrial and Engineering Chemistry 54, 174–183 (2017).

4.	Lin, H. et al. Facile fabrication of natural superhydrophobic eleostearic acid-SiO2@cotton fabric for efficient separation of oil/water mixtures and emulsions. Sustainable Materials and Technologies 32, e00418 (2022).

5.	Yang, S., Li, M., Fang, G., Xue, M. & Lu, Y. Flexible cement-sand coated cotton fabrics with superhydrophilic and underwater superoleophobic wettability for the separation of water/oil mixtures and oil-in-water emulsions. Colloids and Surfaces A: Physicochemical and Engineering Aspects 608, 125611 (2021).

6.	Zhang, Y.-R., Chen, J.-T., Hao, B., Wang, R. & Ma, P.-C. Preparation of cellulose-coated cotton fabric and its application for the separation of emulsified oil in water. Carbohydrate Polymers 240, 116318 (2020).

7.	Yang, S., Chen, L., Wang, S. & Liu, S. Production of superwetting cellulose II based membranes with excellent oil/water emulsions separation performance. Industrial Crops and Products 177, 114554 (2022).

Corresponding author. Tel.: +86 580 2550623. E-mail: chenyan@zjou.edu.cn.