SUPPORTING INFORMATION

Magnetically-activated 3D printable PLA/PCL/Fe3O4 composites for magnetic induction heating generation

Itziar Galarreta-Rodriguez1-2* (0000-0001-9172-4319), Alberto Lopez-Ortega1-2*(0000-0003-3440-4444), Eneko Garayo1-2(0000-0002-3144-7898), Juan Jesús Beato-López1-2, Paulo La Roca1-2-3(0000-0003-0856-6052), Vicente Sanchez-Alarcos1-2(0000-0002-9282-7683), Vicente Recarte1-2(0000-0002-5342-5403), Cristina Gómez-Polo1-2 (0000-0001-8919-4822) and Jose Ignacio Pérez-Landazábal1-2(0000-0003-1172-6141)

1Departamento de Ciencias, Universidad Pública de Navarra, Campus de Arrosadía, 31006, Pamplona, Spain

2Institute for Advanced Materials and Mathematics (INAMAT2), Universidad Pública de Navarra, Campus de Arrosadía, 31006, Pamplona, Spain

3Centro Atómico Bariloche (CNEA), CONICET, Bariloche 8400, Argentina

*Itziar Galarreta-Rodriguez: galarretarodriguez.itziar@gmail.com

*Alberto Lopez-Ortega: lopezortega.alberto@gmail.com

| Table S1. Weight loss percentages for prepared PLA/PCL and PLA/PCL/MNP filaments |  |  |  |
| --- | --- | --- | --- |
|  | PLA | PCL | Rest |
| Composite | % weight | % weight | % weight |
| P0% | 9 | 90 | 1 |
| P5% | 13 | 82 | 5 |
| P10% | 7 | 81 | 12 |
| P20% | 8 | 71 | 21 |
| P40% | 7 | 53 | 40 |
| P60% | 6 | 37 | 57 |

Fig. S1. AC hysteresis loops of the filaments measured at 311 kHz frequency. SAR values are obtained from the area. The magnetization is normalized by the mass of NPs

Fig. S2. Thermogravimetry and DTG curves of net PLA and PCL polymers.