Supporting Information

Overcoming lattice mismatch for heterostructures

Wen Kiat Chan,a# Zhongzheng Yu, a,b#*  Donglei Zhou,c Junzhi Ye,b Alasdair Tew,b Lars van Turnhout,b Akshay Rao,b and Timothy Thatt Yang Tana*

a School of Chemistry, Chemical Engineering and Biotechnology, Nanyang Technological University, 637459, Singapore

b Cavendish Laboratory, University of Cambridge, Cambridge, CB3 0HE, United Kingdom

c State Key Laboratory of Integrated Optoelectronics, College of Electronic Science and Engineering, Jilin University, Changchun, 130012, China

*Corresponding author at: School of Chemistry, Chemical Engineering and Biotechnology, Nanyang Technological University, 637459, Singapore.

E-mail address: yuzh0010@e.ntu.edu.sg (Z. Yu), tytan@ntu.edu.sg (T.T.Y. Tan).

#These authors contributed equally: Wen Kiat Chan, Zhongzheng Yu.

Materials

Yttrium (III) acetate hydrate (Y(CH3COO)3∙xH2O), gadolinium acetate hydrate (Gd(CH3COO)3∙xH2O), ytterbium acetate hydrate (Yb(CH3COO)3∙xH2O), thulium acetate hydrate (Tm(CH3COO)3∙xH2O), cesium carbonate (Cs2CO3, 99.9%), lead chloride (PbCl2, 99.999%), lead bromide (PbBr2, 99.99%), lead iodide (PbI2, 99.999%), 1-octadecene (ODE, 90%), oleic acid (OA, 90%), oleylamine (OAm, 70%) and n-hexane (HPLC grade) were purchased from Sigma-Aldrich and used directly without any further purification.

Supplementary Fig. 1 (a)(i) TEM image of ultrasmall α-NaYF4 LnNPs. TEM images of (ii) α-NaYF4@CsPbCl3 NCs and nanoplatelets, (iii) α-NaYF4@CsPbBr3 NCs and (iv) α-NaYF4@CsPbI3 NWs and NCs. (b) EDS elemental mapping of (i) α-NaYF4@CsPbCl3 NCs, (ii) α-NaYF4@CsPbBr3 NCs, and (iii) α-NaYF4@CsPbI3 NWSCs.

Supplementary Fig. 2 (a) HRTEM images of (i) ultrasmall α-NaYF4 LnNPs, (ii) α-NaYF4@CsPbCl3, (iii) α-NaYF4@CsPbBr3 and (iv) α-NaYF4@CsPbI3.  (b) XRD patterns of α-NaYF4@CsPbX3 samples and α-NaYF4.

Supplementary Fig. 3 Particle size distributions of (a) pure (i) CsPbCl3 NCs, (ii) CsPbBr3 NCs, and (iii) CsPbI3 NCs, (b) α-NaYF4 LnNPs, (c) CsPbCl3+α-NaYF4 (i) nanoplatelet length, and (ii) nanoplatelet width, and (d) (i) α-NaYF4@CsPbCl3, (ii) α-NaYF4@CsPbBr3 and (iii) α-NaYF4@CsPbI3.

Supplementary Fig. 4 TEM (i) and HRTEM (ii) images of pure (a) CsPbCl3, (b) CsPbBr3, and (c) CsPbI3 samples synthesized using hot injection. (d) XRD patterns of pure CsPbX3 samples.

Supplementary Fig. 5 Emission spectra of (a) pure CsPbCl3 and α-NaYF4@CsPbCl3, (b) pure CsPbBr3 and α-NaYF4@CsPbBr3 (inset: Enlarged portion of emission spectra showing blue shifted emission for CsPbBr3+α-NaYF4 compared to pure CsPbBr3), and (c) pure CsPbBr3 and α-NaYF4@CsPbI3. Samples excited under 365 nm light and dispersed in hexane.

Supplementary Fig. 6 ECPs of pure (a) CsPbCl3, (b) CsPbBr3, and (c) CsPbI3. Samples excited under 365 nm light and dispersed in hexane.

Supplementary Fig. 7 ECPs of (a)(i) α-NaYF4@CsPbCl3, (ii) α-NaYF4@CsPbBr3, and (iii) α-NaYF4@CsPbI3. (b) ECP of β-NaGdF4 @CsPbBr3. Samples excited under 365 nm light and dispersed in hexane.

Supplementary Fig. 8 Photographs of samples taken under UV light.

Supplementary Fig. 9 UV-Vis absorption spectra for (a) pure (i) CsPbCl3, (ii) CsPbBr3, and (iii) CsPbI3, and (b)(i) α-NaYF4@CsPbCl3+, (ii) α-NaYF4@CsPbBr3, and (iii) α-NaYF4@CsPbI3.

Supplementary Fig. 10 Particle size distribution for (a) β-NaGdF4, and (b) β-NaGdF4 @CsPbBr3.

Supplementary Fig. 11 (a) HRTEM images of (i) β-NaGdF4, and (ii) β-NaGdF4@CsPbBr3. (b) XRD patterns of β-NaGdF4 and β-NaGdF4@CsPbBr3. (c) UV-Vis absorption spectra of β-NaGdF4@CsPbBr3.

Supplementary Fig. 12 TEM image of (a) α-NaYF4:Yb,Tm LnNPs and (b) β- NaGdF4:Yb,Tm@CsPbBr3.  (c) HRTEM of α-NaYF4:Yb,Tm@CsPbBr3. (d) EDS elemental mapping of α-NaYF4:Yb,Tm@CsPbBr3.

Supplementary Fig. 13 (a) Particle size distributions of (i) α-NaYF4:Yb,Tm and (ii) β-NaGdF4:Yb,Tm  LnNPs. (b) Particle size distributions of (i) α-NaYF4:Yb,Tm@CsPbBr3 and (ii) β-NaGdF4:Yb,Tm@CsPbBr3.

Supplementary Fig. 14 (a) Emission spectra of α-NaYF4:Yb,Tm and β-NaGdF4:Yb,Tm  LnNPs under 980 nm laser excitation. (b) Absorption spectra of α-NaYF4:Yb,Tm and β-NaGdF4:Yb,Tm LnNPs in NIR range. Samples prepared with concentration of 20 mg ml-1. (c) Absorption spectra of (i) α-NaYF4:Yb,Tm@CsPbBr3 and (ii) β-NaGdF4:Yb,Tm@CsPbBr3 in visible range at different concentrations.

Supplementary Fig. 15 ECPs of (a) α-NaYF4:Yb,Tm@CsPbBr3 and (b) β-NaGdF4:Yb,Tm@CsPbBr3. Samples excited under 365 nm light and dispersed in hexane.

Supplementary Fig. 16 Photographs of samples taken with UV light and 980nm laser excitation.

Supplementary Fig. 17 TEM images of (a)(i) core LnNPs, (ii) core-shell LnNPs, (b)(i) CsPbCl3+CSS, (c)(i) CsPbBr3+CSS, and (d)(i) CsPbI3+CSS samples. HRTEM images of (b)(ii) CsPbCl3+CSS, (c)(ii) CsPbBr3+CSS, and (d)(ii) CsPbI3+CSS samples.

Supplementary Fig. 18 Particle size distributions of (a) (i) core LnNPs, (ii) core-shell LnNPs, (iii) CSS LnNPs, (b) CsPbCl3 NCs, and (c) CsPbBr3 NCs.

Supplementary Fig. 19 (a) Emission spectra of CSS LnNPs under 980nm laser excitation. Emission spectra of (b) CsPbCl3+CSS under (i) 980nm, (ii) 365nm excitation, (c) CsPbBr3+CSS under 365nm excitation, (d) CsPbI3+CSS under (i) 980nm, and (ii) 365nm excitation. Samples are dispersed in hexane. (e) XRD patterns of CSS LnNPs and CsPbX3+CSS samples. (f) NIR emission of CsPbCl3+CSS and CsPbBr3+CSS.

Supplementary Fig. 20 EDS scans of the (a) CsPbCl3+CSS, and (b) CsPbI3+CSS samples.

Supplementary Fig. 21 UV-Vis absorption spectra of (a) CsPbCl3+CSS, (b) CsPbBr3+CSS, and (c) CsPbI3+CSS samples.