Supplementary Figure Legend

Fig. S1 Cupriavidus necator GX_5 colonies grown on LB agar

Supplementary Table Heading

Table S1 The effect of initial mental concentration on adsorption capacity of Cupriavidus necator GX_5 for Cd (II)

Table S2 The effect of initial mental concentration on removal efficiency of Cupriavidus necator GX_5 for Cd (II)

Table S3 The effect of biosorbent dosage on adsorption capacity of Cupriavidus necator GX_5 for Cd (II)

Table S4 The effect of biosorbent dosage on removal efficiency of Cupriavidus necator GX_5 for Cd (II)

Supplementary Figure

Fig. S1 Cupriavidus necator GX_5 colonies grown on LB agar

Supplementary Table

Table S1 The effect of initial mental concentration on adsorption capacity of Cupriavidus necator GX_5 for Cd (II)

| D Initial Cd2+ concentration (mg/L) Adsorption capacity (mg/g) Biosorbents | 5 | 10 | 20 | 50 | 100 | 200 |
| --- | --- | --- | --- | --- | --- | --- |
| Live | 3.03h±0.12 | 4.29fgh±0.03 | 5.16efg±0.26 | 7.52cd±0.54 | 11.25b±0.88 | 17.17a±1.62 |
| Dead | 3.93gh±0.03 | 5.42ef±0.14 | 6.46de±0.44 | 8.76c±0.43 | 12.02b±1.45 | 17.55a±1.70 |

Table S2 The effect of initial mental concentration on removal efficiency of Cupriavidus necator GX_5 for Cd (II)

| D Initial Cd2+ concentration (mg/L) Removal efficiency (%) Biosorbents | 5 | 10 | 20 | 50 | 100 | 200 |
| --- | --- | --- | --- | --- | --- | --- |
| Live | 60.51b±2.36 | 42.91d±0.31 | 25.78f±1.32 | 15.05h±1.08 | 11.25i±0.88 | 8.58j±0.81 |
| Dead | 78.53a±0.60 | 54.23c±1.44 | 32.32e±2.19 | 17.52g±0.86 | 12.02i±1.45 | 8.77j±0.85 |

Table S3 The effect of biosorbent dosage on adsorption capacity of Cupriavidus necator GX_5 for Cd (II)

| Dosage (g/L) Adsorption capacity (mg/g) Biosorbents | 0.2 | 0.5 | 1.0 | 2.0 | 4.0 |
| --- | --- | --- | --- | --- | --- |
| Live | 15.97b±1.30 | 9.34de±0.91 | 7.33f±0.64 | 6.44fg±0.06 | 4.39h±0.12 |
| Dead | 21.47a±2.16 | 13.15c±1.01 | 9.57d±0.48 | 7.87ef±0.09 | 5.44gh±0.19 |

Table S4 The effect of biosorbent dosage on removal efficiency of Cupriavidus necator GX_5 for Cd (II)

| D Dosage (g/L) Removal efficiency (%) Biosorbents | 0.2 | 0.5 | 1.0 | 2.0 | 4.0 |
| --- | --- | --- | --- | --- | --- |
| Live | 6.39h±0.52 | 9.34g±0.91 | 14.65f±1.27 | 25.77d±0.23 | 35.15b±0.98 |
| Dead | 8.59g±0.87 | 13.15f±1.01 | 19.13e±0.95 | 31.49c±0.38 | 43.49a±1.54 |