Supporting Information

Prestoring Lithium into SnO2 Coated 3D Carbon Fiber Cloth Framework as Dendrite-Free Lithium Metal Anode

Tao Wei a, Yanyan Zhou a, Cheng Sun a, Lesheng Liu a, Sijia Wang a, Mengting Wang a, Ye Liu a, Shanliang Chen d, Quanchao Zhuang b,, Yongfu Tang c,

a School of Energy and Power, Jiangsu University of Science and Technology, Zhenjiang 212003, China.

b Li-ion Batteries Lab, School of Materials Science and Engineering, China University of Mining and Technology, Xuzhou, China.

c Hebei Key Laboratory of Applied Chemistry, School of Environmental and Chemical Engineering, Yanshan University, Qinhuangdao, 066004, China.

d Institute of Micro/Nano Materials and Devices, Ningbo University of Technology, Ningbo City, 315211, P.R. China.

Experimental Section

Materials Synthesis

Commercial carbon fiber cloths (CFCs) (Hesen Tech Co., Ltd) were treated with concentrated nitric acid before use, then ultrasonically cleaned with deionized water and alcohol, and finally dried under vacuum at 60°. For the synthesis of SnO2 nanoparticle on CFC, First, 1.077 g SnCl2·2H2O was dissolved in 48 mL N, N-dimethylformamide, which was denoted as solution A, and a piece of carbon cloth with a dimension of 2.5 cm × 2.5 cm was immersed in solution A with stirring for 30 minutes. Second, 0.428 g of terephthalic acid was dissolved in 12 mL of absolute ethanol, which was denoted as solution B. Then solution B was poured into the above solution and stirred until clarified. Third, the obtained solution was transferred into a 100 mL Teflonlined stainless steel autoclave and placed in an oven at 170 °C for 10 h. Afterwards, the CFC@SnO2 electrodes was dried at 60 °C for 6 h under vacuum, and then cut into a round shape with a diameter of 14 mm and thickness of 0.29 mm for use. The CFC@SnO2 electrodes was obtained by heating at 400 °C for 3 h at a ramp rate of 3°C min-1 in a muffle furnace. A piece of Li foil was first polished to remove impurities and then melted in a stainless-steel battery case above the heating stage at a temperature of 350 °C. Finally, a facile molten infusion approach used to be utilized to embed molten Li into the 3D CFC@SnO2 skeleton.

Materials Characterizations

At the scanning rate of 3°C min−1, X-ray diffractometer (XRD, Brook-D8 Advance) was used to study the crystal morphology of the material powder in the range of 10º to 50º. X-ray photoelectron spectroscopy (XPS, AXIS-ULTRA DLD) was employed to probe the electronic states of the Sn and O in the surface. The crystallization of nanomaterials was studied using transmission electron microscopy (TEM, JEOL 2100f, 200 kV) to observe the morphology and dispersion of nanoparticles, and scanning electron microscopy (SEM, JEOL JSM7500) was used to observe the high-resolution microstructure and the distribution of elements in microregions of the growths on the materials so that the nanoscale phase and grain size could be determined by lattice streaking.

Electrode fabrication and electrochemical Characterization

Full cells were prepared with a commercial LiFePO4 (LFP) cathode. The LFP powders, carbon black, and PVDF were mixed with the weight ratio of 7:2:1 using NMP as the solvent, subsequently coated on the aluminum foil and dried in a vacuum oven at 120 ℃ for 12 h after drying at 60 ℃ for 4 h. Electrochemical measurements were carried out using a two electrode cells assembled in an argon-filled glove box with water and oxygen contents below 1.0 ppm. A 1:1 mixture of ethylene carbonate (EC) and dimethyl carbonate (DMC) served as the electrolyte, which contained 1 M LiPF6. The dosage of electrolyte in every full cell was 30µL. Li foil was used as a counter electrode with a diameter of 15.6 mm and thickness of 0.45 mm, and polypropylene (Celgard 2400) membrane was employed as the separator. The galvanostatic charge/discharge experiments were carried out on a battery measurement system (LAND CT2001A, Wuhan Jinnuo Electronics, Ltd.). Electrochemical impedance spectroscopy (EIS) measurements and cyclic voltammetry (CV) were performed on CHI 660D (Shanghai Chen Hua Instrument Company, China) electrochemical workstation at room temperature. EIS measurements were carried out in the frequency range from 100 kHz to 0.01 Hz with an amplitude of 5 mV at open circuit voltage. CV curves were obtained in the range from 2.4-4 V at a scan rate of 0.2 mV s-1.

Fig. S1 XRD pattern of SnO2.

Fig. S2 (a) Coulombic efficiency of CFC and CFC@SnO2 electrodes in half cells at 1 mA cm-2 for 1 mAh cm-2. (b) Corresponding first circle discharge profiles.

Fig. S3 (a) Voltage profiles of metal Li plating/stripping in two symmetric cells (bare Li and CFC@SnO2@Li) at 2 mA cm-2 for 2 mAh cm-2.

Fig. S4 Nyquist plot of EIS spectra of bare Li and CFC@SnO2@Li symmetric cells (a) before cycling, (b) after 100 cycles at a current density of 1 mA cm-2 with a capacity of 1 mAh cm-2.

Fig. S5 Nyquist plots and their corresponding fitting curves of symmetric Li cells with different electrodes (inset is the equivalent circuit). CFC@SnO2@Li: (a) before and (b) after 100th cycles. Bare Li: (c) before and (d) after 100th cycles.

Fig. S6 (a) Typical capacity voltage curve of bare Li||LFP cell at different current rates of 0.2-5C. (b) Cycling performance of the CFC@SnO2@Li||LFP cell at 0.5C. (c) Corresponding charge-discharge profiles of that cell. (d) Cyclic voltammetry curves at 0.2 mV s−1.

Table S1. Weight of bare Li ,CFC, CFC@SnO2 and CFC@SnO2@Li electrode.

| Materials | Average weight/ mg |
| --- | --- |
| Bare Li | 41.0 |
| CFC | 22.0 |
| CFC@SnO2 | 25.0 |
| CFC@SnO2@Li | 60.0 |
| Li in CFC@SnO2@Li electrode | 35.0 |

The areal capacity of CFC@SnO2@Li electrode

= Theoretical specific capacity of Li × Areal loading of Li

= 3860 × 35 / 1.91 mAh cm−2

≈70.73 mA h cm−2

The specific capacity of CFC@SnO2@Li electrode

= Theoretical specific capacity of Li × Weight percentage of Li in the CFC@SnO2@Li electrode

= 3860 × 35 / 60 mAh g-1

≈ 2252 mAh g-1

Table S2. Comparison of the electrochemical performance of CFC@SnO2@Li with the previous literature results.

| Materials | Current density (mA cm−2) | Capacity (mAh cm-2) | Cycle number | Cyclic lifespan (h) | Refer- ences |
| --- | --- | --- | --- | --- | --- |
| CFC@SnO2@Li | 1 | 1 | 1000 | 2000 | This work |
|  | 2 | 2 | 1000 | 2000 |  |
|  | 5 | 5 | 800 | 1600 |  |
| Li coated SNF skeletons | 3 | 1 | 857 | 600 | [S1] |
|  | 5 | 1 | 1380 | 600 |  |
| Li@ZnO@CC | 1 | 2 | 280 | 560 | [S2] |
|  | 2 | 1 | 160 | 160 |  |
|  | 3 | 1 | 160 | 107 |  |
| CF@Sn@Li | 1 | 1 | 500 | 1000 | [S3] |
|  | 3 | 1 | 1000 | 700 |  |
| Li-Co3O4-NF | 1 | 1 | 500 | 1000 | [S4] |
|  | 3 | 1.5 | 480 | 480 |  |
| 3DHF-Li | 1 | 1 | 450 | 900 | [S5] |
|  | 3 | 1 | 500 | 320 |  |
| MCuF@Li | 1 | 2 | 300 | 600 | [S6] |
|  | 3 | 2 | 827 | 300 |  |
| CC@CN-Co | 2 | 1 | 800 | 800 | [S7] |
|  | 2 | 3 | 160 | 500 |  |
|  | 5 | 5 | 500 | 1000 |  |

Table S3. Simulation results of equivalent circuit in Fig. S5.

|  | Rs/Ω | Rint/Ω |
| --- | --- | --- |
| Bare Li (before) | 3.365 | 201.5 |
| Bare Li (after) | 9.692 | 15.558 |
| CFC@SnO2@Li (before) | 4.013 | 51.32 |
| CFC@SnO2@Li (after) | 5.415 | 3.766 |

Notes: Semicircles at high and low-frequency regions in the Nyquist plots are associated with the SEI formation on the electrode surface, and the charge transfer process between the electrode/electrolyte interface, respectively. Rs: electrolyte resistance; Rf: surface film resistance; Rct: charge transfer resistance; CPE: constant phase element; W1: Warburg element (open). Rint= Rf + Rct, representing interfacial resistance between the electrode and the electrolyte.

References

- Xia Y, Jiang Y, Qi YY, Zhang WQ, Wang Y, Wang SF et al (2019) 3D stable hosts with controllable lithiophilic architectures for high-rate and high-capacity lithium metal anodes. J Power Sources 442:227214. https://doi.org/10.1016/j.jpowsour.2019.227214.

- Jin DQ, Hu K, Hou R, Shang H, Wang XY, Ding Y et al (2021) Vertical nanoarrays with lithiophilic sites suppress the growth of lithium dendrites for ultrastable lithium metal batteries. Chem Eng J 405:126808. https://doi.org/10.1016/j.cej.2020.126808.

- Liu TC, Chen XD, Zhan CC, Cao XH, Wang YW, Liu JH (2020) Selective Lithium Deposition on 3D Porous Heterogeneous Lithiophilic Skeleton for Ultrastable Lithium Metal Anodes. Chem Nano Mat 6:1200-1207. https://doi.org/10.1002/cnma.202000220.

- Wei T, Lu JH, Zhang P, Yang G, Sun C, Zhou YY et al (2022) Metal-organic framework-derived Co3O4 modified nickel foam-based dendrite-free anode for robust lithium metal batteries. Chinese Chem Lett 26:107947. https://doi.org/10.1016/j.cclet.2022.107947.

- Qi YY, Lin L, Jian ZL, Qin KY, Tan YX, Zou YJ et al (2020) Three-Dimensional Hierarchical Framework Loaded with Lithiophilic Nanorod Arrays for High‐Performance Lithium-Metal Anodes. Chem Electro Chem 7:4201-4207. https://doi.org/10.1002/celc.202000858.

- Zhou Y, Zhao K, Han Y, Sun ZH, Zhang HT, Xu LQ et al (2019) A nitrogen-doped-carbon/ZnO modified Cu foam current collector for high-performance Li metal batteries. J Mater Chem A 7:5712-5718. https://doi.org/10.1039/c8ta12064a.

- Zhou T, Shen JD, Wang ZS, Liu J, Hu RZ, Ouyang LZ et al (2020) Regulating Lithium Nucleation and Deposition via MOF-Derived Co@C-Modified Carbon Cloth for Stable Li Metal Anode. Adv Funct Mater 30:1909159. https://doi.org/10.1002/adfm.201909159.

Corresponding author: T. Wei (wt863@just.edu.cn; wt863@126.com).

Corresponding author: Q. C. Zhuang (zhuangquanchao@126.com).

Corresponding author: Y. F. Tang (tangyongfu@ysu.edu.cn).