Supplementary material

An environmentally friendly method for extraction of Cobalt and Molybdenum from spent catalysts using deep eutectic solvents (DESs)

Ehsan Ebrahimi¹, Hassan Safari¹, Mohammad Rezaee ¹, Ali Rezaei ¹, Hadi Abdollahi*¹

¹School of Mining Engineering, College of Engineering, University of Tehran, Tehran, Iran

* Corresponding author. Tel./Fax: +98-21-88008838; +98-912-5032335

E-mail address: h_abdollahi@ut.ac.ir (H. Abdollahi).

ORCID: Hadi Abdollahi      http://orcid.org/0000-0002-9099-7451

Tables

Table S1 List of kinetic models used in this study and their equations

| No | Kinetic mechanisms | Model equations | Reference |
| --- | --- | --- | --- |
| 1 | Diffusion through the liquid film (constant size cp, sp, pp) | kt = X | (Levenspiel, 1998) |
| 2 | Diffusion through the product layer (constant size pp) | kt = X² | (Levenspiel, 1998) |
| 3 | Diffusion through the product layer (constant size cp) | kt= X+(1-X)ln(1-X) | (Levenspiel, 1998) |
| 4 | Diffusion through the product layer (Crank–Ginstling and Brounshtein Model sp) | kt = 1-3(1-X)2/3+2(1-X) | (Fogler, 2016) |
| 5 | Diffusion through the product layer (Jander's Equation sp) | kt =[1-1-X13]² | (Fogler, 2016) |
| 6 | Diffusion through the product layer and interfacial transfer | kt=13ln1-X–[1-(1-X)-1/3] | (Dickinson and Heal, 1999) |
| 7 | chemical reaction on the particle surface (constant size cp) | kt= 1-(1-X)1/2 | (Levenspiel, 1998) |
| 8 | chemical reaction on the particle surface (constant size sp) | kt= 1-(1-X)1/3 | (Levenspiel, 1998) |
| 9 | The surface chemical reaction (shrinking sp) | kt= 1-(1-0.45X)1/3 | (Padilla et al., 2008) |
| 10 | Mixed control model (surface reaction control; and diffusion through product layer) | kt =-ln(1-X) | (Sokić et al., 2009) |

X is the leaching efficiency of Cobalt/Molybdenum (%), k is the apparent rate constant, and t is the leaching time, h. (sp: spherical particles, pp: prismatic particles, cp: cylindrical particle)

Table S2 List of kinetic models calculated for (DES-1, Cobalt) at different temperatures and their correlation coefficients (R²), (0-48 hour)

| No | Kinetic Model equations | Correlation coefficients (R²) of kinetics models |  |  |
| --- | --- | --- | --- | --- |
|  |  | 100°C | 75°C | 50°C |
| 1 | kt = X | 0.0124 | 0.4693 | 0.835 |
| 2 | kt = X² | 0.9041 | 0.9339 | 0.9946 |
| 3 | kt= X+(1-X)ln(1-X) | 0.9645 | 0.9647 | 0.9862 |
| 4 | kt = 1-3(1-X)2/3+2(1-X) | 0.9808 | 0.9733 | 0.9819 |
| 5 | kt =[1-1-X13]² | 0.9964 | 0.9848 | 0.9717 |
| 6 | kt=13ln1-X–[1-(1-X)-1/3] | 0.982 | 0.9907 | 0.9465 |
| 7 | kt= 1-(1-X)1/2 | 0.5734 | 0.1741 | 0.008 |
| 8 | kt= 1-(1-X)1/3 | 0.7715 | 0.741 | 0.9245 |
| 9 | kt= 1-(1-0.45X)1/3 | 0.2578 | 0.5685 | 0.8717 |
| 10 | kt =-ln(1-X) | 0.948 | 0.1166 | 0.064 |

Table S3 List of kinetic models calculated for (DES-1, Molybdenum) at different temperatures and their correlation coefficients (R²), (0-48 hour)

| No | Kinetic Model equations | Correlation coefficients (R²) of kinetics models |  |  |
| --- | --- | --- | --- | --- |
|  |  | 100°C | 75°C | 50°C |
| 1 | kt = X | 0.361 | 0.5375 | 0.835 |
| 2 | kt = X² | 0.9416 | 0.9825 | 0.9946 |
| 3 | kt= X+(1-X)ln(1-X) | 0.9755 | 0.9859 | 0.9885 |
| 4 | kt = 1-3(1-X)2/3+2(1-X) | 0.9844 | 0.9839 | 0.9855 |
| 5 | kt =[1-1-X13]² | 0.9914 | 0.976 | 0.9785 |
| 6 | kt=13ln1-X–[1-(1-X)-1/3] | 0.9767 | 0.9489 | 0.9614 |
| 7 | kt= 1-(1-X)1/2 | 0.01 | 0.07 | 0.05 |
| 8 | kt= 1-(1-X)1/3 | 0.8456 | 0.7649 | 0.9091 |
| 9 | kt= 1-(1-0.45X)1/3 | 0.5237 | 0.626 | 0.8659 |
| 10 | kt =-ln(1-X) | 0.9625 | 0.5584 | 0.08 |

Table S4 List of kinetic models calculated for (DES-2, Cobalt) at different temperatures and their correlation coefficients (R²), (0-48 hour)

| No | Kinetic Model equations | Correlation coefficients (R²) of kinetics models |  |  |
| --- | --- | --- | --- | --- |
|  |  | 100°C | 75°C | 50°C |
| 1 | kt = X | 0.7599 | 0.8984 | 0.983 |
| 2 | kt = X² | 0.9975 | 0.9894 | 0.8621 |
| 3 | kt= X+(1-X)ln(1-X) | 0.9825 | 0.9742 | 0.8533 |
| 4 | kt = 1-3(1-X)2/3+2(1-X) | 0.9679 | 0.967 | 0.8503 |
| 5 | kt =[1-1-X13]² | 0.9271 | 0.9513 | 0.8445 |
| 6 | kt=13ln1-X–[1-(1-X)-1/3] | 0.8491 | 0.9162 | 0.8335 |
| 7 | kt= 1-(1-X)1/2 | 0.8161 | 0.7046 | 0.8805 |
| 8 | kt= 1-(1-X)1/3 | 0.9774 | 0.9661 | 0.9767 |
| 9 | kt= 1-(1-0.45X)1/3 | 0.8444 | 0.9266 | 0.9808 |
| 10 | kt =-ln(1-X) | 0.9861 | 0.9837 | 0.9725 |

Table S5 List of kinetic models calculated for (DES-2, Molybdenum) at different temperatures and their correlation coefficients (R²), (0-48 hour)

| No | Kinetic Model equations | Correlation coefficients (R²) of kinetics models |  |  |
| --- | --- | --- | --- | --- |
|  |  | 100°C | 75°C | 50°C |
| 1 | kt = X | 0.7599 | 0.8984 | 0.983 |
| 2 | kt = X² | 0.9975 | 0.9894 | 0.8621 |
| 3 | kt= X+(1-X)ln(1-X) | 0.9916 | 0.9792 | 0.8555 |
| 4 | kt = 1-3(1-X)2/3+2(1-X) | 0.9869 | 0.9748 | 0.853 |
| 5 | kt =[1-1-X13]² | 0.9724 | 0.9652 | 0.8485 |
| 6 | kt=13ln1-X–[1-(1-X)-1/3] | 0.9395 | 0.9434 | 0.8398 |
| 7 | kt= 1-(1-X)1/2 | 0.971 | 0.8887 | 0.9647 |
| 8 | kt= 1-(1-X)1/3 | 0.9358 | 0.9512 | 0.9875 |
| 9 | kt= 1-(1-0.45X)1/3 | 0.9801 | 0.9893 | 0.9855 |
| 10 | kt =-ln(1-X) | 0.9701 | 0.9693 | 0.9755 |

Figures

Fig.S1 Plots of (a)Cobalt leaching efficiency at different temperatures for (DES-1), (b) kt = 1-3(1-X)2/3+2(1-X) , (c) kt= 1-(1-X)1/3 , and (d) kt =-ln1-X  vs time, (0-48 hours)

Fig.S2 Plots of (a) Molybdenum leaching efficiency at different temperatures for (DES-1), (b) kt = 1-3(1-X)2/3+2(1-X) , (c) kt= 1-(1-X)1/3 , and (d) kt =-ln1-X  vs time, (0-48 hours)

Fig.S3 Plots of (a)Cobalt leaching efficiency at different temperatures for (DES-2), (b) kt = 1-3(1-X)2/3+2(1-X) , (c) kt= 1-(1-X)1/3 , and (d) kt =-ln1-X  vs time, (0-48 hours)

Fig.S4 Plots of (a) Molybdenum leaching efficiency at different temperatures for (DES-2), (b) kt = 1-3(1-X)2/3+2(1-X) , (c) kt= 1-(1-X)1/3 , and (d) kt =-ln1-X  vs time, (0-48 hours)

References

Dickinson, C.F., Heal, G.R., 1999. Solid–liquid diffusion controlled rate equations. Thermochim. Acta 340–341, 89–103. https://doi.org/10.1016/S0040-6031(99)00256-7

Fogler, H.S., 2016. Elements of Chemical Reaction Engineering, 5 th. ed, Pearson. Pearson, Philadelphia.

Levenspiel, O., 1998. Chemical reaction engineering, 3rd editio. ed, Wiley. Wiley. https://doi.org/https://doi.org/10.1002/aic.690190143

Padilla, R., Pavez, P., Ruiz, M.C., 2008. Kinetics of copper dissolution from sulfidized chalcopyrite at high pressures in H2SO4–O2. Hydrometallurgy 91, 113–120. https://doi.org/10.1016/j.hydromet.2007.12.003

Sokić, M.D., Marković, B., Živković, D., 2009. Kinetics of chalcopyrite leaching by sodium nitrate in sulphuric acid. Hydrometallurgy 95, 273–279. https://doi.org/10.1016/j.hydromet.2008.06.012