“Kinetic Trapping of 2,4,6-Tris(4-pyridyl)benzene and ZnI2 into M12L8 poly-[n]-catenanes using unconventional self-assembling processes”

Javier Martí-Rujas*,†,⁋, Antonino Famulari†,#

† Dipartimento di Chimica Materiali e Ingegneria Chimica ‘‘Giulio Natta’’, Politecnico di Milano, Via L. Mancinelli 7, 20131 Milan, Italy.

⁋ Center for Nano Science and Technology@Polimi, Istituto Italiano di Tecnologia, Via Pascoli 70/3, 20133 Milano, Italy.

# INSTM Consorzio Interuniversitario Nazionale per la Scienza e Tecnologia dei Materiali

*E-mail: javier.marti@polimi.it; antonino.famulari@polimi.it

Contents

Materials and methods

Single crystal XRD of 1 and 2

Powder X-Ray Diffraction Experiments

TG experiments

Density Functional Theory Calculations

Slow crystallization experiments using TPB and ZnI2 in various aromatic solvents: nitrobenzene, toluene, chlorobenzene.

Instant synthesis using TPB and ZnI2 in various aromatic solvents: nitrobenzene, toluene, chlorobenzene.

Solid-state synthesis of amorphous poly-[n]-catenane (a2).

Amorphous-to-crystalline transformation by uptake of xylenes.

References

Materials and Methods.

Single crystal XRD of 1 and 2.

Single crystal X-ray data of poly-[n]-catenane 1 and 2 were recorded using a XtaLAB Synergy-S, Dualflex, HyPix-6000HE diffractometer.  Single block-shaped crystals of 1 and plate-like crystals of 2 were obtained in the same crystallization tube using the three-layering method as shown in Figure S1.  A suitable crystal of each sample 1 and 2 were selected and mounted on a suitable support on an XtaLAB Synergy-S, Dualflex, HyPix-6000HE diffractometer.  The crystal was kept at a steady T ≈ 300 K during data collection. The structure was solved with the ShelXT structure solution program using the Intrinsic Phasing solution method and by using Olex2 as the graphical interface.  The model was refined with version 2014/7 of ShelXL 2014/71 using Least Squares minimization.  The structures were solved and the space group R-3 for 1 and C2/c for 2 determined by the ShelXT1 structure solution program using Intrinsic Phasing and refined by Least Squares using version 2014/7 of ShelXL 2014/7.1 All non-hydrogen atoms were refined anisotropically. Hydrogen atom positions were calculated geometrically and refined using the riding model.

Crystal Data (1). C204H150I24N30O12Zn12, Mr = 7043.57, trigonal, R-3 (No. 148), a = 38.6805(7) Å, b = 38.6805(7) Å, c = 16.0202(3) Å,  = 90°, β = 90°, = 120°, V = 20757.9(8)  Å3, T = 303(2) K, Z = 3.  Table S1 contains further crystallographic information.

The reference CCDC code for 1 is 2233049.

Crystal Data (2). C54H40Cl2I6N6Zn3, Mr = 1801, monoclinic, C2/c (No. 15), a = 24.1055(4) Å, b = 14.4843(2) Å, c = 18.2201(2) Å,  = 90°, β = 100.8630(10)°, = 90°, V = 6247.57(15) Å3, T = 303(2) K, Z = 4. Table S2 contains further crystallographic information.

The reference CCDC code for 2 is 2233048.

Powder X-Ray diffraction experiments.

All the powder X-ray diffraction experiments were carried out using a Bruker D2-Phaser diffractometer equipped with Cu radiation (λ = 1.54184 Å) using Bragg-Brentano geometry.  The experiments were performed at room temperature.

TG experiments.

Thermogravimetrical analysis was carried out using a Perkin Elmer Thermal Analysis instrument at the Laboratorio Analisi Chimiche at the Dipartimento di Chimica, Materiali ed Ingegneria Chimica, Politecnico di Milano.  The analyzed microcrystalline samples were heated within the temperature range from 30 °C to 700 °C using a heating rate of 10 °C/min under N2.

Density Functional Theory

Molecular modelling studies are performed in the gas phase. The calculations rely on the gradient corrected GGA PBE functional.  A numerical double zeta numerical basis set centered on atoms (including polarisation functions on all atoms), roughly comparable with the usual 6-31G** gaussian basis, has been employed. Explicit van der Waals corrections were also used to improve the description of van der Waals intra-particle interactions.  The DMol3 package was employed for all the calculations.

The geometries of the molecules have been extracted from experimental single crystal X-ray determined structures and optimised. Electrostatic Potentials have been plotted by employing the above mentioned DFT electron density.

Slow crystallization experiments using TPB and ZnI2 in various aromatic solvents: nitrobenzene, toluene, chlorobenzene.

Crystallization using nitrobenzene: In a typical layer difussion experiment 7.5 mg of TPB were disolved in a mixture of nitrobenzene/methanol (3:2 ml) forming the bottom layer in the crystallization tube. Then 3 ml of methanol as a middle layer was added. The last layer, the methanolic solution of ZnI2 (11.5 mg ZnI2 / 1 ml methanol), was added on top dropwise.  The crystallization tube was left to stand for 5 days in the lab.

Figure S1. (a) Simulated powder XRD pattern of TPB-ZnI2 synthesized using slow crystallization (layering) method with nitrobenzene as templating solvent.  The data was recorded at room temperature. The structure is the poly-[n]-catenane 1. (b) Simulated powder XRD pattern of the TPB-ZnBr2 M12L8 poly-[n]-catenane including para-chlorotoluene as guest whose SC-XRD structure was measured at 100K and is published in Ref. 7.

Crystallization using chlorobenzene: In a typical layer difussion experiment 7.5 mg of TPB were disolved in a mixture of chlorobenzene/methanol (3:2 ml) forming the bottom layer in the crystallization tube. Then 3 ml of methanol as a middle layer was added. The last layer, the methanolic solution of ZnI2, was added on top dropwise.  The crystallization tube was left to stand for 5 days in the lab.

Figure S2. Simulated powder XRD pattern of TPB-ZnI2 synthesized using slow crystallization (layering) method using chlorobenzene as templating agent.  The data was recorded at room temperature.

Figure S3. Picture showing the 1D channels viewed along the three crystallographic directions of 2. The void space corresponds to 30 % of the total unit cell volume.

Crystallization using toluene: In a typical layer difussion experiment 7.5 mg of TPB were disolved in a mixture of toluene/methanol (7:3 ml) forming the bottom layer in the crystallization tube. Then 3 ml of methanol as a middle layer was added. The last layer, the methanolic solution of ZnI2, was added on top dropwise.  The crystallization tube was left to stand for 5 days in the lab.

Figure S4. Cartoon showing the slow crystallization carried out by triple layering with a bottom TPB solution including the templating solvent chlorobenzene, the middle layer of MeOH separating the metal that is added as a top layer.  All the three layers are deposited dropwise to avoid rapid mixing of the self-assembling components.  The same methodology was used using nitrobenzene and o-dichlorobenzene.

Instant synthesis using TPB and ZnI2 in various aromatic solvents: nitrobenzene, toluene, chlorobenzene.

Instant precipitation of the M12L8 poly-[n]-catenane was carried out using the following aromatic solvents: nitrobenzene, toluene and chlorobenzene.

Fast crystallization using nitrobenzene as aromatic solvent: The fast crystallization using nitrobenzene as aromatic solvent was carried out by dissolving TPB (30 mg) in a mixture nitrobenzene/methanol (6/3 mL) which was kept stirring vigorously at room temperature.  Then the ZnI2 (48 mg) dissolved in methanol was added to the stirring TPB solution. Immediately a yellowish precipitate was formed.

Figure S5. (a) Vial containing the “sticky” product after filtration the suspension generated upon instant synthesis. (b) Actual view of the sample mounted and measured by powder XRD.

Figure S6. 1H NMR of the sample a1 obtained by instant synthesis after being immersed in toluene/methanol. The 1H NMR plot shows that no nitrobenzene nor methanol are present but toluene.

Fast crystallization using toluene as aromatic solvent: The fast crystallization using toluene as aromatic solvent was carried out by dissolving TPB (30 mg) in a mixture toluene/methanol (24/10 mL) which was kept stirring vigorously at room temperature.  Then the ZnI2 (48 mg) dissolved in methanol was added to the stirring TPB solution. Immediately a precipitate was formed. Upon filtration the solid obtained was 20 mg.  The powder XRD pattern was measured right after the synthesis (Figure S11a) and one month later (Figure S11b).  Clearly, the sample is not able to maintain its crystallinity.

Figure S7. (a) Experimental powder XRD pattern of the solid product obtained from the instant synthesis of TPB and ZnI2 using toluene as templating aromatic solvent measured after the synthesis (i.e., within 1 h after filtration). (b) The same sample measured after one month kept in the vial.

Figure S8.  TG corresponding to the sample obtained upon instant synthesis using toluene as templating agent which was left stored in the vial for one month.  The reaction was carried out at room temperature.

Fast crystallization using chlorobenzene as aromatic solvent: The fast crystallization using chlorobenzene as aromatic solvent was carried out by dissolving TPB (30 mg) in a mixture chlorobenzene/methanol (10/7 mL) which was kept stirring vigorously at room temperature.  Then the ZnI2 (48 mg) dissolved in methanol was added to the stirring TPB solution. Immediately a yellowish precipitate was formed. Upon filtration the solid obtained was 52 mg.  (a) The powder XRD diffraction pattern measured after the synthesis and filtration of the solid shows the crystalline poly-[n]-catenane (Figure S13a).  The same sample measured after one month in the closed vial shows that the material retains its crystallinity (Figure S13b).

Figure S9. (a) Experimental powder XRD pattern of the solid product obtained from the instant synthesis of TPB and ZnI2 using chlorobenzene as templating aromatic solvent measured after the synthesis (i.e., within 1 h after filtration).  (b) The same sample measured after one month kept in the vial at room temperature.

Figure S10.  TG corresponding to the sample obtained upon instant synthesis using chlorobenzene as templating agent measured after one month of its synthesis.  The sample used is the same used to do the powder XRD shown in Figure S13b.

Solid-state synthesis of amorphous poly-[n]-catenane (a2).

Figure S11. Images of the mortar taken during the neat grinding experiment. The actual product after removing it from the mortar and transferred to a vial was 74 mg.

Figure S12. Experimental powder XRD pattern of the amorphous phase (a2) obtained upon neat grinding TPB and ZnI2.

Figure S13. (a) Simulated powder XRD pattern of 1 at room temperature. (b) Experimental powder XRD pattern obtained after immersing the amorphous phase a2 obtained upon neat grinding in toluene/methanol overnight measured at room temperature.1

Amorphous-to-crystalline transformation by uptake of xylenes.

Uptake of o-xylene by a2 in a solid-liquid heterogeneous reaction.  In a round bottom flask containing 4ml of o-xylene and 1ml of methanol were introduced 30 mg of a2 obtained via neat grinding. The suspension was left stirring overnight.  Then the solid was filtered and mounted for powder XRD analysis.  The obtained diffractogram shown in Figure S15 demonstrates that the sample is crystalline.

Figure S14.  Powder XRD pattern obtained after immersing the amorphous phase a2 in o-xylene/methanol measured at room temperature.

Uptake of m-xylene by a2 in a solid-liquid heterogeneous reaction.  In a round bottom flask containing 4ml of m-xylene and 1ml of methanol were introduced 30 mg of a2 obtained via neat grinding.  The suspension was left stirring overnight.  Then the solid was filtered and subjected to powder XRD analysis (Figure S14).  The obtained diffractogram demonstrates that the sample is crystalline and the structural transformation can be considered as an amorphous-to-crystalline process.

Figure S15.  Powder XRD pattern obtained after immersing the amorphous phase a2 in m-xylene/methanol measured at room temperature.

Uptake of p-xylene by a2 in a solid-liquid heterogeneous reaction.  In a round bottom flask containing 4ml of p-xylene and 1ml of methanol were introduced 30 mg of amorphous phase a2 obtained via neat grinding.  The suspension was left stirring overnight.  Then the solid was filtered and subected to powder XRD analysis.  The obtained diffractogram demonstrates that the sample is crystalline and it is very similar to the diffractogram obtained after exposing a2 to m-xylene and o-xylene.

Figure S16.  Powder XRD pattern obtained after immersing the amorphous phase a2 in p-xylene/methanol measured at room temperature.

Figure S17.  (a) Simulated powder XRD pattern of 1 from single crystal XRD data at room temperature. (b) Experimental powder XRD data obtained after immersing the amorphous phase a2 in para-xylene also recorded at room temperature.

Solid-state synthesis of amorphous M12L8 poly-[n]-catenane using TPB and ZnCl2.

Here we also report the solid-state synthesis of the M12L8 poly-[n]-catenane in the amorphous state upon grinding TPB and ZnCl2.  The powder XRD pattern has the profile typical of the amorphous poly-[n]-catenanes of M12L8 interlocked cages with two broad bumps as in the bromide and iodide amorphous solids.  The formation of the poly-[n]-catenane is corroborated by the guest uptake (1,2-dichlorobenzene) which induces the transformation from amorphous to crystalline via an amorphous-to-crystalline transformation.  The powder XRD pattern after guest uptake matches with those of the TPB-ZnCl2 poly-[n]-catenane including similar aromatic molecules. See ESI for further information.

Figure S18.  Powder XRD pattern obtained after grinding TPB and ZnCl2. The product clearly shows that is amorphous.

Figure S19.  Powder XRD pattern obtained after immersing in o-DCB/methanol the amorphous phase obtained from grinding TPB and ZnCl2. The product clearly shows that became crystalline after following an amorphous-to-crystalline transformation.

Table S1.  Crystal data and structure refinement for the poly-[n]-catenane 1.

Identification code 	1

Empirical formula 	C204 H150 I24 N30 O12 Zn12

Formula weight 	7043.57

Temperature 	303(2) K

Wavelength 	1.54184 Å

Crystal system 	Trigonal

Space group 	R -3 :H

Unit cell dimensions	a = 38.6805(7) Å	a = 90°.

b = 38.6805(7) Å	b = 90°.

c = 16.0202(3) Å	g = 120°.

Volume	20757.9(8) Å3

Z	3

Density (calculated)	1.690 Mg/m3

Absorption coefficient	22.539 mm-1

F(000)	9936

Crystal size	0.100 x 0.080 x 0.050 mm3

Theta range for data collection	3.058 to 76.440°.

Index ranges	-42<=h<=36, -46<=k<=48, -19<=l<=16

Reflections collected	42589

Independent reflections	9032 [R(int) = 0.0780]

Completeness to theta = 67.684°	99.6 %

Absorption correction	"cylinder"

Max. and min. transmission	0.1295 and 0.0323

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9032 / 92 / 386

Goodness-of-fit on F2	1.052

Final R indices [I>2sigma(I)]	R1 = 0.0753, wR2 = 0.2362

R indices (all data)	R1 = 0.0887, wR2 = 0.2561

Extinction coefficient	n/a

Largest diff. peak and hole	2.457 and -0.990 e.Å-3

Table S2.  Crystal data and structure refinement for the coordination polymer 2.

Identification code 	2

Empirical formula 	C54 H40 Cl2 I6 N6 Zn3

Formula weight 	1801.33

Temperature 	304(2) K

Wavelength 	1.54184 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 24.1055(4) Å	a = 90°.

b = 14.4843(2) Å	b = 100.8630(10)°.

c = 18.2201(2) Å	g = 90°.

Volume	6247.57(15) Å3

Z	4

Density (calculated)	1.915 Mg/m3

Absorption coefficient	25.704 mm-1

F(000)	3392

Crystal size	0.100 x 0.070 x 0.060 mm3

Theta range for data collection	3.577 to 76.599°.

Index ranges	-30<=h<=30, -17<=k<=17, -22<=l<=14

Reflections collected	29701

Independent reflections	6171 [R(int) = 0.0526]

Completeness to theta = 67.684°	99.4 %

Absorption correction	"multi-scan"

Max. and min. transmission	1.0 and 0.19306

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6171 / 13 / 286

Goodness-of-fit on F2	1.105

Final R indices [I>2sigma(I)]	R1 = 0.0797, wR2 = 0.2443

R indices (all data)	R1 = 0.0900, wR2 = 0.2560

Extinction coefficient	n/a

Largest diff. peak and hole	1.908 and -1.688 e.Å-3

References

Sheldrick, G. M., Crystal structure refinement with SHELXL. Acta Cryst., 2015, C71, 3–8.

Dolomanov, O. V.; Bourhis, L. J.; Gildea, R. J.; Howard, J. A. K.; Puschmann, H. Olex2: A complete structure solution, refinement and analysis program. J. Appl. Cryst., 2009, 42, 339-341.

a) Perdew, J. P.; Burke, K. Ernzerhof, M. E. Generalized Gradient Approximation Made Simple. Phys. Rev. Lett., 1996, 77, 3865–3868; b) Perdew, J. P.; Burke, K.; Ernzerhof, M. E. Generalized Gradient Approximation Made Simple. Phys. Rev. Lett., 1997, 78, 1396–1396.

Grimme, S. Semiempirical hybrid density functional with perturbative second-order correlation. J. Chem. Phys., 2006, 124, 34108.

a) Baggioli, A.; Meille, S. V.; Raos, G.; Po, R.; Brinkmann, M. Famulari, A. Intramolecular CH/π interactions in alkylaromatics: Monomer conformations for poly(3-alkylthiophene) atomistic models. Int. J. Quantum Chem., 2013, 113, 2154; b) Baggioli, A.; Famulari, A. On the inter-ring torsion potential of regioregular P3HT: a first principles reexamination with explicit side chains. Phys. Chem. Chem. Phys., 2014, 16, 3983.

Delley, B. From molecules to solids with the DMol3 approach. J. Chem. Phys., 2000, 113, 7756.

Martí-Rujas, J.; Ma, S.; Famulari, A. Experimental X-ray and DFT structural analyses of M12L8 poly-[n]-catenanes using exotridentate ligands. Inorg. Chem., 2022, 61, 10863-10871.