Supplementary Materials

Chiral Dirac fermion in a collinear antiferromagnet

Ao Zhang1†, Ke Deng1†, Jieming Sheng1,2†, Pengfei Liu1†, Shiv Kumar3, Kenya Shimada3, Zhicheng Jiang4, Zhengtai Liu4, Dawei Shen4, Jiayu Li1, Jun Ren1, Le Wang1, Liang Zhou1, Yoshihisa Ishikawa5, Qiang Zhang6, Garry McIntyre7, Dehong Yu7, Enke Liu8, Liusuo Wu1*, Chaoyu Chen1* and Qihang Liu1*

1Shenzhen Institute for Quantum Science and Technology and Department of Physics, Southern University of Science and Technology, Shenzhen, 518055, China

2Academy for Advanced Interdisciplinary Studies, Southern University of Science and Technology, Shenzhen, 518055, China

3Hiroshima Synchrotron Radiation Centre, Hiroshima University, Higashi-Hiroshima, Hiroshima 739-0046, Japan.

4State Key Laboratory of Functional Materials for Informatics and Center for Excellence in Superconducting Electronics, Shanghai Institute of Microsystem and Information Technology, Chinese Academy of Sciences, Shanghai 200050, China.

5Neutron Science and Technology Center, Comprehensive Research Organization for Science and Society, Tokai, Ibaraki 319-1106, Japan

6Neutron Science Division, Oak Ridge National Laboratory, Oak Ridge, Tennessee 37831, USA

7Australian Nuclear Science and Technology Organisation, Locked bag 2001, Kirrawee DC, New South Wales 2232, Australia

8State Key Laboratory for Magnetism, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, China

†These authors contributed equally to this work.

*Correspondence should be addressed to L.W. (wuls@sustech.edu.cn), C.C. (chency@sustech.edu.cn) and Q.L. (liuqh@sustech.edu.cn)

Contents

S1. Dirac-like field with chirality	3

S2. Single crystal X-ray diffraction refinement	6

S3. Magnetic structure analysis	7

S4. Magnetization measurements	10

S5. Symmetry analysis of CoNb3S6	11

S5.1. Doubly degenerate bands of CoNb3S6	11

S5.2. Chern number and robust Fermi-arc surface states	13

S5.3. The electronic structure and fermi surface of nonmagnetic CoNb3S6	14

S6. Momentum distribution curves of β at EF	14

S7. ARPES spectra taken with different polarization light	15

S8. Anomalous hall conductivity tensors of bulk and slab CoNb3S6	15

S9. Electric transport measurements	17

Supplementary references	19

S1. Dirac-like field with chirality

First, we briefly review the Dirac field. Its field operators furnish a 4D irreducible representation of the Lorentz group. After that, we considered the symmetry condition supporting the flavor Weyl field. The Lorentz group is the group of Minkowski space-time symmetries obeying the principle of relativity. Such a group can be written as a combination of two disconnected pieces—O3,1=SO3,1+P SO3,1, where SO3,1 is a connected subgroup of O3,1. Any irreps of SO3,1 can be labeled by the irreps of two su(2) algebras, denoted as j+,j-, with j±=0, 1/2, 1, 3/2,…, because the Lie algebra of SO3,1 consists of six generators forming two individual su(2) algebras commuting with each other. Weyl fields—the simplest fields for spin-½ fermions—furnish the irrep (0,1/2) or (1/2,0) for right or left-handedness, satisfying two-component massless Weyl equations when P is broken. The reducible representation of SO3,1, i.e., (0,1/2)⨁(1/2,0), in the presence of P, becomes irreducible for the Lorentz group O(3,1), giving rise to the Dirac fields.

The Dirac fields obey the famous Dirac equation, (-iαi∂i+mβ)ψ(x)=i∂0ψ(x), where αi=τx⨂σi and β=τz⨂σ0. It explains several new phases and phenomena such as antimatter, SOC, and Zeeman effect. However, seldom considered is the possibility of elementary spin-1/2 particles described by four-component fields having 1/2,01/2,0 (or equivalently, 0,1/20,1/2). To achieve such fields, P should be broken, reducing the corresponding symmetry group to SO3,1. Therefore, 1/2,01/2,0 would become a reducible representation, corresponding to a field that naturally decomposes into two Weyl fields. Second, additional internal symmetries need to be assumed to elevate the symmetry hierarchy of the system, rendering 1/2,01/2,0 representation irreducible. Internal symmetry operations are required to decouple the space-time operations according to the Coleman–Mandula theorem1. Furthermore, we selected them to form an SU(2) group connecting two Weyl fields with the same chirality, analogous to the SU(2) flavor symmetry in high-energy physics. Specifically, it is analogous to the isospin symmetry proposed by Heisenberg, pairing a proton and a neutron forming an SU2 doublet2.

Such isospin symmetry can stabilize free and causal quantum fields that follow the representation 1/2,01/2,0 (and 0,1/20,1/2). The corresponding fields are called flavor Weyl fields, described by the following massless Dirac-like equation:

iαi∂iψ(x)=±i∂0ψ(x),                            (1)

where ψ(x) denotes a four-component free field operator and αi=τi⨂σ0. Furthermore, the energy spectrum of equation (1) is doubly degenerate owing to the protection of the additional SU2 group, resembling the role of P in the Dirac equation.

To construct such flavor Weyl field, we firstly assume that inversion symmetry is broken such that left-handed Weyl field and right-handed Weyl field could exist individually. Then, we further assume a four component Dirac field can be written as the form ψ=ψL1ψL2 where ψL1 and ψL2 are two left-handed and 2-component Weyl fields following the irreducible representation (1/2,0) of the proper orthochronous Lorentz transformation. Then the representation matrices of the angular momentum operators and boost operators of proper orthochronous Lorentz transformation are J=12τ0⊗σ, K=-i2τ0⊗σ, where τi and σj (i=0,x,y,z) are Pauli matrices.

Such field is reducible under proper orthochronous Lorentz transformation, to stabilize this field, we further assumes that there is an internal SU(2) symmetry group with generators represented as I=12τ⊗σ0, which implies that the elements of SU(2) group transform on ψ=ψL1ψL2 by exp(-iθ⋅12τ)ψL1ψL2, identical to the transformation properties of SU(2) isospin symmetry on two quantum fields in standard model. Then, it is obvious that such field describe one particle formed by two Weyl fields connected by the internal SU(2) symmetry group.

From quantum field theory, the field operator can be written as the following form

ψlx=κψl+x+μψlc-x,	 	                 (2)

ψl+x=s1, s2∫d3p(2π)3/2 ulp, s1, s2 ap,  s1, s2 eipx,	       (3)

ψlc-x=s1, s2∫d3p(2π)3/2 vlp, s1, s2 ac†p, s1, s2e-ipx,        (4)

where l labels the 4 components of the field operator, ap,  s1, s2 and ac†p, s1, s2 are the annihilation operator of a spin-1/2 particle and creation operator of the antiparticle, with eigenvalue of momentum operator to be  p , helicity s1 (s1=±1/2) and eigenvalue of third component of the internal SU2 symmetry Iz to be s2 (s2=±1/2).  ulp, s1, s2 and vlp, s1, s2 are components of 4×1 column vectors, that are complex functions of p, s1 and  s2.

Then, by assuming the operation of internal SU2 symmetry group on ap,  s1, s2 to be s2exp(-iθ⋅12σ)s2 s2ap,  s1, s2 and follow the process of constructing field operator provided in Ref. 3, we can see that ψ can be constructed for describing massless spin-1/2 particles following the causal relation ψlx,ψl†y∓=0 for x-y space like. It could also be shown that this field obeys the following equation

-∂0+αi∂iψx=0,                            (5)

where αi=σ0⨂σi. This 4-component field have 4 independent variables, however, when we do not assume internal SU2 symmetry group, the field operator will reduce to operators with two independent variables, which is actually the Weyl field. Thus, this SU2 symmetry group helps to stabilize the flavor Weyl field.

S2. Single crystal X-ray diffraction refinement

Single crystals of CoNb3S6 were grown using chemical vapor transport method. The crystal structure of CoNb3S6 was characterized using a Bruker D8 Quest diffractometer with Mo-K𝛼 radiation (𝜆 = 0.71069 Å). The data integration and reduction were performed with the commercial Bruker APEX2 software suite. The refined lattice parameters and the atomic occupations are presented in Tables S1 and S2. It is worthy to note that the ratio of the refined atomic occupations for Co:Nb:S is about to 0.995:2.975:6, nearly equal to the nominal stoichiometric composition 1:3:6, indicating the single crystal is high quality.

S3. Magnetic structure analysis

Fig. S1. Powder neutron diffraction pattern of CoNb3S6 with Rietveld refinement fit at 100 K.

Fig. S2. The in-plane spin configurations for three equivalent magnetic propagation vectors a, qm1= (0.5,0,0), b, qm2= (0,0.5,0) and c, qm3= (0.5,-0.5,0). e and f are the schematics of the triple-q magnetic order with a vector sum of three magnetic domains “1+2+3” and “1+2-3”, respectively. The bule circles have no moments. A total of four domains could be expected for the triple-q magnetic order with different combination of the“1,2,3” three magnetic structures.

By our single crystal neutron diffraction measurements, three magnetic domains with different magnetic propagation vectors (0.5, 0, 0), (0, 0.5, 0) and (0.5, -0.5, 0) were identified. However, due to the limited magnetic reflections of the single crystal neutron diffraction experiment, an additional powder neutron diffraction experiment was performed to determine the magnetic structure of CoNb3S6.  Fig. S1 and Fig. 1(c) of the main text present the powder neutron diffraction patterns measured at 100 K and 10 K, respectively. Consistent with our single crystal X-ray diffraction results, the Rietveld refinement of the neutron diffraction data at 100 K confirms the Hexagonal structure of CoNb3S6 with space group P6322. For T = 10 K, a new set of reflections emerge around the low-Q region of the diffraction pattern, and can be indexed by (0.5, 0, 0), (0, 0.5, 0) or (0.5, -0.5, 0) magnetic propagation vectors, indicating the magnetic origin. Here, we chose qm = (0.5, 0, 0) as the magnetic propagation vector. The magnetic structure of CoNb3S6 was analyzed by representation theory. For space group P6322 (No.182) with Co site at (1/3, 2/3, 1/4), the spin configuration can be described by four different irreducible representations (IRs). Table S3 lists the basis vectors for IRs Γ1, Γ2, Γ3 and Γ4, respectively. For Γ1 and Γ4, the moments are constrained in the ab plane. The spin arrangement between Co1 and Co2 is ferromagnetic for Γ1 and antiferromagnetic for Γ4. For Γ2 and Γ3, the moments are allowed to lie in the bc plane.  The spin components align ferromagnetically along the b axis and antiferromagnetically along the c axis between Co1 and Co2 for Γ2, while Γ3 shows the opposite arrangement. By Rietveld refinement, we found that Γ4 could give the best fit with Rp = 2.88 and Rwp = 3.68 for powder neutron diffraction data at 10 K, as shown in Fig. 1(c) of the main text.

Due to the in-plane C3 symmetry, besides the possibility of three equivalent magnetic domains,  the compound could also have a triple-q magnetic order. However, diffraction from three magnetic domains with equal populations would in principle be indistinguishable from a triple-q magnetic order. As shown in Fig.S2 a-c are the schematics of the magnetic structures for three different magnetic domains. A triple-q magnetic order can be understood as a vector sum of the above three magnetic domains (Fig.S2 e and f).

S4. Magnetization measurements

Fig. S3. Temperature dependence of the magnetization measured at H=0.1 T with field along the a and c axis. The bule and red lines represent the field cooled (FC) and zero field cooled (ZFC) measurements, respectively.

Fig. S3 shows the temperature evolution of the magnetization M(T) measured at H=0.1 T with field along the a and c axis. For H//a, the zero-field cooled (ZFC) and field cooled (FC) measurements show identical behaviors. Both the M(T) curves exhibit a broad peak around T=30 K and a sharp decrease at T=28.3 K, suggesting antiferromagnetic (AFM) phase transition in CoNb3S6. For H//c, M(T) curves show an irreversible behavior between the FC and ZFC measurements below TN. The ZFC magnetization initially increases on cooling and reaches the maximum at 28.5 K, followed by an abruptly decrease around TN=28.3 K. Further lowering the temperature, it shows an additional upturn feature below 26.1 K. As a comparison, the FC magnetization shows an abruptly increase around TN, reaches a maximum at 27.6 K and decreases on further cooling. These irreversible behaviors observed in M(T) indicate the presence of ferromagnetic component along the c axis.

Fig. S4. Field dependence of the magnetization measured from 22 K to 29 K with field along the c axis.

The isothermal magnetization M (H) curves, measured from 22 K to 29 K with H//c, are shown in the Fig. S4. For T=29 K>TN, nearly linear M (H) curves were observed between 7 T and -7 T, while, for T<TN, a small ferromagnetic hsyteresis loop gradually began to emerge, implying the ferromagnetic component was accompanied by the AFM phase transition. As lowering the temperature, the hysteresis loop gradually becomes larger due to the increase of the ferromagnetic coercive field. When the temperature is below 24 K, the coercive field becomes larger than 7 T, beyond the limit of our experimental MPMS magnet, which results in the incomplete hysteresis loops, as shown in Fig. S4 b.

S5. Symmetry analysis of CoNb3S6

S5.1. Doubly degenerate bands of CoNb3S6

CoNb3S6 belongs to space group P6322 (No. 182). It is a collinear antiferromagnet with magnetic moments oriented along a crystal axis within the a-b plane. This magnetic structure corresponds to the magnetic space group PB21212 (No. 18.22) and the spin space group PB 121 121 12  ∞m1. According to previous work4, the elements of this spin space group are listed in Table S4. From Table S4, we can prove that the element {Uz(π)||E|τ(a+b)/2} is included in the spin space group without SOC. In addition, the {Uz(π)||E|τ(a+b)/2} preserve double degeneracy in the whole Brillouin zone.

In fact,{Uz(π)||E|τ(a+b)/2}is an symmetry keeping the Hamiltonian invariant,  {Uz(π)||E|τ(a+b)/2}ε(s,k)=ε(s,k). At the same time, we apply this element on the spin and momentum-dependent energy band ε(s,k). Since all spins point along x direction in CoNb3S6 (Fig 1d), Uz(π) will reverse the good quantum number of spin, {Uz(π)||E|τ(a+b)/2}ε(s,k)=ε(-s,k). Hence ε(s,k)=ε(-s,k). The band structure is at least double-degenerate everywhere in the whole Brillouin zone.

Table S4. Group elements of the magnetic space group and spin group describing CoNb3S6.

|  | Spin space group | Group elements |
| --- | --- | --- |
| w/ SOC | PB 221 221 22 | H: {E¦¦E¦0}, {Ux(π)¦¦Cx(π)¦0}, {Uy(π)¦¦Cy(π)¦τ(b+c)/2}, {Uz(π)¦¦Cz(π)¦τ(b+c)/2} M: {T¦Eτ(a+b)/2},{TUx(π)¦¦Cx(π)¦τ(a+b)/2}, {TUy(π)¦¦Cy(π)¦τ(a+c)/2}, {TUz(π)¦¦Cz(π)¦τ(a+c)/2} |
| w/o SOC | Nontrivial: PB 121 121 12 | H: {E¦¦E¦0}, {E¦¦Cx(π)¦0}, {E¦¦Cy(π)¦τ(a+c)/2}, {E¦¦Cz(π)¦τ(a+c)/2} M: {T¦Eτ(a+b)/2},{T¦Cx(π)τ(a+b)/2}, {T¦¦Cy(π)¦τ(b+c)/2}, {T¦¦Cz(π)¦τ(b+c)/2} |
|  | Trivial: ∞m1 | {TUn(π)¦¦E¦¦0} (n=cosφy+sinφz, φ∈(0,π]) {Ux(θ)¦¦E¦¦0} (θ∈(0,2π]) |

τ(a+b)/2=(1/2,1/2,0), τ(b+c)/2=(0,1/2,1/2),τ(a+c)/2=(1/2,0,1/2);

H/M: elements without/with time-reversal symmetry.

S5.2. Chern number and robust Fermi-arc surface states

Fig. S5. The Fermi-arc surface states and Chern number of CoNb3S6. a, The Fermi-arc surface states of CoNb3S6 contain both bulk and surface contribution.  b, Fermi-arc surface states of CoNb3S6 with only surface contribution. c, The 40-layer slab bands calculation with projection on Co-3d (yellow), Nb-4d (green) and S-3p (red) orbitals in the first unit cell of NbS2 surface. Fermi-arc surface states are denoted by black arrows. d, e The Wannier charge centers (WCCs) of the flavor Weyl points (N1 and P1) and their Chern numbers. N1(0.40793, 0.00008, 0.00002), P1(0.00001, 0.26514, 0.00003).

S5.3. The electronic structure and fermi surface of nonmagnetic CoNb3S6

Fig. S6. The electronic structure and Fermi surface of nonmagnetic CoNb3S6. a and b ARPES spectra taken with 123 eV photons along the K-Γ-K and M-Γ-M, respectively. The DFT calculation of nonmagnetic CoNb3S6 along the above two k-paths with SOC are overlaid on top of ARPES Data. The red arrows indicate the main mismatch between APRES measurement and DFT calculation. c and d denote the ARPES Fermi surface mapping and DFT calculated Fermi surfaces with only surface state spectral weight for nonmagnetic CoNb3S6, respectively.

S6. Momentum distribution curves of β at EF

Fig. S7. The ARPES spectra and momentum distribution curves (MDCs) at EF of β. a, ARPES spectra cuts of β at different kz value along K-Γ-K direction, black dashed lines denote K points. b, Corresponding MDCs at EF for β in a (solid lines), appended with two Lorentzian peak fitting (dashed lines). c, Fitted peak positions for β at EF (kF), with the error bars defined by FWHM of the fitted curves.

S7. ARPES spectra taken with different polarization light

Fig. S8. ARPES spectra taken with different polarized light. a, b ARPES cuts along  K-Γ-K direction taken with 80 eV LH (p) and LV (s) polarized light respectively. c, d ARPES cuts along  M-Γ-M direction taken with 80 eV p and s polarized light respectively.

S8. Anomalous hall conductivity tensors of bulk and slab CoNb3S6

According to symmetry analysis, the magnetic space group of bulk CoNb3S6 without/with canting are PB21212 (No. 18.22) and P2121'2' (No. 18.19), respectively. And the magnetic space group of slab CoNb3S6 without/with canting are PS1 (No. 1.3) and P1 (No. 1.1), respectively. The group elements of these magnetic space groups are listed in table S5. Bulk and slab CoNb3S6 without canting are preserved the Tτ12120. In addition, the main differences between the slab and bulk CoNb3S6 are all rotation symmetry is broken for slab.

Table S5. Group elements of the magnetic space group describing bulk and slab CoNb3S6 without/with canting.

|  | Bulk |  | Slab |  |
| --- | --- | --- | --- | --- |
|  | w/o canting | w/ canting | w/o canting | w/ canting |
| Magnetic space group | PB21212 | P2121'2' | PS1 | P1 |
| w/ SOC | E TC2zτ0012 TC2yτ0012 C2x Tτ12120 C2zτ121212 C2yτ121212 TC2xτ12120 | E TC2yτ0012 C2zτ121212 TC2xτ12120 | E Tτ12120 | E |

For bulk CoNb3S6 without canting magnetic moment, the magnetic space group is PB21212 (No. 18.22). Its form of anomalous hall conductivity tensor is σij=σxx000σyy000σzz. Thus the σxy=0 for bulk CoNb3S6 w/o canting. However, when a small canting along the z direction, the magnetic space group becomes P2121'2' (No. 18.19) and the corresponding form of anomalous hall conductivity tensor σij=σxxσxy0-σxyσyy000σzz, thus σxy≠0.

For slab CoNb3S6 w/o canting magnetic moment, the magnetic space group is PS1 (No. 1.3). Its form of anomalous hall conductivity tensor is σij=σxxσxyσxzσxyσyyσyzσxzσyzσzz. The σxy=σyx according to the form of anomalous hall conductivity tensor. At the same time, σxy is an antisymmetric tensor, which lead to σxy=-σyx. Thus, σxy=0 for slab CoNb3S6 w/o canting. However, when a small canting along the z direction, the magnetic space group becomes P1 (No. 1.1) and the corresponding form of anomalous hall conductivity tensor σij=σxxσxyσxzσyxσyyσyzσzxσzyσzz, thus σxy≠0 for slab CoNb3S6 with canting.

S9. Electric transport measurements

Fig. S9. Temperature dependence of the electrical resistivity with current along the a aixs for CoNb3S6.

The zero-field electrical resistivity as a function of temperature measured with current along the a axis is presented in Fig. S9. The anomaly around 28.7 K in ρxx(T) curve further confirmed the antiferromagnetic transition observed in the magnetization measurements.

Fig. S10. a, Field evolution of the Hall resistivity measured at different temperatures. b, Field evolution of the anomalous Hall resistivity obtained by subtracting the ordinary Hall resistivity. c, Field evolution of the anomalous Hall conductivity. d, Field evolution of the longitudinal resistivity measured at different temperatures.

Fig. S10 a illustrates the field dependent Hall resistivity measured between 29 K and 22 K with current along the a axis and field along the c axis. By subtracting the linear background, large anomalous Hall resistivity can be obtained for T< TN, as shown in Fig. S10 b. The corresponding anomalous Hall conductivity σxyA=ρxyA/(ρxyA2+ρxx2) at different temperatures are presented in Fig. S10 c. As shown in Fig. S10 d is the field evolution of the longitudinal resistivity ρxx measured at different temperatures. Only a small magnetoresistance (MR ~5%) is observed below TN. The small jumps observed in the MR curves correspond to the flips of ferromagnetic components.

Fig. S11. Temperature dependence of a the ordinary Hall coefficient and b carrier concentration.

Fig. S11 a are the ordinary Hall coefficients extracted from the linear fits of the isothermal field dependent Hall effect at different temperatures. If a single band model was assumed, the carrier concentration of the holes can be estimated by n = 1/|eR0| , and presented in Fig. S11 b. The temperature evolution of the carrier concentration shows a concave-like feature with the minimum around 1.4×1021 cm-3 between 23 K and 28 K.

Supplementary reference

1	Coleman, S. & Mandula, J. All Possible Symmetries of the S Matrix. Phys. Rev. 159, 1251-1256 (1967).

2	Heisenberg, W. Über den Bau der Atomkerne. I. Zeitschrift für Physik 77, 1-11 (1932).

3	Weinberg, S. The quantum theory of fields. Vol. 2 (Cambridge university press, 1995).

4	Liu, P., Zhang, A., Han, J. & Liu, Q. Chiral Dirac-like fermion in spin-orbit-free antiferromagnetic semimetals. The Innovation 3, 100343 (2022).