Interfacial Disordering and Heterojunction Enabling Fast Proton Conduction

Muhammad Yousaf1, #, Yuzheng Lu2, #, Enyi Hu1, Muhammad Akbar3, M.A.K Yousaf Shah1, Naveed Mushtaq1, Senlin Yan2, Chen Xia3,4**, Bin Zhu1,5*

1Energy Storage Joint Research Center, School of Energy and Environment, Southeast University, No.2 Si Pai Lou, Nanjing 210096, China

2School of Electronic Engineering, Nanjing Xiaozhuang University, Nanjing 211171, P.R. China

3School of Microelectronics and Faculty of Physics and Electronic Science, Hubei University, Wuhan, Hubei 430062, P. R. China

4Hubei Yangtze Memory Laboratories, Wuhan 430205, China

5State Key Laboratory of Multiphase Flow in Power Engineering, School of Energy and Power Engineering, Xi’an Jiaotong University, Xian 710049, China

*Correspondence: zhu-bin@seu.edu.cn; chenxia@hubu.edu.cn

#Muhammad Yousaf and Yuzheng Lu contributed equally to this work.

Figures

Fig. S1: XRD pattern of ZFO-CeO2 sample.

Fig. S2: Tuac’s plots of UV-Vis absorption spectra of pure ZFO and CeO2 samples.

Before OG                                    After OG

Fig. S3: Lattice disorder and different site radii in ZFO-CeO2 sample interface before and after optimization geometry (OG)

Fig. S4: (a)ZnFe2O4 (ZFO) crystal structure with their basic information i.e., space group, space group number, (b) CeO2 crystal structure information, i.e., space group, space group number, (c) ZFO-CeO2 interfacial structural disorder transformed to another phase.

Fig. S5: Ag/ZFO/CeO2/Ag layered structure under N2 gas atmosphere at 550 °C

To further distinguish chemical states and heterostructure components, Ce 3d and O 1s core level spectra of both prepared samples are deconvoluted Gaussian functions and Shirley background. Moreover, the deconvolution of Ce4+ to Ce3+ ions at the heterostructure surface was detected and presented in supplementary Fig. S6. The Ce3+ existence can be attributed due to the mutual diffusion of Fe and Ce at the ZFO/CeO2 interface.

Fig. S6: XPS core level spectra of Ce 3d from ZFO-CeO2 sample.

Fig S7: (a, b and c) EIS measurements of ZFO, CeO2 and ZFO-CeO2 at different operational temperature (485 °C to 360 °C) under H2 and air.

Supplementary Table S1: EIS fitting parameters of ZFO-CeO2 sample using ZSIMPWIN software, where R represents to the resistance and Q is constant phase elements (CPE). The R and Q have the units of Ω.cm2 and F cm-2, respectively.

| Temperature (℃) | Ro | R1 | Qct | N1 | C1 | Rmt | Qmt | N2 | C2 | RP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 510 | 0.071 | 0.06 | 0.28 | 0.39 | 4.6E-04 | 0.19 | 0.17 | 0.796 | 0.070532 | 0.25 |
| 485 | 0.076 | 0.09 | 0.128 | 0.51 | 1.75E-3 | 0.27 | 0.35 | 0.64 | 0.092843 | 0.36 |
| 460 | 0.082 | 0.12 | 0.08 | 0.669 | 8.03E-2 | 0.36 | 0.343 | 0.7 | 0.139952 | 0.48 |
| 435 | 0.091 | 0.16 | 0.912 | 0.8 | 5.64E-01 | 0.74 | 0.54 | 0.8 | 0.429339 | 0.9 |
| 410 | 0.11 | 0.24 | 1.035 | 0.88 | 8.55E-01 | 1.37 | 0.63 | 0.98 | 0.628 | 1.61 |
| 385 | 0.16 | 0.39 | 2.4 | 0.55 | 2.273 | 2.54 | 0.8 | 0.88 | 0.881 | 2.93 |
| 360 | 0.44 | 1.2 | 2.3 | 0.56 | 5.106 | 3.86 | 1.2 | 1 | 1.20 | 5.06 |

Supplementary Table S2: EIS fitting parameters of ZFO sample using ZSIMPWIN software, where R represents to the resistance and Q is constant phase elements (CPE). The R and Q have the units of Ω.cm2 and F cm-2, respectively.

| Temperature (℃) | Ro | R1 | Qct | N1 | C1 | Rmt | Qmt | N2 | C2 | RP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 510 | 0.25 | 0.06 | 0.21 | 0.28 | 2.73E-06 | 0.53 | 0.404 | 0.532 | 0.104126 | 0.53 |
| 485 | 0.32 | 0.1 | 0.270 | 0.26 | 9.26E-06 | 1.06 | 0.71 | 0.9 | 0.687928 | 1.06 |
| 460 | 0.45 | 0.38 | 0.002 | 0.8 | 3.32E-4 | 2.47 | 0.920 | 0.77 | 1.1802 | 2.85 |

Supplementary Table S3: EIS fitting parameters of CeO2 sample using ZSIMPWIN software, where R represents to the resistance and Q is constant phase elements (CPE). The R and Q have the units of Ω.cm2 and F cm-2, respectively.

| Temperature (℃) | Ro | R1 | Qct | N1 | C1 | Rmt | Qmt | N2 | C2 | RP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 510 | 0.13 | 0.07 | 0.086 | 1 | 0.086 | 0.419 | 0.88 | 0.42 | 0.221 | 0.489 |
| 485 | 0.14 | 0.19 | 0.40 | 0.8 | 0.210 | 0.99 | 0.41 | 0.62 | 0.235 | 1.18 |
| 460 | 0.17 | 0.26 | 0.31 | 0.8 | 0.165 | 1.13 | 0.62 | 0.44 | 0.394 | 1.39 |

Fig. S8: Electrochemical impedance spectra ZFO-CeO2 electrolyte measured in H2 (5%), D2, pure H2(95%) and H2/air atmosphere at 510 °C.

Fig. S9: I-V and I-P curves of pure ZFO fabricated fuel cell device.

Fig. S10: I-V and I-P curves of pure CeO2 fabricated fuel cell device.

Fig. S11: I-V and I-P curves of ZFO-CeO2 with different mass ratios of 3:7, 4:6 and 5:5 constructed electrolytes.

Fig. S12: I-V and I-P curves of Ni-NCAL/BZY/ZFO/BZY/Ni-NCAL device at 510 °C.