Supplementary Information

Supplementary Note 1: the POEM and some important findings from the POEM study of the C-NP system

Following Equations (3), (4) and (5) in the manuscript, we have the complete form of solution as Equation (S1), which is further consolidated as Equation (S2).

(S1)

(S2a)

(S2b)

The eigenvalues,are calculated as

(S3)

According to Equation (S2),  is at a pole when one or both of the denominators vanish, i.e. or . As an example, pole on the first eigenvalue () is considered. For and , the pole appears when the following conditions are met.

(S4a)

(S4b)

To solve Equations (S4a) and (S4b), we let

(S5)

where , for . Calculation and simplification then show that   and .

The expression is generally greater than zero as and  in the dielectric C-NP systems.

From Equation (S4a) and (S5), we have

() 	(S6)

For , Equation (S6) returns

(S7)

For, the pole is on the second eigenvalue, i.e. , which also returns Equation (S7).

From Equation (S4b) and (S5), we have

(S8)

The expression for the real frequency that gives rise to a pole is then derived as Equation (S9), where the pole is associated with the first and second eigenstate according to (first eigenstate for  and second for).

,	(S9a)

,(S9b)

With Equation (S7), any single unknown from the set , ,  and (with the rest three known) can be found by solving this cubic equation.

Particularly, Equation (S7) yields a solution for that becomes invalid when

(S10)

Simplification of Equation (S10) reveals that the coupling factor must satisfy   in order for the system to have a pole at all.

On the other hand, when, i.e. , Equation (S4a) becomes impossible as it then implies that . Unless the losses of both oscillators are zero – a scenario that is generally nonexistent in real world – such system does not have a pole. Coincidentally, the resonance has symmetric line-shape for. Hence, it follows that the pole must come from a resonance with an asymmetric line-shape.

Differentiating both sides of Equation (S2a), we have Equation (S11), which shows that the pole of  is also the pole of .

(S11)

Supplementary Note 2: POEM study of the NP, R and R + NP structures

Table S1 summarizes the values of parameters adopted in the POEM study for the six structures discussed in the manuscript. For standalone dielectric NP, oscillator 1 is the NP while oscillator 2 is a flat background with large loss. For standalone R, oscillator 1 is the flat background with large loss while oscillator 2 is the ring.

When the adsorption layer is added, the resonance red shifts, resulting in a non-zero ( for NP + A and  for R + A). Field localization gives rise to larger spectral shift with the NP than with the R, so NP + A is given a larger  than R + A. For simplicity,  associated with the R in the R + NP + A structure is neglected.

For the standalone dielectric NP, as coupling between the NP resonance and the background is weak, the phase of the coupling factoris assumed 0. Coupling between the R and its background is stronger, so is given a nonzero phase.

The loss factors  and  are assigned values that are representative of their respective resonance Q-factors. For the standalone NP, as the adsorption layer increases the resonance Q-factor,  is made smaller for NP + A than for NP. For standalone R, the addition of adsorption brings the ring closer to a complete loop, so there is a slight decrease in . For the R + NP structure, as the coupled resonance has much higher Q-factor, the decrease in loss introduced by adsorption layer is negligible. So  is kept the same as that of the R.

The magnitude of coupling factor affects the extinction ratio of the resultant resonance and different values are chosen for different structures.

Plots of R and R + A are normalized to the maximum value of R; plots of R + NP and R + NP + A are normalized to the maximum of R +NP. However, since the standalone NP resonance peak is directly proportional to the NP scattering and the NP + A structure has larger scattering than NP, R + NP and R + NP + A are normalized to the maximum value of NP + A.

Table S1.

| NP | 0.25 | 1 | 0.25 | 0 | N/A | N/A |
| --- | --- | --- | --- | --- | --- | --- |
| NP + A | 0.23 | 1 | 0.251 | 0 | 0.01 | 0 |
| R | 1 | 0.001 | 0.008 | 0.1π | N/A | N/A |
| R + A | 1 | 0.0095 | 0.0075 | 0.1π | 0 | 0.00017 |
| R + NP | 0.25 | 0.00015 | 0.004 | 0.9π | N/A | N/A |
| R + NP + A | 0.25 | 0.00015 | 0.004 | 0.9π | 0 | 0.0005 |

Dipole moment plots of the NP and NP + A structure obtained by POEM are shown in Fig. S1a; transmission plots of the NP and NP + A structure by FDTD simulation are shown in Fig. S1b. Instead of integrating scattering flux in all directions, the transmitted spectra only collects power transmission in one direction. That’s why there is a shift of peak from the expected wavelength (650 nm) in the spectra of Fig. S1b.

Fig. S1 a.  spectra of the standalone NP and NP + A structure modeled by the POEM; b. transmitted power spectra of the standalone NP and NP + A structure simulated by FDTD.

Supplementary Note 3: dynamic FDTD simulation of the pump-probe experiment with gain-assisted open ring

The polarization densities  of the transition 0 ↔ 3 and  of the transition 1 ↔ 2 are driven by the local electric field according to

, . 	(S12)

Where  is the population inversion,  is a phenomenological coupling constant, and  is the FWHM of the atomic transition at central frequency  (Fig. S2). For lasing transition,  can generally be calculated as . The electron occupation density for each energy level , , , obey the following rate equations.

(S13)

Where the lifetimes ,, and characterize the transitions between specified energy levels (Fig. S2). Table S2 summarizes the values of all aforementioned parameters used in the dynamic modeling of the four-level atomic system.

Fig. S2 Schematic representation of the four-level atomic system and the parameters involved to describe it.

Table S2 Major parameters used in describing the four-level gain system and their values

|  | (1015 s-1) | (1015 s-1) | (ns) | (ns) | (ns) | (ns) |
| --- | --- | --- | --- | --- | --- | --- |
|  | 3.86 | 0.052 | 0.01 | 10.25 | 0.01 | 4.1 |
|  | 3.42 | 0.044 |  |  |  |  |

The gain level corresponding to a certain population inversion in a four-level gain system can be inferred from the complex valued refractive index 1.

(S14)

The gain coefficient is calculated from the complex dielectric constant as, where .

To numerically simulate the pump-probe experiment, an intense Gaussian pump pulse is first launched. The pump wave is incident onto the whole structure from above in a way that the ring is spatially covered by the pump light except for a strip of area encompassing the ring opening where the dielectric NP detects the adsorption of sensing target. The reason for excluding the ring opening is to mimic the real bio-sensing scenario in which case direct pumping of the sensing spot is preferably avoided to protect the nature of the bio-materials. Figure S3 shows the logarithmic scale occupation densities of all four levels in the gain material as a function of time after the pump pulse is launched at time 0.

Fig. S3 Occupation densities of the four-level gain medium in time. Data is recorded at the center point of the nanocube surface in the xy-plane.

30 ps after the injection of the pump pulse, all four occupation densities level off and a weak probe pulse is incident onto the ring opening. The spatial coverage of the incident probe pulse is slightly larger than the opening – the same configuration with the simulation of passive R + NP system. A time monitor placed on the dielectric NP records the oscillation of electric field over time. Figure S4 shows the field oscillation in a time span of 260 ps after the injection of the pump pulse for the case where pumping rate Np = 2.4 x 109 /s. The pump pulse is indicated in blue while the field after the launching of probe pulse is indicated in red. Upper insets of Fig. S4 show the detailed view of the probe pulse and its corresponding frequency spectrum obtained by fast Fourier transform (FFT); the lower right inset of Fig. S4 zooms in on a time region where the simulation is close to converge (t = 229 ps); the lower left inset shows the corresponding frequency spectrum by FFT.

Fig. S4 Electric field amplitude of the pump-probe simulation of R + NP + A structure at the critical gain.

Supplementary Note 4: sensing with gain-assisted ring, another scenario

Pole of the R + NP structure is found for Np = 2.65 x 109. When the adsorption layer with Δn = 0.01 is enclosed onto the SiN nanoparticle, the transmitted peak red shifts about 30 pm. Under such gain condition, the R + NP is critically amplified while the R + NP + A system is over-amplified, resulting in 10 pm and 25 pm FWHM respectively. The gain has not reached saturation, and the peak height of R + NP + A is more than two times that of the R + NP. The transmitted power spectra are shown in Fig. S5. The NOAR is calculated as 82.5%.

Fig. S4 Electric field amplitude of the pump-probe simulation of R + NP + A structure at its critical gain.

Reference

1.	Wuestner, S., Pusch, A., Tsakmakidis, K. L., Hamm, J. M. & Hess, O. Overcoming Losses with Gain in a Negative Refractive Index Metamaterial. Phys. Rev. Lett. 105, 127401 (2010).