Supporting Information

Sunlight active cellulose/g-C3N4/TiO2 nano-photocatalyst for degradation of industrial dye and pharmaceutical drug in real wastewater

Anushka Garga, Anjali Chauhanb, Charu Agnihotric, Bhim Pratap Singhc, Vasundhara Mondemb,  Soumen Basua and Shekhar Agnihotric,d*

aSchool of Chemistry and Biochemistry, Thapar Institute of Engineering and Technology, Bhadson Road, Patiala 147004, Punjab, India

bDepartment of Biotechnology, Thapar Institute of Engineering and Technology, BhadsonRoad, Patiala 147004, Punjab, India

cDepartment of Agriculture and Environmental Sciences, National Institute of Food Technology Entrepreneurship and Management, Kundli, Sonepat 131028, Haryana, India

dCentre for Advanced Translational Research in Food Nano-Biotechnology (CATR-FNB), National Institute of Food Technology Entrepreneurship and Management, Kundli, Sonepat-131028, Haryana, India

*Corresponding author: agnish@niftem.ac.in

S1	Materials Required

Titanium butoxide (>97% purity), cellulose, absolute ethanol (99.9% pure) and NaOH pellets were procured from Sigma-Aldrich, India while urea (ultrapure, >99.9% purity) were purchased from Loba-Chemie Pvt. Ltd, India. Methylene blue dye (>99% purity) was received from SD Fine Chemicals, Mumbai. Atenolol drug (generic salt) was received as a gift from a local manufacturer of active pharmaceutical ingredients. Antibacterial studies were carried out against Escherichia coli MTCC 739 strain, obtained from the microbial type culture collection (MTCC) at CSIR-IMTECH, Chandigarh, India. The real industrial wastewater (as, secondary effluent) was obtained from a textile industry in Ludhiana (Punjab, India). All reagents were of analytical grade and used without any further purification. All working solutions were prepared in deionized water.

S2	Material characterization

The surface morphology of samples was determined through scanning electron microscopy (SEM, JSM-7600F) while the elemental composition was evaluated energy dispersive X-ray (EDX) spectroscopy. Diffuse reﬂectance spectroscopy (DRS) was carried out using an integrating sphere spectrophotometer setup (Shimadzu UV-2600, Japan) at 8˚ incidence in a range 350 –750 nm, integrated over a period of 5s. To characterize the phase and crystallinity of the samples, X-Ray Diffraction (XRD, PANalyticaX'Pert Pro) equipped with graphite monochromatized Cu Kα radiation was operated in a 2θ range from 10ᵒ to 80ᵒ. BET analyzer (Microtrac Belsorp Mini-II, Japan) was employed to determine the surface area of compounds through Barrett–Joyner–Halenda (BJH) method via pore size distribution from N2 adsorption-desorption isotherms. The dynamic light scattering (DLS) and zeta potential for bionanocomposite was analyzed using Brookhaven 90 Plus particle size analyzer. FTIR (Bruker Inc., Germany) spectroscopy was done to examine the functional moieties present in synthesized bionanocomposite. The photocatalytic performance of synthesized nanocomposite and bionanocomposite was monitored using a UV-Vis spectrophotometer (Shimadzu 2600) for degradation of methylene blue (664 nm) and atenolol (224 nm) at their absorption maxima.

S3	Bang Gap Energy Estimation using DRS data

The band gap energies of the samples were estimated by Kubelka−Munk transformation, αhv = A(hv − Eg), where α represents the absorption coefficient, h is Planck's constant, v is the light frequency, Eg is the band gap energy, and A is a constant. Usually, the determination of Eg involves plotting αhv against hν.

The CB and VB potentials of TiO2 and g-C3N4 can be further estimated according to the following equations:

EVB =X ‒ Ec + 0.5Eg

ECB = EVB ‒ Eg

Where EVB represents the VB edge potential, ECB is the CB edge potential, X stands for the electronegativity of the semiconductor (5.81 eV for TiO2 and 4.64 eV for g-C3N4). Ec represents the energy of free electrons on the hydrogen scale (about 4.5 eV) while, Eg is the band gap energy of the semiconductor.

S4	Decolouration rate and Kinetic models

The average decolouration rate (g/h) under optimized conditions was also calculated as follows

Average decolouration rate =C × %D × 1000100 × t

Where, C= initial dye concentration (mg/L), D= rate of dye decoloration (%) after time t (h).

The kinetics of degradation of dyes was studied using the following four kinetics equation.

In general, Langmuir-Hinshelwood kinetic model is used to explain the dependency of photocatalytic reaction rates on the concentration of organic pollutants

r=dCdt= krKC1+KC

The above reaction can be written simplified to a pseudo first order equation

lnCoC=kappt

where r is the oxidation rate of the reactant (mg/L h-1), C the concentration of the reactant at time t (mg/L), C0 the initial concentration of the reactant (mg/L), t the illumination time, k the reaction rate constant (h-1), and K is the adsorption coefficient of the reactant onto the catalyst particles (L/mg). the rate constant were determined using linear fitted plots of lnCoC  versus t, the time interval of reaction grounded on the dye degradation curves by the approximation of the slope of a line. The R2 for first, second and pseudo

First order kinetics: 		ln(COC)=kapp ×t

Psuedo-first order kinetics:	 1Ct = 1CO+ Kapp ×t

Second order kinetic :		1C-1Co=Kappt

Psuedo second order                 tC = tCo - 1KappC2

Where, C0 = initial concentration of dye, C= dye concentration at time t, kapp= apparent rate constant.

Table S1: BET measurement of Surface area, mean pore diameter & pore volume of composites

| Parameters | g-C3N4/TiO2 | cellulose-TiO2 | gC3N4/TiO2/cellulose |
| --- | --- | --- | --- |
| Mean pore diameter (nm) | 9.80 | 8.34 | 10.77 |
| Specific Surface area(m2/g) | 125.76 | 6.49 | 2.997 |
| Total pore volume (cm3/g) | 0.308 | 0.013 | 0.008 |

Table S2: Kinetic parameters for degradation of MB under sunlight illumination

| Models | Equation | Rate constant, k | R2 values |
| --- | --- | --- | --- |
| First-order | ln [Co-C] = - kappt | 18.52 x 10-3 min-1 | 0.894 |
| Pseudo First-order | ln [C-Co] = kappt | 8.78 x 10-3 min-1 | 0.996 |
| Second-order | 1C - 1Co = kappt | 2.74 x 10-3 mg-1∙L min-1 | 0.588 |
| Pseudo Second-order | tC = tCo - 1kappC2 | 3.58 x 10-1 mg-1 L min-1 | 0.574 |

Table S3: A comparative study of degradation efﬁciency and rates of degradation of contaminants

| Type of nano-photocatalyst | Contaminants | Degradation efficiency (%) | Light source | Ref.† |
| --- | --- | --- | --- | --- |
| g-C3N4/TiO2 | Methylene Blue | 81% | Xenon lamp (300 W，λ>420 nm) | Duong et al. 2019 |
| g-C3N4/TiO2 | Pharmaceutical contaminants | 95% | oxygen plasma-treated | Liu et al. 2020 |
| Fe/Si/TiO2 | Metronidazole | 93% | 220 W Xe lamp (λ = 400 nm) | Du et al. 2018 |
| g-C3N4/TiO2/Cellulose | Methylene Blue | 95% | Sunlight | Present Work |
| g-C3N4/TiO2/Cellulose | Atenolol | 90.2% | Sunlight | Present Work |

†

- Duong, D.P.T., Van, T.D., Dai, P.B., Tran, T.N.N., Nguyen, T.N.U., Minh, T.C., Nguyen, T.K., Kim, Y.S. and Van, V.P., 2019. Excellent visible light-driven photocatalytic performance and band alignment of g-C3N4/TiO2 nanotube heterostructures. Materials Research Express, 6(8), p.085061.

- Liu, R., Sun, L., Qiao, Y., Bie, Y., Wang, P., Zhang, X. and Zhang, Q., 2020. Efficient Photocatalytic degradation of pharmaceutical pollutants using plasma‐treated g‐C3N4/TiO2. Energy Technology, 8(7), p.2000095.

- Du, W., Xu, Q., Jin, D., Wang, X., Shu, Y., Kong, L. and Hu, X., 2018. Visible-light-induced photo-Fenton process for the facile degradation of metronidazole by Fe/Si co-doped TiO2. RSC advances, 8(70), pp.40022-40034.

Figure S1: Corresponding degradation kinetics for single parameter studies during optimization (a) Catalyst dose (b) initial dye conc. (c) time and (d) pH

Figure S2: COD and TOC removal in textile wastewater