Supplemental Material

Chemically and Electronically Active Metal Ions on InAs Quantum Dots for Infrared Detectors

Seongchan Kim‡,1, Sooyeon Yeon‡,1, Minwoo Lee1, Junyoung Jin2, Seungki Shin1, Namyoung Gwak1, Inyoung Jeong1, Hyunwoo Jang1, Gyu Weon Hwang2 and Nuri Oh*,1

1Division of Materials Science and Engineering, Hanyang University, 222, Wangsimni-ro, Seongdong-gu, Seoul, 04763, Republic of Korea, and 2Center for Neuromorphic Engineering, Korea Institute of Science and Technology, 5 Hwarang-ro 14-gil, Seongbuk-gu, Seoul, 02792, Republic of Korea

Figure S1. (a) TEM image, (b) absorption, and (c) XRD pattern of zinc arsenide amorphous particles. (JCPDS No. 04-002-0147)

Figure S1. (a) TEM image, (b) absorption, and (c) XRD pattern of zinc arsenide amorphous particles. (JCPDS No. 04-002-0147)

Figure S2. Absorption spectra of InAs QDs synthesized at 330 °C by changing the Zn/In molar ratio from 0 (red) to 2 (green).

Figure S2. Absorption spectra of InAs QDs synthesized at 330 °C by changing the Zn/In molar ratio from 0 (red) to 2 (green).

Figure S3. XRD patterns of InAs QDs synthesized at 330 °C by changing the Zn/In molar ratio from 0 (red) to 2 (green).

Figure S3. XRD patterns of InAs QDs synthesized at 330 °C by changing the Zn/In molar ratio from 0 (red) to 2 (green).

Table S1. Molar ratios of In to As and In to Zn obtained by ICP-OES

Table S1. Molar ratios of In to As and In to Zn obtained by ICP-OES

| In : As : Zn (mole fraction) | Molar ratio obtained by ICP-OES |  |  |
| --- | --- | --- | --- |
|  | In | As | Zn |
| 2 : 1 : 0 | 1 | 0.9379 | - |
| 2 : 1 : 2 | 1 | 0.9368 | 0.01677 |
| 2 : 1 : 4 | 1 | 0.9320 | 0.02152 |

Figure S4. XPS spectra for P 2p level of InAs QDs synthesized (a) without and (b) with Zn precursor.

Figure S4. XPS spectra for P 2p level of InAs QDs synthesized (a) without and (b) with Zn precursor.

Figure S5. The size distribution and histograms measured diameters for (a) InAs QDs and (b) InAs:Zn QDs.

Figure S5. The size distribution and histograms measured diameters for (a) InAs QDs and (b) InAs:Zn QDs.

Figure S6. Photographs of (a) InAs and (b) InAs:Zn QDs two months after the synthesis.

Figure S6. Photographs of (a) InAs and (b) InAs:Zn QDs two months after the synthesis.

Figure S7. UPS spectra (a) of InAs and InAs:Zn QDs (The inset shows the secondary electron cut-off), and (b) Tauc plots of both QDs.

Figure S7. UPS spectra (a) of InAs and InAs:Zn QDs (The inset shows the secondary electron cut-off), and (b) Tauc plots of both QDs.

Figure S8. Photocurrent of (a) bare InAs and (b) InAs:Zn QD-photodiodes as a function of bias with different power density of 1050 nm IR illumination.

Figure S8. Photocurrent of (a) bare InAs and (b) InAs:Zn QD-photodiodes as a function of bias with different power density of 1050 nm IR illumination.

Figure S9. Photocurrent versus bias voltage plots under illumination of 1050nm: (a) bare InAs QD- and (b) InAs:Zn QD-photodiodes with EDT ligand exchange.

Figure S9. Photocurrent versus bias voltage plots under illumination of 1050nm: (a) bare InAs QD- and (b) InAs:Zn QD-photodiodes with EDT ligand exchange.

Figure S10. Frequency response of QD-photodiodes at 9.55 mW/cm2 for 808 nm illumination.

Figure S10. Frequency response of QD-photodiodes at 9.55 mW/cm2 for 808 nm illumination.