Table 1
Inhibition efficiency for corrosion of mild steel in 0.5 M HCl in the presence of different concentrations of TIB and BTP from weight loss measurments
	Inhibitor
	Concentration of inhibitor in 0.5M HCl (µM)
	Weight of steel before immersion(gr)
	Weight of steel after immersion(gr)
	Weight loss(mg)
	Corrosion rate (CR in mg/cm2h)
	θ
	Inhibition Efficiency (ηw %)

	TIB
	0
	13.151
	12.850
	301
	0.664
	-
	- 

	
	200
	11.964
	11.733
	231
	0.509
	0.232
	23.34

	
	400
	13.005
	12.813
	192
	0.423
	0.362
	36.29

	
	600
	11.897
	11.847
	50
	0.110
	0.834
	83.43

	
	800
	12.065
	11.963
	102
	0.225
	0.661
	66.11

	
	1000
	12.173
	12.019
	154
	0.340
	0.488
	48.80

	BTP
	0
	13.151
	12.85
	301
	0.648
	-
	- 

	
	200
	12.822
	12.552
	270
	0.581
	0.103
	10.30

	
	400
	12.163
	12.101
	62
	0.133
	0.794
	79.41

	
	600
	12.024
	11.954
	70
	0.151
	0.767
	76.74

	
	800
	11.923
	11.764
	159
	0.342
	0.472
	47.18

	
	1000
	12.021
	11.846
	175
	0.377
	0.418
	41.86


















