Table 1

Inhibition efficiency for corrosion of mild steel in 0.5 M HCl in the presence of different concentrations of TIB and BTP from weight loss measurments

| Inhibitor | Concentration of inhibitor in 0.5M HCl (µM) | Weight of steel before immersion(gr) | Weight of steel after immersion(gr) | Weight loss(mg) | Corrosion rate (CR in mg/cm2h) | θ | Inhibition Efficiency (ηw %) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TIB | 0 | 13.151 | 12.850 | 301 | 0.664 | - | - |
|  | 200 | 11.964 | 11.733 | 231 | 0.509 | 0.232 | 23.34 |
|  | 400 | 13.005 | 12.813 | 192 | 0.423 | 0.362 | 36.29 |
|  | 600 | 11.897 | 11.847 | 50 | 0.110 | 0.834 | 83.43 |
|  | 800 | 12.065 | 11.963 | 102 | 0.225 | 0.661 | 66.11 |
|  | 1000 | 12.173 | 12.019 | 154 | 0.340 | 0.488 | 48.80 |
| BTP | 0 | 13.151 | 12.85 | 301 | 0.648 | - | - |
|  | 200 | 12.822 | 12.552 | 270 | 0.581 | 0.103 | 10.30 |
|  | 400 | 12.163 | 12.101 | 62 | 0.133 | 0.794 | 79.41 |
|  | 600 | 12.024 | 11.954 | 70 | 0.151 | 0.767 | 76.74 |
|  | 800 | 11.923 | 11.764 | 159 | 0.342 | 0.472 | 47.18 |
|  | 1000 | 12.021 | 11.846 | 175 | 0.377 | 0.418 | 41.86 |