Table 3

Thermodynamic parameters for the adsorption of TIB and BTP on mild steel at optimum concentration in 0.5 M HCl at 298 K

| Inhibitor | R2 | Kads×10-6 (mol-1) | -ΔGads° (kJ/mol) |
| --- | --- | --- | --- |
| TIB | 0.982 | 0.0102 | 45.62 |
| BTP | 0.941 | 0.00261 | 39.04 |