Table 1. NL refractive indices measured for ethanol and SiO2 colloids, with different volume fractions (f), using Z-scan, D4σ and IC-scan techniques.

| NL optical technique |  | n2ethanol (cm2/W) | n2SiO2-colloid (cm2/W) |  |
| --- | --- | --- | --- | --- |
|  |  |  | f = 8.2 x 10-3 | 4.1 x 10-3 |
| Z-scan |  | -2.8 x 10-8 | -2.6 x 10-8 | -1.1 x 10-8 |
| D4σ |  | -2.2 x 10-8 | -2.2 x 10-8 | -1.0 x 10-8 |
| IC-scan | self-correlation | -2.2 x 10-8 | -2.1 x 10-8 | -1.3 x 10-8 |
|  | cross-correlation |  | -2.1 x 10-8 | -2.1 x 10-8† |

†NL refractive index measured for intensities up to 15 kW/cm2.

Table 2. NL refractive indices measured for Au-NR colloids using Z-scan, D4σ and IC-scan techniques.

| NL optical technique |  | n2AuNR-colloid (x 10-6 cm2/W) |  |  |
| --- | --- | --- | --- | --- |
|  |  | f = 2.5 x 10-5 | 5.0 x 10-5 | 7.5 x 10-5 |
| Z-scan |  | -0.56 | -0.86 | -0.75 |
| D4σ |  | -0.27 | -0.45 | -0.46 |
| IC-scan | self-correlation | -0.56 | -0.88 | -1.04 |
|  | cross-correlation | -0.86 | -1.26 | -1.73 |