Supplementary Information for

Efficient Liquid Multicarbon Production from Overall CO2 Photoreduction by Creating a Superhydrophobic Gas Storage Space

Hailing Huo1, Zhengwei Du1, Hua He2, Xin Guan2, Chengxi Huang1, Fang Wu3, Yongping Du1, Hongbin Xing1, Jingjing Ma4, Ang Li*1 and Erjun Kan*1

1 MIIT Key Laboratory of Semiconductor Microstructure and Quantum Sensing, Department of Applied Physics, Nanjing University of Science and Technology, Nanjing 210094, P. R. China

2 State Key Laboratory of Heavy Oil Processing and College of Chemical Engineering, China University of Petroleum (East China), Qingdao 266580, P. R. China

3 College of Information Science and Technology, Nanjing Forestry University, Nanjing 210037, P. R. China

4 State Key Laboratory of High-efficiency Utilization of Coal and Green Chemical Engineering, Ningxia University, Ningxia 750021, P. R. China

Corresponding Author

*Ang Li—Email: liang2100@njust.edu.cn

*Erjun Kan—Email: ekan@njust.edu.cn

Supplementary Experimental Procedures

Materials

Copper chloride (CuCl2·2H2O, AR), copper bromide (CuBr2, AR), tetrabutylammonium bromide ((C4H9)4NBr, AR), ascorbic acid (AR), 1-dodecanethiol (C12H25-SH, 99.5%), scopoletin (C10H8O4, 98%) and horseradish peroxidase (≥500 units/mg) were purchased from Aladdin. Copper nitrate (Cu(NO3)2·3H2O, AR) and potassium bicarbonate (KHCO3, AR) were purchased from Macklin. Sodium hydroxide (NaOH, AR), ethanol (AR), silvernitrate (AgNO3, >99.0%), and ammonium sulfate ((NH4)2SO4, AR) were purchased from Sinopharm Chemical Reagent Co., Ltd. Polyvinylpyrrolidone (PVP, M.W=30000) was purchased from Shanghai Yuanye Bio-Technology Co., Ltd. Dimethyl sulfoxide (DMSO) was purchased from Sigma-Aldrich. Cy5 NHS ester was purchased from Shanghai So-Fe Biomedicine Co., Ltd. Deionized water (DI water, 18.25 MΩ·cm) supplied by a UP Water Purification System was used in the whole experimental processes. All chemicals were obtained from commercial suppliers and used without further purification.

Characterizations

Transmission electron microscope (TEM) was performed on a JEOL JEM 2100F electron microscope. Scanning electron microscope (SEM) was performed on Hitachi SU8220. Crystalline structures were evaluated by X-ray diffraction (XRD) analysis using a Bruker D8 Focus operating at 40 kV and 40 mA equipped with a nickel-filtered Cu Kα radiation (λ=1.54056 Å). Specific surface areas and pore structures of catalysts were measured using Micromeritics, ASAP 2460 by nitrogen adsorption at 77 K. The specific surface areas were calculated from the isotherms using the BET method. The pore distribution was obtained by the BJH method from the adsorption branch of the adsorption isotherms. Room temperature photoluminescence (PL) spectra were performed on FL 970 fluorescence spectrophotometer under the excitation wavelength of 380 nm with 510 nm filter. UV-vis diffuse reflectance spectra were recorded using UV-2600 under the visible light of 400-800 nm. Here reflectivity was used to detect the light absorption through the conversion of Kubelka-Munk formula and BaSO4 was used as the reference sample. X-ray photoelectron spectroscopy (XPS) was performed on ThermoFischer, ESCALAB 250Xi with Al K X-ray source to reveal chemical states, and the binding energies were calibrated by the C 1s electron peak (BE=284.8 eV). Fourier transform infrared spectroscopy (FTIR) spectra were recorded by Thermo Fisher Nicolet IS10 in absorbance mode. In situ FTIR spectra were performed on Thermo Fisher Nicolet IS50. Water contact angles were measured by SDC-350 instrument with the samples uniformly dispersed on glass substrates using ethanol as solvent. The volume of the water droplet was 7 μL and the final results were average values obtained from more than three positions. Total internal reflection fluorescent microscope (TIRFM) measurements were carried out on Nikon A1.

Supplementary Fig. 1 | As-prepared Cu2O photocatalysts. a CHS and O-CHS. b CSS and O-CSS. c O-CNS.

Supplementary Fig. 2 | SEM image. The SEM image of the obtained O-CHS.

Supplementary Fig. 3 | TEM and HRTEM images. a-c HRTEM images of CSS (a), O-CSS (b) and O-CNS (c). Insets in a-c are the TEM image of CSS, O-CSS and O-CNS, respectively. The scale bar in the insets is 100 nm.

The lattice spacings of CSS, O-CSS and O-CNS are all 0.244 nm, which are in good agreement with the (111) planes of Cu2O, revealing that these structures are composed of the Cu2O material.

Supplementary Fig. 4 | XPS results of catalysts. a XPS survey spectra of CHS (1), CSS (2), O-CHS (3), O-CSS (4) and O-CNS (5). b The atomic percentages of S and Cu obtained from XPS measurements for O-CHS, O-CSS and O-CNS. The low atomic percentages of S show the low contents of S, implying the low amount of 1-dodecanethiol used for hydrophobic modification. Meanwhile, the similar atomic percentages of S and Cu for O-CHS, O-CSS and O-CNS also illustrate their similar situations of the hydrophobic modification.

Supplementary Fig. 5 | The interaction between 1-dodecanethiol and Cu2O. Schematic diagram of 1-dodecanethiol molecule adsorbed on the surface of the Cu2O catalyst.

Supplementary Fig. 6 | Water contact angle of O-CHS. a After Xe lamp irradiation for 5 hours. b After a long storage time of 20 days.

Supplementary Fig. 7 | Results of Ag+ probe experiment for O-CHS. a-c HAADF-STEM image (a), HRTEM image (b), and EDS spectrum (c) of O-CHS loaded with Ag nanopaticles. d-g EDS elemental mapping images for Ag, Cu, O and S of O-CHS loaded with Ag nanopaticles. h Cu and Ag overlap signals of O-CHS loaded with Ag nanopaticles.

A typical lattice distance of 0.235 nm is clearly identified (Supplementary Fig. 7b), which can be assigned to the (111) facet of Ag. Meanwhile, EDS mapping images (Supplementary Fig. 7d-h) display clearly that Ag particles are uniformly distributed on the surface, where photogenerated electrons are accumulated with holes consumed by methanol. More importantly, the ratio of Ag/Cu (1:3.5395) for O-CHS (Supplementary Fig. 7c) is almost equal to that for CHS (1:3.5378) shown in Supplementary Fig. 8c, indicating their similar charge transfer. Thus, the hydrophobic treatment has no obvious effect on the charge transfer from the surface to the adsorbate, which would be due to the small amount of 1-dodecanethiol used.

Supplementary Fig. 8 | Results of Ag+ probe experiment for CHS. a-c HAADF-STEM image (a), HRTEM image (b), and EDS spectrum (c) of CHS loaded with Ag nanopaticles. d-f EDS elemental mapping images for Ag, Cu, and O of CHS loaded with Ag nanopaticles. g Cu and Ag overlap signals of CHS loaded with Ag nanopaticles.

Similar to Supplementary Fig. 7, a typical lattice distance of 0.235 nm is clearly identified, which can be assigned to the (111) facet of Ag. EDS mapping images display clearly that Ag particles are uniformly distributed on the surface, demonstrating the successful synthesis of CHS loaded with Ag nanoparticles.

Supplementary Fig. 9 | Spectral characterizations. a-c The normalized UV-vis diffuse reflectance spectra (a), Tauc plots (b) and Photoluminescence (PL) spectra under 380 nm laser irradiation with 510 nm filter (c) of CHS, O-CHS, CSS, O-CSS and O-CNS.

Supplementary Fig. 10 | The results of nitrogen adsorption-desorption measurements. a Nitrogen adsorption-desorption isotherms and the corresponding BET surface areas of CSS and O-CSS. b Nitrogen adsorption-desorption isotherms and the corresponding BET surface areas of CHS, O-CHS and O-CNS.

CHS and O-CHS have slightly larger surface areas than CSS and O-CSS, and also O-CNS has the largest surface area. In addition, compared with the unmodified structures, the surface areas of modified O-CNS and O-CSS slightly decrease, illustrating the modest impact of hydrophobic modification.

Supplementary Fig. 11 | Schematic diagram of dye fluorescence. Schematic diagrams of the fluorescence performances for O-CHS (left) and CHS (right) after dyeing with Cy5 NHS ester under 635 nm excitation in TIRFM measurements.

Theoretically, the fluorescent molecule dissolved in water can penetrate into the cavity of CHS through the mesopores and be concentrated inside, especially near the shell due to the adsorption. Thus, the fluorescence signal would appear in both the interior and exterior of CHS, and also the intensity near the shell would be stronger than that of bulk solution. While for O-CHS, because of the superhydrophobic surface, it is difficult for the fluorescent molecules to penetrate the shell into the cavity. It would accumulate in large quantities around the shell, where high fluorescence intensity would be displayed. Then the fluorescence intensity away from the shell gradually weakens due to the diffusion of the fluorescent molecules, resulting in a faint fluorescent ring outside the shell.1

Supplementary Fig. 12 | The original data obtained from GC. The original data of methanol and ethanol generation over O-CHS detected by GC. The characteristic peaks of methanol and ethanol obviously increased along with reaction time.

Supplementary Fig. 13 | Standard curves. a-b The standard curves used to calculate the contents of methanol (a) and ethanol (b) generated during photocatalytic CRR.

Supplementary Fig. 14 | Supplemental photocatalytic CRR performance. a Selectivity towards carbon derivatives over CSS, O-CSS, CHS, O-CHS and O-CNS. b Photoluminescence (PL) spectra of the scopoletin assay of the reaction solution after photocatalytic CRR with different catalysts. As the amount of H2O2 in the reaction solution was low, a sensitive chemiluminescence detection method by scopoletin assay was performed. The fluorescent scopoletin could be oxidized by H2O2 in the presence of horseradish peroxidase, leading to the loss of its fluorescence. Thus, the higher intensity of the emission peak for scopoletin at 463 nm in the PL spectra indicates a lower concentration of H2O2 in the reaction solution, and vice versa. Comparing the results between the reference (experiment without reaction solution) and photocatalysts, it can be inferred that a small amount of H2O2 is produced over every photocatalyst. c Control experiments under different reaction conditions for photocatalytic CRR on O-CHS. Several blank experiments were performed to ensure that obtained products were from the photocatalytic CRR. First, a test using CO2 and water as reactants but without the photocatalyst was conducted. No carbon derivatives were detected, indicating that the CRR could not happen in the absence of the photocatalyst. When the test was performed in the existence of the catalyst and CO2 but without Xe lamp irradiation, little-to-no carbon derivatives were obtained, which may result from the CRR triggered by natural light. When the reactor was vacuumed and purged Ar instead of CO2, no carbon derivatives were detected under light irradiation in the presence of water and catalyst, demonstrating that the carbon source for ethanol and methanol production in the CRR was CO2. d Generation rates of carbon derivatives on the O-CHS and CHS as a function of irradiation time.

Supplementary Fig. 15 | Performance comparison diagram. Comparison of the ethanol generation rate over different photocatalysts for CRR.

Supplementary Fig. 16 | Isotope-labelling results. a GC-MS spectra of ethanol, generated from 13CO2 photoreduction and 12CO2 photoreduction experiments over O-CHS. b GC-MS spectra of methanol, generated from 13CO2 photoreduction and 12CO2 photoreduction experiments over O-CHS.

Supplementary Fig. 17 | Structural characterization and wettability after reaction. a-b SEM images of O-CHS (a) and CHS (b) after reaction. c XRD patterns, d C 1s XPS spectra and e Cu 2p XPS spectra of O-CHS and CHS after reaction. f-g WCAs of O-CHS (f) and CHS (g) after reaction.

The SEM image and XRD pattern of spent O-CHS show that the morphology and structure of O-CHS are maintained after 6 h of reaction. However, for spent CHS, the SEM image displays serious agglomeration. Meanwhile, extra characteristic diffraction peaks at 24.10° and 31.24° in the XRD pattern of spent CHS are observed, which are assigned to the (220) and (201) planes of basic copper carbonate (Cu2(OH)2CO3), respectively (JCPDS Card No. 41-1390)2. The existence of Cu2(OH)2CO3 in spent CHS can be further proved by the C 1s XPS spectra. The sharp peak at 284.8 eV is attributed to carbon-containing contamination, which is adventitious for spectral calibration. The peaks at 286.2 and 289.5 eV are corresponding to O-C=O and C-O, respectively, demonstrating the formation of Cu2(OH)2CO3.3 This transformation could be owing to the reoxidation of reduced copper species generated during CRR, which can occur easily when exposed to air.4, 5 The more Cu2(OH)2CO3 signal for CHS indicates the more reduced copper species formed. Additionally, the high-intensity shake-up satellites at ca. 940.5, 943.9 and 962.7 eV in Cu 2p XPS spectra assigned to CuO for CHS also illustrate the more serious photocorrosion occurred in CHS.6 Conversely, O-CHS shows better stability. This could be attributed to the shield provided by its superhydrophobic surface, which can repel H2O from the surface of O-CHS. Thus, the electron-mediated photocorrosion involving H2O of Cu2O could be weakened.7, 8 Meanwhile, due to the faster reaction rate for O-CHS to consume more photogenerated holes, hole-mediated photocorrosion could also be inhibited.9, 10 What’s more, the wettability is almost unchanged after reaction, indicating the abundant triphase microenvironments can be kept for O-CHS during CRR.

Supplementary Fig. 18 | CO2 dissolution rate in the suspension of catalysts. a Testing device. b The enlarged view of the temperature and pressure displayed on the actuator. The actuator can display the real-time CO2 pressure in the gas phase of the system and the temperature of the connected Labsolar 6A. c The reactor used in the tests. d The changes of relative amounts of CO2 in the gas phase in the CO2 photoreduction test system with the dissolution time over O-CHS and CHS. e The changes of relative amounts of CO2 in liquid phase in the CO2 photoreduction test system with the dissolution time over O-CHS and CHS.

Supplementary Fig. 19 | Top and side views of different configurations. a-d Slab model of the ideal Cu2O (111) surface (a), Two different adsorption sites of Cu on Cu2O (111) surface (b), Slab model with CO adsorbed on the site of CuCUS (c), and Slab model with CO adsorbed on the site of CuCAS (d). The brown, gray, and red balls represent Cu, C, and O atoms, respectively.

The surface of Cu2O (111) is described by a periodic (3×3) slab and three layers thick (Supplementary Fig. 19a). In order to display the different coordination situations of Cu atoms clearly, the ball-stick model is used for the first layer and the other two layers are replaced by line segments. As shown in Supplementary Fig. 19b, CuCUS represents the coordinatively unsaturated surface Cu atom marked with blue circles, and the other Cu atoms are coordinatively saturated Cu atoms (CuCAS). CO can bond with CuCUS stably (Supplementary Fig. 19c), but not with CuCAS (Supplementary Fig. 19d). Thus, CuCUS is selected as the active site for the DFT calculation and there are nine CuCUS sites on the Cu2O (111) slab (marked with blue circles in Supplementary Fig. 19b).

Supplementary Fig. 20 | The configurations with different *CO coverages. a high *CO coverage. b low *CO coverage of Cu2O. The brown, gray, and red balls represent Cu, C, and O atoms, respectively.

Four CO molecules are placed on CuCUS sites of the Cu2O model, representing the high *CO coverage of O-CHS. In contrast, low *CO coverage of CHS with two CO molecules placed on CuCUS sites is adopted. The Gibbs free energy change (ΔG) of CO adsorption on CuCUS at different *CO coverages are then calculated. The results of -2.450 and -2.398 eV at high *CO coverage and low *CO coverage, respectively, illustrate the stable binding of CO with CuCUS (Supplementary Table 1).

Supplementary Fig. 21 | Top and side views of different configurations. a-l Top and side views of optimized adsorption configurations for main reaction intermediates during CRR to ethanol on Cu2O (111) surface at high *CO coverage. The brown, gray, red, and white balls represent Cu, C, O and H atoms, respectively. TS means transition state; * represents surface adsorption.

Supplementary Fig. 22 | Top and side views of different configurations. a-l Top and side views of optimized adsorption configurations for main reaction intermediates during CRR to ethanol on Cu2O (111) surface at low *CO coverage. The brown, gray, red, and white balls represent Cu, C, O and H atoms, respectively. TS means transition state; * represents surface adsorption.

Supplementary Fig. 23 | Top and side views of different configurations. a-h Top and side views of optimized adsorption configurations for main reaction intermediates during CRR to methanol on Cu2O (111) surface at high *CO coverage. The brown, gray, red, and white balls represent Cu, C, O and H atoms, respectively. TS means transition state; * represents surface adsorption.

Supplementary Fig. 24 | Top and side views of different configurations. a-h Top and side views of adsorption configurations of main reaction intermediates during CRR to methanol on Cu2O (111) surface at low *CO coverage. The brown, gray, red, and white balls represent Cu, C, O and H atoms, respectively. TS means transition state; * represents surface adsorption.

Supplementary Table 1. Gibbs free energy change (∆G) of CO adsorption on the ordered Cu2O(111) surface at different *CO coverages.

| *CO coverage | ∆G (eV) |
| --- | --- |
| high *CO coverage | -2.44952 |
| low *CO coverage | -2.39796 |

Supplementary Table 2. Different intermediates possibly formed under different numbers of H+ transferred and the corresponding energies during ethanol generation at high *CO coverage.

| Number of H+ transferred | Intermediate | Energy（eV） |
| --- | --- | --- |
| 1 | CHO | -805.29535 |
|  | COH | -803.35949 |
| 2 | COCHOH | -808.62853 |
|  | COCH2O | -808.55206 |
|  | COHCHO | -808.01623 |
|  | CHOCHO | -808.25042 |
| 3 | CHOCHOH | -812.61667 |
|  | COCH2OH | -812.40418 |
|  | COCH + H2O | -812.08371 |
|  | COHCHOH | -811.85635 |
| 4 | CHOHCHOH | -817.08981 |
|  | CHOCH2OH | -816.21638 |
|  | CH2OCHOH | -815.88745 |
|  | CHOCH + H2O | -815.44839 |
| 5 | CH2OHCHOH | -820.14588 |
|  | CHOHCH2OH | -820.12281 |
|  | CHOHCH + H2O | -819.41174 |
|  | CHCHOH + H2O | -819.24416 |
| 6 | CH2CHOH + H2O | -824.7696 |
|  | CH3OHCHOH | -823.5143 |
|  | CH2OHCH2OH | -823.97908 |
|  | CH2OHCH + H2O | -822.48591 |
| 7 | CH3CHOH | -813.61466 |
|  | CH2CH2OH | -813.43481 |
|  | CH2CH + H2O | -812.60829 |

In a series of continuous H+ transfer processes, different hydrogenation positions are considered, and the state with the lowest energy is selected and marked in bold and blue (shown in Supplementary Table 2). The initial step is the hydrogenation of *CO. It can be seen that the total energy for the addition of one *H to the carbon atom of *CO to form *CHO is lower than that for the addition of *H to oxygen of *CO to form *COH. Therefore *CHO is considered as the result of *CO hydrogenation. Then *CO-*CHO coupling occurs and hydrogenation processes continue. The different situations of the hydrogenation of *CO-*CHO illustrate that *COCHOH is the state with the lowest energy. In the same way, *CHOCHOH, *CHOHCHOH, *CH2OHCHOH, *CH2CHOH, *CH3CHOH are the results of a series of cascading hydrogenerations.

Supplementary Table 3. Different intermediates possibly formed under different numbers of H+ transferred and the corresponding energies during ethanol generation at low *CO coverage.

| Number of H+ transferred | Intermediate | Energy（eV） |
| --- | --- | --- |
| 1 | CHO | -772.54737 |
|  | COH | -770.28191 |
| 2 | COCHOH | -775.72891 |
|  | COCH2O | -775.69805 |
|  | COHCHO | -775.44682 |
|  | CHOCHO | -775.38418 |
| 3 | CHOCHOH | -779.74153 |
|  | COCH2OH | -779.66037 |
|  | COCH + H2O | -779.23103 |
|  | COHCHOH | -778.82308 |
| 4 | CHOHCHOH | -784.22011 |
|  | CHOCH2OH | -783.28004 |
|  | CH2OCHOH | -783.26036 |
|  | CHOCH + H2O | -781.78617 |
| 5 | CH2OHCHOH | -787.22776 |
|  | CHOHCH2OH | -787.1894 |
|  | CHOHCH + H2O | -786.53899 |
|  | CHCHOH + H2O | -786.26208 |
| 6 | CH2CHOH + H2O | -791.88701 |
|  | CH3OHCHOH | -791.37778 |
|  | CH2OHCH2OH | -791.21733 |
|  | CH2OHCH + H2O | -789.58538 |
| 7 | CH3CHOH | -780.716 |
|  | CH2CH2OH | -780.51346 |
|  | CH2CH + H2O | -779.70392 |

The optimal hydrogenation results for ethanol path at low *CO coverage are similar with those at high *CO coverage and displayed in Supplementary Table 3 with bold and blue.

Supplementary Table 4. Different intermediates possibly formed under different numbers of H+ transferred and the corresponding energies during methanol generation at high *CO coverage.

| Number of H+ transferred | Intermediate | Energy（eV） |
| --- | --- | --- |
| 1 | CHO | -805.29535 |
|  | COH | -803.35949 |
| 2 | CH2O | -809.35756 |
|  | CHOH | -808.78468 |
| 3 | CH3O | -813.23303 |
|  | CH2OH | -813.00428 |

In a series of continuous H+ transfer processes, different hydrogenation positions are considered, and the state with the lowest energy is selected and marked in bold and blue (shown in Supplementary Table 4). The initial step is the hydrogenation of *CO. It can be seen that the total energy for the addition of one *H to the carbon atom of *CO to form *CHO is lower than that for the addition of *H to oxygen of *CO to form *COH. Therefore *CHO is considered as the result of *CO hydrogenation. Then hydrogenation of *CHO continues. The different situations of the hydrogenation of *CHO illustrate that *CH2O is the state with the lowest energy. In the same way, *CH3O is the result of next hydrogeneration.

Supplementary Table 5. Different intermediates possibly formed under different numbers of H+ transferred and the corresponding energies during methanol generation at low *CO coverage.

| Number of H+ transferred | Intermediate | Energy（eV） |
| --- | --- | --- |
| 1 | CHO | -772.54737 |
|  | COH | -770.28191 |
| 2 | CH2O | -776.45335 |
|  | CHOH | -775.8547 |
| 3 | CH3O | -780.4859 |
|  | CH2OH | -780.39353 |

The optimal hydrogenation results for methanol path at low *CO coverage are similar with those at high *CO coverage and displayed in Supplementary Table 5 with bold and blue.

Supplementary Table 6. The possible reaction paths during photocatalytic CRR to ethanol on the catalyst.

Ethanol reaction path

CO2 + e- → CO2-

CO2- + H+ + e- → *COOH

*COOH + H+ + e- → *CO + H2O

*CO + H+ + e- → *CHO

*CO + *CHO + e- → *COCHO + *

*COCHO + H+ + e- → *COCHOH

*COCHOH + H+ + e- → *CHOCHOH

*CHOCHOH + H+ + e- → *CHOHCHOH

*CHOHCHOH + H+ + e- → *CH2OHCHOH

*CH2OHCHOH + H+ + e- → *CH2CHOH + H2O

*CH2CHOH + H+ + e- → *CH3CHOH

*CH3CHOH + H+ + e- → *CH3CH2OH

*CH3CH2OH → CH3CH2OH (g) + e- + *

Supplementary Table 7. The possible reaction paths during photocatalytic CRR to methanol on the catalyst.

Methanol reaction path

CO2 + e- → CO2-

CO2- + H+ + e- → *COOH

*COOH + H+ + e- → *CO + H2O

*CO + H+ + e- → *CHO

*CHO + H++ e- → *CH2O

*CH2O + H+ + e- → *CH3O

*CH3O + H+ + e- → *CH3OH

*CH3OH → CH3OH (g) + e- + *

Supplementary Table 8. Typical photocatalytic systems for reduction of CO2 to ethanol11, 12, 13

| Photocatalyst | Formation rate (μmol g−1 h−1) |  | Light source, reaction mode | Ref. |
| --- | --- | --- | --- | --- |
|  | Methanol (CH3OH) | Ethanol (CH3CH2OH) |  |  |
| O-CHS | 1073.04 | 996.18 | Xe lamp (> 420 nm), Solid-liquid | This work |
| Red phosphorus/Bi2MoO6 | 30.2 | 51.8 | Xe lamp (> 400 nm), Solid-liquid | 14 |
| u-g-C3N4 | 6.3 | 4.5 | Xe lamp (> 420 nm), Solid-liquid | 15 |
| m-g-C3N4 | - | 3.6 | Xe lamp (> 420 nm), Solid-liquid | 15 |
| Monoclinic BiVO4 | - | 101 | Xe lamp (> 400 nm), Solid-liquid | 16 |
| Tetragonal BiVO4 | - | 5.6 | Xe lamp (> 400 nm), Solid-liquid | 16 |
| 1 wt% Co-doped TiO2 | 26 | 18 | Hg lamp (> 380 nm), Solid-vapour | 17 |
| Cu2+-doped TiO2 | 24 | 47 | 365 nm LED lamp, Solid-vapour | 18 |
| TiO2 | 6.7 | 6.3 | 365 nm LED lamp, Solid-vapour | 18 |
| AgBr-NG-g-C3N4 | 21 | 51 | Xe lamp (> 420 nm), Solid-liquid | 19 |
| GO-TiO2 | 12 | 145 | Hg lamp, Solid-liquid | 20 |
| Rh nanowires/TiO2 | - | 12.1 | Xe lamp (< 400 nm), Solid-vapour | 21 |
| TiO2-Pd nanowires | - | 13 | Xe lamp (< 400 nm), Solid-vapour | 21 |
| NiO/Na1-xLaxTaO3+x | 60 | 19 | Hg lamp (300-700 nm), Solid-liquid | 22 |
| MWCNTs/TiO2(anatase) | - | 29.9 | UV lamp (365 nm), Solid-vapour | 23 |
| Cu2O/ml-G | - | 545 | UV lamp (254 nm), Solid-liquid | 24 |
| Pt/TaON | - | 2.03 | Xe lamp (> 420 nm), Solid-liquid | 25 |
| TiO2/Ni(OH)2 | 0.58 | 0.37 | Xe lamp (Simulated sunlight), Solid-vapour | 26 |
| 1.5 wt%Ni2+–TiO2 | 5.58 | 13.2 | Halogen and mercury lamp, Solid-vapour | 27 |
| 5%GQDs/V-TiO2 | 22.5 | 13.5 | Xe lamp (Simulated sunlight), Solid-liquid | 28 |
| 23.2% AgBr/TiO2 | 77.87 | 13.28 | Xe lamp (> 420 nm), Solid-liquid | 29 |
| ZnO/g-C3N4 | 19.0 | 2.5 | Xe lamp (Simulated sunlight), Solid-liquid | 30 |
| Ag3PO4/g-C3N4 | - | 1.3 | Xe lamp (Simulated sunlight), Solid-liquid | 31 |
| 5.8wt%Pd/g-C3N4 | - | 2.18 | Xe lamp (> 420 nm), Solid-vapour | 32 |
| Cu/Pt-HCa2Ta3O10 | 7.4 | 113.2 | Xe lamp (Simulated sunlight), Solid-vapour | 33 |
| BiVO4/RGO | - | 5.15 | Xe lamp (Simulated sunlight), Solid-liquid | 34 |
| Ag@AgBr/CNT | 17.21 | 2.94 | Xe lamp (> 420 nm), Solid-liquid | 35 |
| Red Ag/AgCl | 29.2 | 44.6 | Xe lamp (> 420 nm), Solid-liquid | 36 |
| Sr3Ti(2-x-y)FexSyO(7-z)Nz | 60.1 | 9.9 | Hg lamp (300-700 nm), Solid-liquid | 37 |
| Zn0.8Cd0.2S | 2.5 | 6.0 | Xe lamp (> 400 nm), Solid-liquid | 38 |
| Pd/Mn-TiO2 | 0.104 | 5.699 | Xe lamp (UV light), Solid-liquid | 39 |
| Na(1−x)LaxTaO(3+x) | 35.0 | 3.1 | Hg lamp (300-700 nm), Solid-liquid | 40 |
| CoTPP/Na(1−x)LaxTaO(3+x) | 36.2 | 21.4 | Hg lamp (300-700 nm), Solid-liquid | 40 |
| Cu SAs/UiO-66-NH2 | 5.33 | 4.22 | Xe lamp (400 nm), Solid-liquid | 41 |
| Trimodal silica/g-C3N4 | - | 90 | Xe lamp (λ > 420 nm), Solid-liquid | 42 |
| g-C3N4 (Defect) | 3.85 | 1.98 | Xe lamp (λ > 420 nm), Solid-vapour | 43 |
| SnxNb1−xO2 | 5.25 | 130.36 | Xe lamp, Solid-vapour | 44 |
| SrTiO3(La Cr)/Cu @ Ni/TiN | - | 21.3 | Xe lamp, Solid-liquid | 45 |
| Cu/Cd0.5Zn0.5S | - | 2.26 μmol/h | Xe lamp, Solid-liquid | 46 |
| Cu2O/Pt/NH2-MIL-125(Ti) | 144.82 | 239.49 | Xe lamp (400 nm), Solid-liquid | 47 |
| Cu2O/g-C3N4 | - | 375.66 | Xe lamp (> 420 nm), Solid-liquid | 48 |
| 1.0 wt% AuCu/g-C3N4 | - | 211.9 | Xe lamp (> 420 nm), Solid-liquid | 49 |
| Cu2O-modified layered BiOI | 152.26 | 68.49 | Xe lamp, Solid-liquid | 50 |
| 1%CeO2/3%CuO/TiO2 | - | 30.5 | UV lamp (254 nm), Solid-liquid | 51 |
| InCu/PCN | - | 28.5 | Xe lamp, Solid-liquid | 52 |
| PdxIny@N3-COF | 24.605 | 8.645 | Xe lamp (400 nm), Solid-liquid | 53 |

References

1.	Thompson, T. E. S. a. N. L. Total internal reflection with fluorescence correlation spectroscopy: combined surface reaction and solution diffusion. Biophys. J. 80, 1575-1584 (2001).

2.	Li, Z., Xiong, N., Gu, G. Fabrication of a full-spectrum-response Cu2(OH)2CO3/g-C3N4 heterojunction catalyst with outstanding photocatalytic H2O2 production performance via a self-sacrificial method. Dalton Trans. 48, 182-189 (2018).

3.	Yu, H., et al. CO2 bubble-assisted in-situ construction of mesoporous Co-doped Cu2(OH)2CO3 nanosheets as advanced electrodes towards fast and highly efficient electrochemical reduction of nitrate to N2 in wastewater. J. Hazard. Mater. 430, 128351 (2022).

4.	Liu, X., Cao, L., Sun, W., Zhou, Z., Yang, J. AP/N type compounded Cu2O/TiO2 photo-catalytic membrane for organic pollutant degradation. Res. Chem. Intermed. 42, 6289-6300 (2016).

5.	He, Z., Fu, J., Cheng, B., Yu, J., Cao, S. Cu2(OH)2CO3 clusters: novel noble-metal-free cocatalysts for efficient photocatalytic hydrogen production from water splitting. Appl. Catal. B 205, 104-111 (2017).

6.	S. Gonza´lez, M. P. r., M. Barrera, A. R. Gonza´lez Elipe, and R. M. Souto. Mechanism of copper passivation in aqueous sodium carbonate-bicarbonate solution derived from combined X-ray photoelectron spectroscopic and electrochemical data. J. Phys. Chem. B 102, 5483-5489 (1998).

7.	Toe, C. Y., Scott, J., Amal, R., Ng, Y. H. Recent advances in suppressing the photocorrosion of cuprous oxide for photocatalytic and photoelectrochemical energy conversion. J. Photoch. Photobio. C 40, 191-211 (2019).

8.	Zhonghai Zhang, R. D., Lianbin Zhang, Haibo Zhu, Hongnan Zhang, and Peng Wang. Carbon-layer-protected cuprous oxide nanowire arrays for efficient water reduction. ACS Nano 7, 1709-1717 (2013).

9.	Toe, C. Y., et al. Photocorrosion of cuprous oxide in hydrogen production: rationalising self-oxidation or self-reduction. Angew. Chem. Int. Ed. 57, 13613-13617 (2018).

10.	Xia, Y., et al. Improving artificial photosynthesis over carbon nitride by gas-liquid-solid interface management for full light-induced CO2 reduction to C1 and C2 fuels and O2. ChemSusChem 13, 1730-1734 (2020).

11.	Xie, S., et al. Photocatalytic and electrocatalytic transformations of C1 molecules involving C-C coupling. Energ. Environ. Sci. 14, 37-89 (2021).

12.	Albero, J., Peng, Y., García, H. Photocatalytic CO2 reduction to C2+ products. ACS Catal. 10, 5734-5749 (2020).

13.	Song, Y., Chen, W., Wei, W., Sun, Y. Advances in clean fuel ethanol production from electro-, photo- and photoelectro-catalytic CO2 reduction. Catalysts 10, 1287 (2020).

14.	Das, R., Das, K., Ray, B., Vinod, C. P., Peter, S. C. Green transformation of CO2 to ethanol using water and sunlight by the combined effect of naturally abundant red phosphorus and Bi2MoO6. Energ. Environ. Sci. 15, 1967-1976 (2022).

15.	Mao, J., et al. Effect of graphitic carbon nitride microstructures on the activity and selectivity of photocatalytic CO2 reduction under visible light. Catal. Sci. Technol. 3, 1253-1260 (2013).

16.	Liu, Y., et al. Selective ethanol formation from photocatalytic reduction of carbon dioxide in water with BiVO4 photocatalyst. Catal. Commun. 11, 210-213 (2009).

17.	Ola, O., Maroto-Valer, M. M. Transition metal oxide based TiO2 nanoparticles for visible light induced CO2 photoreduction. Appl. Catal. A 502, 114-121 (2015).

18.	Cheng, M., et al. Copper-decorated TiO2 nanorod thin films in optofluidic planar reactors for efficient photocatalytic reduction of CO2. Int. J. Hydrogen Energy 42, 9722-9732 (2017).

19.	Li, H., Gan, S., Wang, H., Han, D., Niu, L. Intercorrelated super hybrid of AgBr supported on engineering photocatalytic activities for water purification and CO2 reduction. Adv. Mater. 27, 6906-6913 (2015).

20.	Pastrana-Martínez, L., et al. Photocatalytic reduction of CO2 with water into methanol and ethanol using graphene derivative-TiO2 composites: effect of pH and copper (I) oxide. Top. Catal. 59, 1279-1291 (2016).

21.	Zhu, Y., et al. Grain boundary engineered metal nanowire cocatalysts for enhanced photocatalytic reduction of carbon dioxide. Appl. Catal. B 206, 282-292 (2017).

22.	Jeyalakshmi, V., Mahalakshmy, R., Krishnamurthy, K. R., Viswanathan, B. Photocatalytic reduction of carbon dioxide in alkaline medium on La modified sodium tantalate with different co-catalysts under UV-Visible radiation. Catal. Today 266, 160-167 (2016).

23.	Xia, X.-H., et al. Preparation of multi-walled carbon nanotube supported TiO2 and its photocatalytic activity in the reduction of CO2 with H2O. Carbon 45, 717-721 (2007).

24.	Hurtado, L., Natividad, R., García, H. Photocatalytic activity of Cu2O supported on multi layers graphene for CO2 reduction by water under batch and continuous flow. Catal. Commun. 84, 30-35 (2016).

25.	Han, Q., et al. Synthesis of single-crystalline, porous TaON microspheres toward visible-light photocatalytic conversion of CO2 into liquid hydrocarbon fuels. RSC Adv. 6, 90792-90796 (2016).

26.	Meng, A., Wu, S., Cheng, B., Yu, J., Xu, J. Hierarchical TiO2/Ni(OH)2 composite fibers with enhanced photocatalytic CO2 reduction performance. J. Mater. Chem. A 6, 4729-4736 (2018).

27.	Ola, O., Maroto-Valer, M. M. Role of catalyst carriers in CO2 photoreduction over nanocrystalline nickel loaded TiO2-based photocatalysts. J. Catal. 309, 300-308 (2014).

28.	Zou, J.-P., et al. A strategy for one-pot conversion of organic pollutants into useful hydrocarbons through coupling photodegradation of MB with photoreduction of CO2. ACS Catal. 6, 6861-6867 (2016).

29.	Abou Asi, M., et al. Photocatalytic reduction of CO2 to hydrocarbons using AgBr/TiO2 nanocomposites under visible light. Catal. Today 175, 256-263 (2011).

30.	He, Y., Wang, Y., Zhang, L., Teng, B., Fan, M. High-efficiency conversion of CO2 to fuel over ZnO/g-C3N4 photocatalyst. Appl. Catal. B 168, 1-8 (2015).

31.	He, Y., Zhang, L., Teng, B., Fan, M. New application of Z-scheme Ag3PO4/g-C3N4 composite in converting CO2 to fuel. Environ. Sci. Technol. 49, 649-656 (2015).

32.	Bai, S., et al. Two-dimensional g-C3N4: an ideal platform for examining facet selectivity of metal co-catalysts in photocatalysis. Chem. Commun. 50, 6094-6097 (2014).

33.	Vu, N.-N., Nguyen, C.-C., Kaliaguine, S., Do, T.-O. Reduced Cu/Pt-HCa2Ta3O10 perovskite nanosheets for sunlight-driven conversion of CO2 into valuable fuels. Adv. Sustainable Syst. 1, 1700048 (2017).

34.	Wang, A., Shen, S., Zhao, Y., Wu, W. Preparation and characterizations of BiVO4/reduced graphene oxide nanocomposites with higher visible light reduction activities. J. Colloid Interface Sci. 445, 330-336 (2015).

35.	Abou Asi, M., et al. Visible-light-harvesting reduction of CO2 to chemical fuels with plasmonic Ag@AgBr/CNT nanocomposites. Catal. Today 216, 268-275 (2013).

36.	Cai, B., et al. A distinctive red Ag/AgCl photocatalyst with efficient photocatalytic oxidative and reductive activities. J. Mater. Chem. A 2, 5280-5286 (2014).

37.	Jeyalakshmi, V., Mahalakshmy, R., Krishnamurthy, K. R., Viswanathan, B. Strontium titanates with perovskite structure as photo catalysts for reduction of CO2 by water: influence of co-doping with N, S & Fe. Catal. Today 300, 152-159 (2018).

38.	Tang, L., et al. ZnxCd1-xS tunable band structure-directing photocatalytic activity and selectivity of visible-light reduction of CO2 into liquid solar fuels. Nanotechnology 29, 064003 (2018).

39.	Peng, T., et al. Photo-driven selective CO2 reduction by H2O into ethanol over Pd/Mn-TiO2: suitable synergistic effect between Pd and Mn sites. Catal. Sci. Technol. 11, 2261-2272 (2021).

40.	Jeyalakshmi, V., et al. Sensitization of La modified NaTaO3 with cobalt tetra phenyl porphyrin for photo catalytic reduction of CO2 by water with UV-visible light. J. Mol. Catal. A: Chem. 420, 200-207 (2016).

41.	Wang, G., et al. Photoinduction of Cu single atoms decorated on UiO-66-NH2 for enhanced photocatalytic reduction of CO2 to liquid fuels. J. Am. Chem. Soc. 142, 19339-19345 (2020).

42.	Wang, Y., et al. Fabrication of trimodal porous silica/g-C3N4 nanotubes for efficient visible light photocatalytic reduction of CO2 to ethanol. Chem. Eng. J. 426, 130877 (2021).

43.	Xia, P., et al. Designing defective crystalline carbon nitride to enable selective CO2 photoreduction in the gas phase. Adv. Funct. Mater. 29, 1900093 (2019).

44.	Gao, S., et al. Creation of SnxNb1-xO2 solid solution through heavy Nb-doping in SnO2 to boost its photocatalytic CO2 reduction to C2+ products under simulated solar illumination. J. Adv. Ceram. 11, 1404-1416 (2022).

45.	Yu, H., Sun, C., Xuan, Y., Zhang, K., Chang, K. Full solar spectrum driven plasmonic-assisted efficient photocatalytic CO2 reduction to ethanol. Chem. Eng. J. 430, 132940 (2022).

46.	Bai, S., et al. Porous fixed-bed photoreactor for boosting C-C coupling in photocatalytic CO2 reduction. eScience 2, 428-437 (2022).

47.	Jia, Q., et al. Z-scheme heterostructure of Cu2O/Pt/NH2-MIL-125(Ti) for photocatalytic CO2 reduction. Mol. Catal. 530, 112599 (2022).

48.	Li, P., Liu, L., An, W., Wang, H., Cui, W. Efficient photothermal catalytic CO2 reduction to CH3CH2OH over Cu2O/g-C3N4 assisted by ionic liquids. Appl. Surf. Sci. 565, 150448 (2021).

49.	Li, P., et al. Ultrathin porous g-C3N4 nanosheets modified with AuCu alloy nanoparticles and C-C coupling photothermal catalytic reduction of CO to ethanol. Appl. Catal. B 266, 118618 (2020).

50.	Cai, J., Xiao, Y., Tursun, Y., Abulizi, A. Z-type heterojunction of Cu2O-modified layered BiOI composites with superior photocatalytic performance for CO2 reduction. Mater. Sci. Semicond. Process. 149, 106891 (2022).

51.	Seeharaj, P., Vittayakorn, N., Morris, J., Kim-Lohsoontorn, P. CeO2/CuO/TiO2 heterojunction photocatalysts for conversion of CO2 to ethanol. Nanotechnology 32, 375707 (2021).

52.	Shi, H., et al. Atomically dispersed indium-copper dual-metal active sites promoting C-C Coupling for CO2 photoreduction to ethanol. Angew. Chem. Int. Ed., e202208904 (2022).

53.	Huang, Y., et al. Filling COFs with bimetallic nanoclusters for CO2-to-alcohols conversion with H2O oxidation. Appl. Catal. B 288, 120001 (2021).