Table 1 | Reductive amination of 5-HMF with NH3 under different reaction conditions.

| Entry | Catalysts | Reductants | Time | HMF conversion | Products yields 1 |  |  |  | TOF 5 (h-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | A | B | C | D, E, F |  |
| 1 | Pd1/BNC | isopropanol | 6 h | ~100% | 96% | <1% | - | 2%, E 1368 |  |
| 2 | Pd1/BNC | formic acid 2 | 6 h | ~100% | 89% | 8% | - | 3%, E 1265 |  |
| 3 | Pd1/BNC | NaBH4 3 | 6 h | ~100% | 36% | 49% | - | 15%, D 512 |  |
| 4 | Pd1/BNC | None 4 | 6 h | 83% | - | - | 81% | 2%, F - |  |
| 5 | Pd1/NC | isopropanol | 6 h | ~100% | 67% | 17% | 7% | 2%, E 893 |  |
| 6 | BNC | isopropanol | 6 h | 35% | 3% | 1% | 29% | 2%, F - |  |
| 7 | 5% Pd/C | isopropanol | 6 h | ~100% | 71% | 25% | 1% | 3%, D 252 |  |
| 8 | None | isopropanol | 6 h | 7% | - | 1% | 6% | - - |  |
| Note 1: Determined by GC using the biphenyl as an internal standard, and the chemical structure of the reaction products were confirmed by GC-MS (The MS spectra of the products A-F could be found in Supplementary Fig. 11) Note 2: 5 mL formic acid as both reductant and solvent Note 3: 20 mM (757 mg) NaBH4 in 5 mL H2O Note 4: 5 mL tetrahydrofuran as solvent Note 5: TOF = mol of product A / mol of single atom sites / 6 h |  |  |  |  |  |  |  |  |  |

Table 2 | Scope of full-spectrum amines synthesized via reductive-amination with the catalysis of Pd1/BNC SAC.