Supporting Information

Linking Molecular Structure and Lubrication Mechanisms in Tetraalkylammonium Orthoborate Ionic Liquids

Jieming Yan1,2, Hsu-Ming Lien1,2, Filippo Mangolini1,3,*

- Texas Materials Institute, The University of Texas at Austin, Austin, TX 78712, USA

- Materials Science and Engineering Program, The University of Texas at Austin, Austin, TX 78712, USA

- Walker Department of Mechanical Engineering, The University of Texas at Austin, Austin, TX 78712, USA

*Corresponding Author: filippo.mangolini@austin.utexas.edu

Characterization of Tetraalkylammonium Orthoborate ILs

The characterization of the as-synthesized, dried ILs by nuclear magnetic resonance (NMR) spectroscopy (Bruker Avance 400 spectrometer) confirmed the molecular structure of both anions and cations. The characteristic 1H, 13C, and 11B are reported below for the three ILs prepared in this study. Notably, the 11B NMR spectrum always exhibited a single, strong signal that could be assigned to orthoborate anions, with minimal residual boric acid.

- Trimethyloctylammonium bis(oxalato)borate ([N1118][BOB]):

1H NMR (400 MHz, Acetone-d6): 3.61 – 3.52 (m, 2H), 3.36 (s, 9H), 2.01 – 1.88 (m, 2H), 1.41 (dq, J = 6.6, 3.7, 2.9 Hz, 4H), 1.33 – 1.24 (m, 6H), 0.88 (t, J = 6.7 Hz, 3H).

13C NMR (101 MHz, Acetone-d6): 158.41, 66.72, 52.82 (t, J = 0.4 Hz), 31.52, 26.03 (t, J = 0.1 Hz), 22.65, 22.33, 13.43.

11B NMR (128 MHz, Acetone-d6): 7.51.

- Triethylhexylammonium bis(oxalato)borate ([N2226][BOB]):

1H NMR (400 MHz, Acetone-d6): 3.38 (q, J = 7.3 Hz, 3H), 3.28 – 3.18 (m, 1H), 1.69 (dq, J = 12.0, 8.2, 7.6 Hz, 1H), 1.29 – 1.23 (m, 5H), 0.75 (t, J = 7.0 Hz, 1H).

13C NMR (126 MHz, Acetone-d6): 205.31, 158.35, 57.12 – 56.65 (m), 52.79 (t, J = 4.1 Hz), 31.00, 25.80 (d, J = 2.0 Hz), 22.14, 21.36, 13.22, 6.85.

11B NMR (128 MHz, Acetone-d6): 7.51.

- Trimethyloctylammonium bis(salicylato)borate ([N1118][BscB]):

1H NMR (400 MHz, Acetone-d6): 7.70 (dd, J = 7.8, 1.8 Hz, 1H), 7.25 (ddd, J = 8.6, 7.3, 1.9 Hz, 1H), 6.75 – 6.64 (m, 2H), 3.33 – 3.23 (m, 1H), 3.07 (s, 4H), 1.63 (dq, J = 14.0, 5.8, 5.0 Hz, 1H), 1.17 – 1.03 (m, 5H), 0.71 (t, J = 6.9 Hz, 1H).

13C NMR (126 MHz, Acetone-d6): 164.18, 159.91, 134.07, 129.44, 118.24, 118.09, 116.22, 66.65, 52.77, 52.74, 52.70, 31.52, 28.83, 26.02, 22.64, 22.33, 13.42.

11B NMR (160 MHz, Acetone-d6): 3.86.

The temperature-dependent viscosity of the three ILs is displayed in Figure S.2. Compared to the ILs with [BOB] anions, a significant increase in viscosity was observed in the case of the IL with [BScB] anion at all temperatures. The viscosity of the [N1118][BOB], [N2226][BOB], and [N1118][BScB] at 353 K (i.e., at the temperature at which tribological tests were performed) was 95±2 mPa s, 47±2 mPa s, and 635±17 mPa s, respectively.

KF titration measurements indicated high levels of water in all ILs, even after drying (e.g., 4.83% and 4.78% for [N1118][BOB] and [N2226][BOB], respectively). This can be attributed to the release of water from the direct reaction of orthoborate anions with methanol during KF titration as previously reported in Ref. [1]. The stoichiometric decomposition of [N1118][BOB] and [N2226][BOB] with methanol yields a water content of 5.02 wt.% and 4.83 wt.%, respectively, which is close to the values obtained with KF titration. In lieu of coulometric measurements, 1H NMR spectroscopy was used to estimate the water content of the as-synthesized orthoborate ILs, which was found to be 6732±335 ppm, 7988±395 ppm, and 504±25 ppm for [N1118][BOB], [N2226][BOB], and [N1118][BScB], respectively. The water uptake resulting from the exposure of the ILs to air for 1 hour at 353 K indicated a minimal (<10%) change in water content.

Figure 1. Schematic of the synthetic approach to prepare tetraalkylammonium orthoborate ionic liquids.

Figure 2. Viscosity as a function of temperature for tetraalkylammonium orthoborate ILs.

References

[1]	W. Larsson, J.C. Panitz, A. Cedergren, Interference-free coulometric titration of water in lithium bis(oxalato)borate using Karl Fischer reagents based on N-methylformamide, Talanta. 69 (2006) 276–280. https://doi.org/10.1016/J.TALANTA.2005.10.004.