Supporting information

Electrospun zein/polyvinyl alcohol nanofabrics incorporated with nanosized hydroxyapatite for efficient heavy metal ion adsorption

Na Ma1, Ke Li2, Bo Xu1,2*, Huafeng Tian2*, Songbai Ma3, Jinlong Li1, Yuge Ouyang2, Qian Liu2, Dagang Liu4*

1 Beijing Advanced Innovation Center for Food Nutrition and Human, Beijing Technology and Business University

2 Beijing Key Laboratory of Quality Evaluation Technology for Hygiene and Safety of Plastics, School of Chemistry and Materials Engineering, Beijing Technology and Business University

3 School of E-Business and Logistics, Beijing Technology and Business University

4 School of Environment Science & Engineering, Nanjing University of Information Science &Technology

*To whom correspondence should be addressed.

xubo@btbu.edu.cn (B Xu)

tianhuafeng@th.btbu.edu.cn (H Tian)

dagang@nuist.edu.cn (D Liu)

Fig. S1 Morphological studies on zein/PVA-based nanofibers with different contents of nHA.

Fig. S2 Diameter distribution curve of zein/PVA-based nanofibers with different content of nHA

Fig. S3 Water contact angle with different nHA of zein/PVA/ nHA nanofibrous films in different time

Fig. S4 SEM of the zein/PVA/nHA fibrous films after immersed in copper ions solution for 24 h.

Table S1 Copper adsorption capacity of nanofibrous films with different nHA content over time.

| Time/h | 0% |  | 4.7% |  | 11.1% |  | 15.8% |  | 20% |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | q(mg/g) | Removal rate(%) | q(mg/g) | Removal rate(%) | q(mg/g) | Removal rate(%) | q(mg/g) | Removal rate(%) | q(mg/g) | Removal rate(%) |  |
| 1 | 7.55 | 15.1 | 7.64 | 15.28 | 8.71 | 17.42 | 8.96 | 17.92 | 9.21 | 18.42 |
| 3 | 16.01 | 32.02 | 16.46 | 32.92 | 19.45 | 38.9 | 20.07 | 40.14 | 20.56 | 41.12 |
| 6 | 18.02 | 36.04 | 19.19 | 38.38 | 20.98 | 41.96 | 21.13 | 42.26 | 21.29 | 42.58 |
| 12 | 20.94 | 41.88 | 21.59 | 43.18 | 22.24 | 44.48 | 23.45 | 46.9 | 23.86 | 47.72 |
| 24 | 20.99 | 41.98 | 21.6 | 43.2 | 22.28 | 44.56 | 23.15 | 46.3 | 22.9 | 45.8 |