Table 1

Kinetic parameters for adsorption of 131I  using P1 and P2.

| Model | Linear Equation | Parameters | P1 | P2 |
| --- | --- | --- | --- | --- |
| Lagergren (PFO) |  | qe, exp. (mg/g) | 0.55 | 0.24 |
|  |  | qe, calc. (mg/g) | 2.91 | 2.20 |
|  |  | K1 (min-1) | 0.0034 | 0.0026 |
|  |  | R 2 | 0.958 | 0.946 |
| Ho and Mckay (PSO) |  | qe, exp. (mg/g) | 7.1 | 6.5 |
|  |  | qe, calc. (mg/g) | 7.6 | 6.9 |
|  |  | K2 (g/mg.min) | 0.0251 | 0.0359 |
|  |  | R 2 | 0.996 | 0.997 |
| Elovich |  | R 2 | 0.981 | 0.996 |
|  |  | β (g/mg) | 0.817 | 0.851 |
|  |  | (g/mg.min) | 0.422 | 0.448 |
| Weber- Morris |  | R 2 | 0.982 | 0.982 |
|  |  | KW&M (mg/g.min1/2) | 1.42 | 1.47 |
|  |  | C (mg/g) | 0.828 | 1.119 |

Table2

Isotherm parameters for Redlich-Peterson, Langmuir, Freundlich and Harkins-jura for adsorption 131I using

| Model | Parameter | P1 | P2 |
| --- | --- | --- | --- |
|  | qmax, exp | 58.5 | 67.9 |
| Redlich-Peterson | R2 | 0.97 | 0.98 |
|  | g | 0.46 | 0.49 |
|  | a | 1.05 | 1.49 |
| Langmuir | R2 | 0.94 | 0.95 |
|  | KL | 0.03 | 0.05 |
|  | qm, calc | 49.19 | 58.99 |
|  | RL | 0.53 | 0.42 |
| Freundlish | R2 | 0.98 | 0.99 |
|  | KF | 0.53 | 0.77 |
|  | n | 0.94 | 1.28 |
| Harkin-Jura | R2 | 0.98 | 0.98 |
|  | A | 56.4 | 67.2 |
|  | B | 462.5 | 683.2 |

Table 3

Comparison data for the sorption capacity of 131I using various sorbents.7

| Sorbents | pH | Capacity mg/g | References |
| --- | --- | --- | --- |
| poly (sodium alginate-acrylic acid) | 3 | 58.5 | Present work |
| poly (sodium alginate-acrylic acid-methacrylic acid) | 3 | 67.9 | Present work |
| Alum industrial iste | 4 | 9.44 | [26] |
| Chabazite N-methylene aniline | 3 | 35.4 | [27] |
| Tri(octyl-decyl)amin-modified Biomass Carbonaceous Arogel | 2 | 6.9 | [28] |
| 1.0% Ag @ Cu2O | 7 | 25.4 | [29] |
| Dried powder of corn stalk | NRa | 0.114 | [30] |
| Dried duckweed powder | NR | 0.228 | [31] |
| Nanostructured MgFe and CoCr layered double hydroxides | 5 | 19.7 | [32] |

aNR not reported

Table 4

Effect of sorbent weight on the removal percent and decontamination factor of 131I.using P1 and P2.

| Sorbent weight | P1 |  |  | P2 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | R % | DF | Kd | R % | DF | Kd |
| 0.012 | 32.99 | 1.49 | 49.24 | 38.56 | 1.62 | 62.77 |
| 0.025 | 65.14 | 2.86 | 186.86 | 69.77 | 3.30 | 230.86 |
| 0.05 | 77.80 | 4.50 | 350.45 | 84.30 | 6.37 | 537.00 |
| 0.075 | 84.01 | 6.25 | 525.63 | 88.35 | 8.58 | 758.99 |
| 0.1 | 89.64 | 9.65 | 865.77 | 93.26 | 14.84 | 1384.28 |
| 0.125 | 93.04 | 14.37 | 1337.35 | 96.57 | 29.15 | 2815.67 |
| 0.15 | 94.90 | 19.64 | 1864.00 | 97.73 | 44.15 | 4315.46 |
| 0.2 | 96.32 | 27.21 | 2621.72 | 98.74 | 79.70 | 7870.77 |

Table 5:

Test results showing prepared polymers decontamination factor for different radio nuclides.

| ion | Ao | Ae | %R | DF |
| --- | --- | --- | --- | --- |
| I- | 47825 | 2016 | 95.78463 | 23.72272 |
| Ce+3 | 4851 | 173 | 96.43373 | 28.04046 |
| Eu+3 | 9875 | 295 | 97.01266 | 33.47458 |
| Co+2 | 6734 | 545 | 91.90674 | 12.35596 |