Supporting information for

Efficient Preparation of Nanoparticles Reinforced Nickel-based Composite Coating with Highly Preferred (220) Orientation

Renjie Ji1†, Hui Jin1†, Yonghong Liu1,2*, Tiancong Dong1, Fan Zhang1, Lilong Zhao1, Xinlei Wu1, Qiang Sun1, Peng Liu1, Hang Dong1, Chi Ma1, Dege Li1, Baoping Cai1

1College of Mechanical and Electronic Engineering, China University of Petroleum (East China), Qingdao, Shandong, 266580, PR China.

2Key Laboratory of Unconventional Oil & Gas Development, China University of Petroleum (East China), Ministry of Education, Qingdao PR China.

*Corresponding author. Email: liuyhupc@163.com (Yonghong Liu)

†These authors contributed equally to this work and should be considered as the co-first authors.

Experimental section

All reagent (AR) are purchased from Sinopharm chemical Reagent Co. Ltd. without further purification. The Ni-SiC nanoparticles, TiO2 nanoparticles and Al2O3 nanoparticles are are purchased from Aladdin chemical Reagent Co. Ltd. Nickel balls and pure titanium rod are purchased from BeiLong metal material Co. Ltd. Deionized water (resistance of 18.2MΩ) are used in all experiments. In the experiment, the purity of SiC nanoparticles is 99.99% and the average particle size is about 50 nm. The morphology and composition are shown in Figure S1.

Figure S1. The morphology and composition of SiC nanoparticles: (a) SEM image, (b) enlarged image, (c) EDS map of Si element, (d) EDS map of C element.

The pure Ni coating, Ni-TiO2 coating and Ni-Al2O3 coating prepared by JED.

In order to explore the effect of nanoparticles in the preparation of nickel-based composite coatings with highly preferred (220) orientation, the pure Ni coating (Figure S2-S3)、Ni-TiO2 composite coating (Figure S4-S5) and Ni-Al2O3 composite coating (Figure S6-S7) are also prepared by JED. The deposition current density is 220 A/dm2 and the injection velocity is 1.76 m/s. The results show that all of the three coatings are all highly preferred (220) orientation structure, which shows that nanoparticles have little effect on the orientation of the grains in the coating.

Figure S2. The XRD pattern of the pure Ni coating prepared by JED.

Figure S3. The EDS spectrum of the pure Ni coating prepared by JED.

Figure S4. The XRD pattern of the Ni-TiO2 composite coating prepared by JED.

Figure S5. The EDS spectrum of the Ni-TiO2 composite coating prepared by JED.

Figure S4. The XRD pattern of the Ni-Al2O3 composite coating prepared by JED.

Figure S4. The EDS spectrum of the Ni-Al2O3 composite coating prepared by JED.

Conventional electrodeposition experiment

In this paper, the Ni-SiC composite coating is prepared by conventional electrodeposition (CED) and compared with the Ni-SiC composite coatings prepared by JED. The schematic diagram of experimental device for CED is shown in Figure S8. The composition of plating solution and experimental parameters is shown in Table S1. The XRD pattern of the Ni-SiC composite coating prepared by CED is shown in Figure S9, which indicates that the Ni-SiC composite coating without highly preferred (220) orientation.

Figure S8. Schematic diagram of experimental device for CED

Table S1. The composition of plating solution and experimental parameters.

| Composition and parameters | Quantity |
| --- | --- |
| NiSO4·6H2O (g/L) | 300 |
| NiCl2·6H2O (g/L) | 40 |
| H3BO4 (g/L) | 40 |
| Saccharin (g/L) | 0.5 |
| Emulsifier OP-10 (g/L) | 1.0 |
| SiC nano-particles (g/L) | 3.0 |
| pH value | 4.0 |
| Distance between anode and cathode (mm) | 100 |
| Stirring speed (rpm) | 150 |
| Current density (A/dm2) | 8 |
| Temperature (℃) | 60 |
| Deposition time (min) | 45 |

Figure S9. The XRD pattern of the Ni-SiC composite coating prepared by CED.

Full immersion corrosion tests

The full immersion corrosion tests of Ni-SiC composite coatings are carried out. The corrosion solution was 3.5 wt% NaCl solution, and the corrosion time was 1 day, 3 days, 5 days and 10 days, respectively. The surface of the coatings after immersion corrosion are observed, and the surface morphologies of different corrosion times are shown in Figure S10-S12 and Figure 7.

Figure S10 The surface morphologies of different Ni-SiC composite coatings after 1 day of immersion corrosion in 3.5 wt% NaCl solution: (a) CED (8 A/dm2), (b) JED (180 A/dm2), (c) JED (190 A/dm2), (d) JED (200 A/dm2), (e) JED (210 A/dm2), (f) JED (220 A/dm2).

Figure S11 The surface morphologies of different Ni-SiC composite coatings after 3 days of immersion corrosion in 3.5 wt% NaCl solution: (a) CED (8 A/dm2), (b) JED (180 A/dm2), (c) JED (190 A/dm2), (d) JED (200 A/dm2), (e) JED (210 A/dm2), (f) JED (220 A/dm2).

Figure S12 The surface morphologies of different Ni-SiC composite coatings after 5 days of immersion corrosion in 3.5 wt% NaCl solution: (a) CED (8 A/dm2), (b) JED (180 A/dm2), (c) JED (190 A/dm2), (d) JED (200 A/dm2), (e) JED (210 A/dm2), (f) JED (220 A/dm2).

Substrate

The substrate material is medium carbon steel. Before the experiment, the substrate is pretreated. The process is as follows: fine grinding - oil removal - acetone ultrasonic cleaning - alcohol ultrasonic cleaning - deionized water ultrasonic cleaning - drying. The EDS spectrum of the substrate is shown in Figure S13, and the XRD pattern of the substrate is shown in Figure S14.

Figure S13. The EDS spectrum of the substrate.

Figure S14. The XRD pattern of the substrate.

DFT calculations

Our DFT calculations were performed by the projector augmented wave method (PAW) as implemented in VASP with the exchange-correlation potentials described by the generalized gradient approximation (GGA) parameterized by Perdew-Burke-Ernzerhof (PBE). The energy cut-off was set as 500 eV and the total energy and forces were set as 10−5 eV/atom and 10−2 eV/Å. Periodic slab models were used to simulate the interfaces by using a finite number of layers of atoms to represent the semi-infinite bulk phase, and these slabs were separated 10 Å vacuum to minimize the inter-slab interactions. The lattice strain can be calculated by the Formula (S1), where and are the lattice parameters after and before deformation, and is lattice strain. The interface mismatch can be calculated by the Formula (S2), where is the overlap area of unit cell with the matche cell areas of and . The ideal work of adhesion can be calculated by the Formula (3), where and are the total energies of isolated slab1 and slab2, the total energy of the interface system including slab1 and slab2, and the interface area. The calculated results are shown in Table S2.

(S1)

(S2)

(3)

Table S2. calculated results of DET calculations.

| Interface |  |  |  |
| --- | --- | --- | --- |
| Ni(220)/Fe(110) | (3.4%,0.7%) | 1.4% | 4.21 |
| Ni(111)/Fe(110) | (3.4%,1.4%) | 1.0% | 3.32 |
| Ni(200)/Fe(110) | (3.4%,0.4%) | 1.9% | 3.96 |