Supplementary materials

Long-term effective remediation of black-odorous water via regulating calcium nitrate sustained-release

Rui Wan 1*, Yunyi Zha 1, Mengqi Wu 1, Xiaoxiao Li 1, 2, Haifeng Yang 3, Hongming Liu 4

(1 School of Ecology and Environment, Anhui Normal University, Wuhu, 241002, China; 2 College of Environment, Hohai University, Nanjing 210098, China, 3 Anhui Phoneya Environmental Technology Co. Ltd., Donghu Innovation Center, Hefei, 230601, China; 4 College of Life Sciences, Anhui Normal University, Wuhu, 241001, China)

*Corresponding author

Tel: +86-553-5910724

E-mail: wanrui910@163.com

Number of pages: 5

Number of tables: 5

Number of figures: 4

Supplementary methods

Morphology of the concretes

The morphological difference was observed using scanning electron microscope (SEM). After long-term experiment, the concrete blocks in the NC and EC group were collected. Immediately, the collected concrete blocks were rinsed with saline solution (0.9%) gently for twice. Subsequently, the concrete blocks were submerged into the Phosphate Buffered Saline (PBS, 10mM, 7.00) containing 2.5% glutaraldehyde at 4oC overnight. After washing away the glutaraldehyde using PBS (10mM, 7.00), the blocks were sequentially dehydrated in the ethanol serials (50%, 70%, 80%, 90%, and 100%) 15 min per step, and dried in air at room temperature. Then, the blocks’ observation was performed using a scanning electron microscope (SEM, JSM-6701F, JEOL, Ltd.)

Supplementary Figures

Figure S1  The schematic graph of experimental protocol.

Figure S2  Effect of Eco-concrete on black-odorous water treatment performance. Evolution of DO (A) and ORP (B).

Figure S3  The final removal efficiency of COD (A), NH4+-N (B), and turbidity (C) of the black-odorous water treated by concrete and ecoN-concrete at each cycle.

Figure S4  Phylogenetic relationships of the detected samples at genus level.