Electronic supplemental material

Silica nanoparticles induce pulmonary damage in rats via VEGFC/D–VEGFR3 signaling-mediated lymphangiogenesis and remodeling

Yanan Yu1, Yujie Pan1, Bing Chang2, Xiaoxu Zhao1, Kunlong Qu1, Yuguo Song1,*

1. Department of Occupational Medicine and Clinical Toxicology, Beijing Chaoyang Hospital, Capital Medical University, Beijing 100020, China.

2. National Institute for Occupational Health and Poison Control, Chinese Center for Disease Control and Prevention, Beijing, 100050, China.

* Corresponding author: Yuguo Song

Department of Occupational Medicine and Clinical Toxicology, Beijing Chaoyang Hospital, Capital Medical University, 8 Worker’s Stadium South Road, Chaoyang District, Beijing 100020, China, Tel: +86 13301176123; E-mail: songrain123@hotmail.com

Table S1. Summary statistical report of particle size measurement.

| NO. | Eff. Diam. (nm) | Polydispersity | Baseline Index | Count Rate (kcps) | Data Retained (%) | Diffusion Coeff. (cm²/s) |
| --- | --- | --- | --- | --- | --- | --- |
| TEST 1 | 135.66 | 0.122 | 9.6 | 468.0 | 98.11 | 3.617 × 10−8 |
| TEST 2 | 133.42 | 0.096 | 8.4 | 465.6 | 94.42 | 3.678 × 10−8 |
| TEST 3 | 136.18 | 0.123 | 9.7 | 472.6 | 100.00 | 3.604 × 10−8 |
| Mean | 135.09 | 0.114 | 9.3 | 468.7 | 97.51 | 3.633 × 10−8 |

Table S2. Summary statistical report of zeta potential

| NO. | Zeta Potential (mV) | Mobility (μ/s)/(V/cm) | Conductance (μS) | Sample Count Rate (kcps) | Ref. Count Rate (kcps) | RMS Residual |
| --- | --- | --- | --- | --- | --- | --- |
| TEST 1 | -55.74 | -2.90 | 305 | 818 | 1,560 | 3.2501 × 10−2 |
| TEST 2 | -53.64 | -2.79 | 306 | 818 | 1,560 | 3.3039 × 10−2 |
| TEST 3 | -58.52 | -3.05 | 306 | 818 | 1,560 | 5.1005 × 10−2 |
| Mean | -55.96 | -2.92 | 306 | 818 | 1,560 | 3.8849 × 10−2 |