Tables lists

Table 1. Characteristic of the woven reinforcement

| Reinforcement architecture | canvas |
| --- | --- |
| Mass of the woven (g) | 21 ± 5 % |
| Count warp | 6 |
| Count welft | 2 |
| Linear density of the fiber (tex) | 255 ± 20 % |

Table 2. Measured geometric dimensions for the elemental cell of the woven fabric.

| Welft spacing/ warp (mm) | 0.1 |
| --- | --- |
| Welft spacing (mm) | 4 |
| Woven tickness (mm) | 1.45 |
| Unit cell total lenght (without welft) (mm) | 10 |
| Unit cell total width (mm) | 3.84 |
| Unit cell volume (mm3) | 55.68 |

Table 3: Density, absorption rate [29] and diffusion coefficient [30] of some wood species used in shipbuilding.

| woods | Acajous | Ayous | Azobé | Doussié | Iroko | Makoré | Moabi | Okoumé | Sapelli | Sipo |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Density (g/cm3) | 0.57 | 0.38 | 1.06 | 0.8 | 0.64 | 0.69 | 0.87 | 0.44 | 0.69 | 0.62 |
| Absorption rate (%) | 28 | 29 | 28 | 19 | 23 | 28 | 23 | 40 | 29 | 30 |
| Humidity (m2/s) at 40oC |  | 2,231*10-10 | 2,64 *10-14 |  | 4,67 *10-12 |  |  |  | 6,45 *10-12 | 3,82 *10-12 |

Table 4: Summary of thermal transfer values

|  | Effusivity (J/m^2Ks^1/2) | Heat capacity (J/m^3K) | Conductivity (W/m k) | Diffusivity (m^2/s) |
| --- | --- | --- | --- | --- |
| Sample 1 | 229.4206 | 183319.468 | 0.28712 | 1.57E-06 |
| Sample 2 | 335.3168 | 306898.591 | 0.36637 | 1.19E-06 |
| Sample 3 | 231.7 | 183321.011 | 0.28534 | 1.55E-06 |
| Sample 4 | 314.8692 | 260846.826 | 0.38008 | 1.46E-06 |
| Sample 5 | 331.0156 | 216582.166 | 0.31555 | 1.51E-06 |
| Average | 288.46444 | 230193.612 | 0.326892 | 1.46E-06 |
| Standard deviation | 53.4119202 | 53391.8791 | 0.04422809 | 1.51911E-07 |

Table 5:  comparison between the model by the FEM and the experimental.

| Experimental (W/m2) | Simulation (W/m2) | Relative Error (%) |
| --- | --- | --- |
| 90925 | 85847.56 | 5.58 |