Supporting Information

Cs3Cu2I5 Single Crystal for Efficient Direct X-ray Detection

Qinhua Weia§, Xiongsheng Fanb,c§, Peng Xianga, Laishun Qina*, Wenjun Liub, Tongyu Shib, Hang Yina,d, Peiqing Caic, Yufeng Tonga, Gao Tanga, Zugang Liuc, Paul K. Chuf, Hongsheng Shie*, Yanliang Liu b* and Xue-Feng Yu b*

a College of Materials and Chemistry, China Jiliang University, Hangzhou 310018, China

b Shenzhen Institute of Advanced Technology, Chinese Academy of Sciences, Shenzhen 518055, Guangdong, China

c College of Optical and Electronic Technology, China Jiliang University, Hangzhou 310018, China

d State Key Laboratory of Molecular Reaction Dynamics, Dalian Institute of Chemical Physics, Chinese Academy of Science, Dalian 116023, China.

e Xinjiang Technical Institute of Physics and Chemistry, Chinese Academy of Sciences, Urumqi 830011

f Department of Physics, Department of Materials Science and Engineering, and Department of Biomedical Engineering, City University of Hong Kong, Tat Chee Avenue, Kowloon, Hong Kong, China

§ These authors contributed equally to this work.

* Corresponding authors: Emails: qinlaishun@cjlu.edu.cn (Laishun Qin); shs1975@126.com (Hongsheng Shi); xf.yu@siat.ac.cn (Xue-Feng Yu), yl.liu4@siat.ac.cn (Yanliang Liu)

Figure S1. XPS survey spectrum of Cs3Cu2I5 crystal.

Figure S2. The current response upon X-ray on/off for the (a) Cs3Cu2I5 and (b) Cs3Cu2I5:Li detectors at different electric fields and various X-ray dose rates

Figure S3. The X-ray on/off experiments of the (a) Cs3Cu2I5 and (b) Cs3Cu2I5:Li detectors under 45 V/mm external electric field and 1579 μGyair s−1 X-ray dose for 3600 s

Figure S4. The temporal baseline tracking of the (a) Cs3Cu2I5 and (b) Cs3Cu2I5:Li detectors

Table S1. Characteristic parameters of various direct perovskite detectors.

| Materials | μτ product (cm2 V-1) | Sensitivity (μC Gy-1cm-2) | Detection limit (nGys-1) | Resistivity (Ω cm) | Ref |
| --- | --- | --- | --- | --- | --- |
| MAPbBr3 crystal | 1. 2×10-2 | 80 | 500 | 1. 7×107 | [1] |
| CsPbBr3 crystal | 2. 5×10-3 | 1256 |  | 7. 85×109 | [2] |
| Cs2AgBiBr6 crystal | 6. 3×10-3 | 105 | 59.7 | 1. 6×1011 | [3] |
| Cs3Bi2I9 crystal | 7. 97×10-4 | 1652.3 | 130 | 2. 79×1010 | [4] |
| Rb3Bi2I9 crystal | 2. 51×10-3 | 159.7 | 8.32 | 2. 3×1011 | [5] |
| MA3Bi2I9 | 2. 87×10-3 | 1947 | 83 | 3.74×1010 | [6] |
| Cs3Cu2I5 crystal | 1.4×10-4 | 441.5 | 335.1 | 4.3×1011 | This work |
| Cs3Cu2I5:Li crystal | 2.9×10-4 | 831.1 | 34.8 | 2.7×1010 | This work |

References

[1] Wei, H.; Fang, Y.; Mulligan, P.; Chuirazzi, W.; Fang, H.-H.;Wang, C.; Ecker, B. R.; Gao, Y.; Loi, M. A.; Cao, L.; et al. Sensitive X-Ray Detectors Made of Methylammonium Lead Tribromide Perovskite Single Crystals. Nat. Photonics 2016, 10, 333-339.

[2] Zhang, H.; Wang, F.; Lu, Y.; Sun, Q.; Xu, Y.; Zhang, B.-B.; Jie, W.; Kanatzidis, M. G. High-Sensitivity X-Ray Detectors Based on Solution-Grown Caesium Lead Bromide Single Crystals. J. Mater. Chem. C 2020, 8, 1248-1256.

[3] Pan, W.; Wu, H.; Luo, J.; Deng, Z.; Ge, C.; Chen, C.; Jiang, X.; Yin, W.-J.; Niu, G.; Zhu, L.; et al. Cs2AgBiBr6 Single-Crystal X-Ray Detectors with a Low Detection Limit. Nat. Photonics 2017, 11, 726-732

[4] Zhang, Y.; Liu, Y.; Xu, Z.; Ye, H.; Yang, Z.; You, J.; Liu, M.; He, Y.; Kanatzidis, M. G.; Liu, S. Nucleation-Controlled Growth of Superior Lead-Free Perovskite Cs3Bi2I9 Single-Crystals for HighPerformance X-Ray Detection. Nat. Commun. 2020, 11, 2304.

[5] Xia M L，Yuan J H，Niu G D，et al. Unveiling the structural descriptor of A3B2X9 perovskite derivatives toward X-ray detectors with low detection limit and high stability［J］. Adv. Funct. Mater., 2020，30（24）：1910648-1-8.

[6] Liu, Y.; Xu, Z.; Yang, Z.; Zhang, Y.; Cui, J.; He, Y.; Ye, H.; Zhao, K.; Sun, H.; Lu, R.; et al. Inch-Size 0D-Structured Lead-Free Perovskite Single Crystals for Highly Sensitive Stable X-Ray Imaging. Matter 2020, 3, 180-196