Supplementary Information

#### Solvent polarity induces significant bathochromic shift on (4Z,4'Z)-4,4'-(((phenylazanediyl) bis (4,1-phenylene)) bis (methaneylylidene)) bis (2-phenyloxazol-5(4H)-one)

#### Maheswar Reddy Gowri, Madhav Ranganathan, and Gurunath Ramanathan*

#### Department of Chemistry, Indian Institute of Technology Kanpur, Kanpur, 208016, India

#### *Corresponding author; Email: gurunath@iitk.ac.in

Content details

| S. No. | Data | Details | P. No. |
| --- | --- | --- | --- |
| 1 | Scheme S1 | General experimental details synthesis and scheme of PPMP. | 2 |
| 2 | Figure. S1 | 1H NMR spectrum of PPMP…………………………………. | 3 |
| 3 | Figure. S2 | 13C NMR spectrum of PPMP………………………………… | 3 |
| 4 | Figure. S3 | ESI-MS of PPMP……………………………………………... | 4 |
| 5 | Figure. S4 | The optimized structure and atom labels of PPMP………….. | 4 |
| 6 | Table. S1 | Solvent parameters are shown as dielectric constant (ɛ), refractive index (n), solvent polarity functions Lippert-Mataga (f1 (ɛ,n)), Bakhshiev (f2 (ɛ,n)), Bilot-Kawski (f3 (ɛ,n)), and Reichardt parameterETN…………………………………………. | 5 |
| 7 | Theory’s | Bilot-Kawski, Lippert-Mataga, Bakhshiev & Reichardt methods | 5-6 |
| 8 | Gaussian input file | Gaussian Input File for calculation of ground-state dipole moment…………………………………………………………. | 7-10 |

1. Synthesis of (4Z, 4ʹZ)-4, 4ʹ-(((phenylazanediyl) bis (4,1-phenylene)) bis (methanylylidene)) bis (2-phenyloxazol-5(4H)-one).

A mixture of 4,4'-(phenylazanediyl) dibenzaldehyde (2.0 g, 1 eq.), N-benzoyl glycine (2.3 g, 2 eq.), anhydrous sodium acetate (1.0 g, 2 eq.), and acetic anhydride (6.2 mL, 10 eq.) was refluxed for 6 hrs at 140 °C. After that, the reaction mixture was left at room temperature, further diluted with ethanol (10 ml), and kept at 0 °C for 20 minutes; the residue was obtained. The deposited solid was filtered under a borosilicate Buchner funnel, washed with ice-cold ethanol, and distilled hot water. The crude compound was dried under reduced pressure and purified by column chromatography (100-200 mesh) with chloroform as an eluent to get the pure compound. The isolated yield: 1.8 g (46%); m.p 220 °C - 222 °C; Rf = 0.4 (30% chloroform): 1H NMR (500 MHz, CDCl3) 8.15 (d, J = 8.8 Hz, 8H), 7.58 (t, J = 7.4 Hz, 2H), 7.51 (t, J = 7.7 Hz, 4H), 7.43 – 7.37 (m, 2H), 7.25 – 7.12 (m, 9H). 13C NMR (125 MHz, CDCl3) 167.99, 162.80, 149.41, 145.84, 134.08, 133.20, 131.81, 131.27, 130.10, 129.05, 128.52, 128.31, 127.03, 125.98, 125.94, 123.21. FT- IR cm-1: 3059, 1768, 1646, 1600-1514. ESI-MS: m/z calculated for C38H25N3O4 [M+H]+ 588.1923 found 588.1918

Scheme-1 Synthesis of PPMP

Figure.S1: 1H NMR spectrum of (4Z, 4ʹZ)-4, 4ʹ-(((phenylazanediyl) bis (4, 1-phenylene)) bis (methanylylidene)) bis (2-phenyloxazol-5(4H)-one) (PPMP).

Figure.S2: 13C NMR spectrum of (4Z, 4ʹZ)-4, 4ʹ-(((phenylazanediyl) bis (4, 1-phenylene)) bis (methanylylidene)) bis (2-phenyloxazol-5(4H)-one) (PPMP).

Figure.S3: ESI-MS of (4Z, 4ʹZ)-4, 4ʹ-(((phenylazanediyl) bis (4, 1-phenylene)) bis  (methanylylidene))bis (2-phenyloxazol-5(4H)-one) (PPMP).

Figure S4: The optimized structure and atom labels of PPMP.

5. Table S1: Solvent parameters are shown as Lippert-Mataga (f1 (ɛ,n)), Bakhshiev (f2  (ɛ,n)), Bilot-Kawski   (f3  (ɛ,n)) and Reichardt parameter (ETN).

| S.No | Solvent | f1 (ɛ,n) | f2 (ɛ,n) | f3 (ɛ,n) | ETN | ν(a)- ν(f) | ν(a)+ν(f) | ν(a)+ν(f)/2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Hexane | 0.0003 | 0.0004 | 0.2550 | 0.00 | 599 | 39969 | 19985 |
| 2 | Cyclo hexane | -0.0016 | -0.0033 | 0.2876 | 0.006 | 467 | 39453 | 19727 |
| 3 | Toluene | 0.0132 | 0.0291 | 0.3499 | 0.099 | 1858 | 38222 | 19111 |
| 4 | 1,4 Dioxane | 0.0205 | 0.0415 | 0.3074 | 0.164 | 1313 | 38213 | 19107 |
| 5 | Diethyl ether | 0.1625 | 0.3645 | 0.4222 | 0.117 | 1562 | 38599 | 19299 |
| 6 | Chloroform | 0.1504 | 0.3774 | 0.4909 | 0.259 | 1825 | 37161 | 18581 |
| 7 | Ethylacetate | 0.2007 | 0.4925 | 0.4996 | 0.228 | 2567 | 37593 | 18797 |
| 8 | Tetrahydrofuran | 0.2096 | 0.5491 | 0.5511 | 0.207 | 2529 | 37312 | 18656 |
| 9 | Dichloromethane | 0.2171 | 0.5903 | 0.5830 | 0.309 | 2697 | 36596 | 18298 |
| 10 | 1-Butanol | 0.2635 | 0.7504 | 0.6466 | 0.586 | 2717 | 36731 | 18365 |
| 11 | Acetone | 0.305 | 0.7904 | 0.6392 | 0.355 | 3913 | 36328 | 18164 |
| 12 | Ethanol | 0.2887 | 0.8129 | 0.6525 | 0.654 | 3414 | 36747 | 18373 |
| 13 | Acetonitrile | 0.3046 | 0.8593 | 0.6640 | 0.460 | 4422 | 35819 | 17910 |
| 14 | Dimethylformamide | 0.275 | 0.839 | 1.037 | 0.39 | 4133 | 35629 | 17814 |
| 15 | Dimethylsulphoxide | 0.263 | 0.842 | 1.105 | 0.44 | 4235 | 35291 | 17645 |

6. Estimating ground (μg) and excited (μe) state dipole moment from the solvatochromic analysis.

(a). Bilot and Kawski

From the solvatochromic analysis, estimation of μg and μe were proposed by Bilot and Kawski using Onsager reaction field theory by varying dielectric constant (ɛ) and refractive index (n). According to this method, the difference and sum of absorption and fluorescence maxima can be expressed by the following two independent equations

νa-νf = mB-K (1) f(ɛ,n) + (constant)                                                                                            (S1)

νa+νf = -mB-K (2) [f(ɛ,n) + 2g(n)]  + (constant)                                                                       (S2)

Where mB-K (1) and -mB-K (2) are slopes in equations (S1) and (S2), respectively. (B-K means Bilot–Kawski), ε and n are the dielectric constant and refractive index of the solvent

fε,n=2n2+1n2+2 ɛ-1 ɛ+2-n2-1n2+2                                                                                                  (S3)

gn=3n4-12n2+22                                                                                                                    (S4)

μg=mB-K(2)-mB-K(1)2hca32mB-K(1)12                                                                                                           (S5)

μe=mB-K(2)+mB-K(1)2hca32mB-K(1)12                                                                                                          (S6)

(b). Lippert–Mataga, Bilot–Kawski (modified), and Bakhshiev methods

Lippert–Mataga, Bilot–Kawski (modified), and Bakhshiev expressed derivations using solvatochromic methods to determine the excited state

νa-νf = m1f1(ɛ,n) + (constant)                                                                                                   (S7)

νa-νf = m2f2(ɛ,n) + (constant)                                                                                                   (S8)

νa+νf / 2 = -m3f3(ɛ,n) + (constant)                                                                                           (S9)

Where,

m1= 2(μe-μg)2 / hca3                                                                                                             (S10)

m2= 2(μe-μg)2 / hca3                                                                                                             (S11)

m3= 2(μe-μg)2 / hca3                                                                                                             (S12) Where νa is the energy of the absorbance maximum in wavenumber, νf is the energy of the emission maximum in wavenumber, h is Planck constant (6.626 x 10-34 J.S), c is the speed of light (3 x 108 m/s), and a is the Onsager cavity radius 6.44 Å. f1, f2, and f3 are solvent polarity functions of Lippert–Mataga, Bakhshiev, and Bilot–Kawski, respectively, and given as

f1ε,n=ɛ-12ɛ+1-n2-12n2+1                                                                                                       (S13)

f2ε,n=2n2+1n2+2 ɛ-1 ɛ+2-n2-1n2+2                                                                                              (S14)

f3ε,n=2n2+12n2+2 ɛ-1 ɛ+2-n2-1n2+2+3n4-12n2+22                                                                     (S15)

(c). Molecular-microscopic solvent polarity parameter (ETN)

Reichardt expressed derivation to estimate μe using ETN solvent parameter

ETN=ET solvent-ET TMSET water-ET TMS=ET solvent-30.732.4                                                                          (S16)

νa-νf=mETNETN+ (constant)                                                                                               (S17)

Where mETN slope obtained from stokes shift versus ETN  from equation (S17)

μe-μg=mETN×8111307.6×6.2/a3                                                                                                (S18)

7. Gaussian Input File

The optimization of the geometry of PPMP in their ground state was carried out in vacuo using the Gaussian 09 program package and the B3LYP functional in conjunction with the 6-31G(d) basis set.

O                 12.52890700   10.19481800    9.14035700

O                 -3.26439700   10.23644100   15.77529400

O                 -2.69292800   12.34897200   15.18415700

O                 11.98848500   12.28624600    9.82634800

N                  4.53362000    8.44412000   12.20595900

N                 -1.45953100    9.07040700   15.04940900

N                 10.60230800    9.07834400    9.56728000

C                  1.83393100   10.94539400   12.70124900

H                  1.61503600   11.80544800   12.42304600

C                  3.36899300    9.08395800   12.66748000

C                  2.97167200   10.34427500   12.19900700

H                  3.47583400   10.77692500   11.54821000

C                  7.73708900    9.03284900   10.48105100

H                  8.31638000    8.55886500    9.92896500

C                  1.38200700    9.01155300   14.04939300

H                  0.83762100    8.54674600   14.64324400

C                  6.01078100   10.40932300   12.16656100

H                  5.44426100   10.86799400   12.74407400

C                  7.17669700   11.00850600   11.72126300

H                  7.36263500   11.88282900   11.97826100

C                  1.00015400   10.29084200   13.62048300

C                 10.40821400   10.41164700    9.94619700

C                 -2.61103300    9.02859000   15.62680600

C                 -0.19579700   10.95894500   14.09077700

H                 -0.24490700   11.87245200   13.92310300

C                  6.55625500    8.45225100   10.88066000

H                  6.33397000    7.60499400   10.56833900

C                  4.57377400    7.00763100   12.25777300

C                  5.68405200    9.11648300   11.74957000

C                  9.32716700   10.97443300   10.52458800

H                  9.38898500   11.88426200   10.70749100

C                 -3.27840200    7.84338900   16.14394700

C                 11.79944600    9.01465100    9.10443500

C                 -1.24276700   10.42229400   14.73919000

C                 12.45027200    7.84939000    8.52422400

C                 11.65495200   11.14576600    9.66958300

C                  3.64653600    6.26828400   11.53652300

H                  3.01077800    6.69872700   11.01170000

C                  2.55232700    8.43095600   13.60459100

H                  2.80337300    7.59649500   13.92974200

C                  8.08334700   10.33478900   10.89473100

C                  5.52861300    6.37476200   13.03894700

H                  6.13970300    6.87594600   13.52902300

C                 -2.40043700   11.18448600   15.21296100

C                 11.74048300    6.64560400    8.48250800

H                 10.88590000    6.59623700    8.84609700

C                 -2.60585700    6.62004900   16.07938800

H                 -1.75561100    6.57507700   15.70528800

C                  3.67431800    4.88774300   11.60389700

H                  3.04419400    4.38801200   11.13702900

C                 -3.20594900    5.47860200   16.57202900

H                 -2.76374400    4.66212600   16.52135800

C                 -4.54907400    7.90456600   16.70909500

H                 -4.99970500    8.71674400   16.75526300

C                 13.73756900    7.91753700    7.99251500

H                 14.21995500    8.71157500    8.03408200

C                 12.30811300    5.53300200    7.90213200

H                 11.84294400    4.72781300    7.88645500

C                  5.56590300    4.98744600   13.08447000

H                  6.21099000    4.55529900   13.59623200

C                 -4.46661100    5.54887700   17.14181200

H                 -4.86126000    4.78012300   17.48540300

C                 13.56914000    5.61353900    7.34360600

H                 13.93536500    4.86844200    6.92447900

C                 -5.14181600    6.75188900   17.20355700

H                 -5.99309900    6.78931100   17.57605100

C                  4.63838900    4.24693700   12.36454500

H                  4.66417400    3.31771100   12.39315000

C                 14.29332300    6.79235100    7.40137800

H                 15.15132500    6.82967600    7.04423000