Supplementary information for

Novel rare earth separation using magnetic susceptibility difference

Liu Chen1, Yongxian Wu1, Hao Chen1, Chunlin He1, Gjergj Dodbiba2, Nguyen Thi Hong Nhung1, Xinpeng Wang1, Yuezhou Wei3, Toyohisa Fujita1*

1 School of Chemistry and Chemical Engineering and College of Resources, Environment and Materials, Guangxi University, School of Resources, Environment and Materials, Guangxi University, Nanning 530004, China,  chenliu@st.gxu.edu.cn (L.C), wuyongxiang7@163.com (Y.W.),  hchen1996@outlook.com (H.C.), helink1900@126.com (C.H.), hnhung_2912@yahoo.com (N.N.), wangxinpeng@gxu.edu.cn (X.W.) fujitatoyohisa@gxu.edu.cn (T.F.)

2 Graduate School of Engineering, The University of Tokyo, Tokyo 113-8656, Japan

dodbiba@g.ecc.u-tokyo.ac.jp (G.D.)

3 School of Nuclear Science and Technology, University of South China, Hengyang, Hunan 421001, China, yzwei@usc.edu.cn (Y.W.)

*Corresponding author. Email: fuitatoyohisa@gxu.edu.cn

This file includes the following:

Fig.S1 to S8

Table S1

Fig. S1. Various rare metal volume magnetic susceptibilities (a) and rare earth oxide volume magnetic susceptibilities (b).

Table S1. Some paramagnetic salt produces paramagnetic liquid.

| Paramagnetic salt | The atomic weight of the molecule (g/mol) | Xs of metal (x10-6 cm3/mol) | Xs/(g/mol) (x10-6 emu/g） | Solubility in H2O (g/100g at 25oC) |
| --- | --- | --- | --- | --- |
| CoCl2 | 129.8 | 12660* | 97.5 | 56.2(CoCl2 6H2O)* |
| MnCl2 | 125.8 | 14350* | 114.0 | 77.3* |
| FeCl2 | 126.8 | 14750* | 116.3 | 65.0* |
| EuCl3 | 222.9 | 26500* | 118.9 |  |
| GdCl3 | 263.6 | 27930* | 106.0 |  |

*(17)

Fig. S2 Magnetization at 1 and 2 T of MnCl2 and GdCl3 paramagnetic aqueous solution depending on density.

Fig. S3  Saturation magnetization of water-based ferrofluid depending on density.

Fig.S4  Magnetization of the matrix of wire and expanded metal (stainless steel SUS 430)

- (B)

Fig.S5. Shear stress and share rate curves depend on the applied magnetic flux density in ferrofluid (A) and MnCl2 paramagnetic aqueous solution (B).

Fig.S6. SEM and size distribution of different rare earth oxide and metal.

(a) La2O3, (b) CeO2, (c) Pr6O11, (d) Nd2O3, (e) Sm2O3, (f) Eu2O3, (g)Gd2O3 ,(h)Tb4O7, (i) Dy2O3, (j) Ho2O3, (k) Er2O3, (l) Tm2O3, (m) Yb2O3, (n) Lu2O3, (o) Sc2O3, (p) Y2O3, (q) Sm metal, (r) Gd metal, (s) Dy metal, (t) Ho metal.

(a)

(b)

(c)

(d)

(e)

(f)

(g)

(h)

(i)

(j)

(k)

(l)

(m)

Fig.  S7. Separation results of two neighboring rare earth particles mixture.

(a) La2O3- CeO2 (b) CeO2-Pr6O11, (c) Pr6O11-Nd2O3, (d) Nd2O3- Sm2O3, (e) Sm2O3- Eu2O3,

(f) Eu2O3- Gd2O3, (g) Gd2O3- Tb4O7, (h) Tb4O7- Dy2O3,  (i) Dy2O3-Ho2O3, Dy-Ho metal

(j) Ho2O3- Er2O3, (k) Er2O3- Tm2O3, (l) Tm2O3 - Yb2O3, (m) Yb2O3-Lu2O3

Water is used in (a) and (b).

Paramagnetic liquid is used in (d) GdCl3 and (m) MnCl2 aqueous solution.

Ferrofluid is used in (c), (d),(e), (f),(g), (h), (i), (j), (k), (l).

(a)

(b)

(c )

Fig. S8. HGMS of two rare earth and oxide mixtures using ferrofluid.

Feed slurry velocity: 78 mm/s, Used liquid: water-based ferrofluid

(a) Eu2O3-Tb4O7 separation, (b) Gd2O3-Sm2O3 separation, (c) Sm-Gd metal separation